Summary of theoretical studies carried out by grand canonical Monte Carlo

simulation for the physisorption of hydrogen on CNF

| Material | Conditions | d-spacing (nm) | H2 Adsorbed (wt%) | Reference |
| --- | --- | --- | --- | --- |
| CNF CNF CNF | -196 °C, 101 bar -73 °C, 101 bar 27 °C, 101 bar | 0.7 1.0 0.7 1.0 1.0 | 4.0 7.0 2.4 2.6 1.2 | (Rzepka et al., 1998) |
| CNF | -196 °C K, 101 bar 25 °C, 101 bar | 0.6 0.9 0.1 0.2 0.6 0.9 0.1 0.2 | 3.0 7.5 9.0 12.5 0.8 1.4 1.6 2.4 | (Wang et al., 1999a; Wang et al., 1999b; Wang et al., 1999c) |
| CNF | 25 °C, 100 bar | 0.3 | 1.5 | (Cracknell, 2001) |

Summary of hydrogen storage capacities of a selection of carbon material recorded

utilsing electrochemical methods

| Sample | Hydrogen Adsorption Measurement | Reference |
| --- | --- | --- |
| Type | Preparation | Doped | H2 Adsorbed (wt%)a | Measurement Method Hydrogen adsorption conditions |  |
| CNT CNT (∅ ~60 nm) SWNT 90 % | Arc-discharge in He CVD, 600 °C, C2H2 using Ni catalyst Laser Ablation Commercial from Smalley | Li Li Li | 0.1 0.6 0.1 0.6 1.6 2.3 | Electrochemical, Ni counter, Ag/AgCl reference, KOH 6M, current 0.4 mA/cm2, 25 °C | (Kibria et al., 2001) |
| SWNT 65 % (∅ 2 nm) | Arc-discharge in H2/Ar |  | 1.8 | Electrochemical, 200 mg carbon, Ni counter, Hg/HgO reference, KOH 6M, current 25 mA/g, 25 °C | (Dai et al., 2002) |

Summary of hydrogen storage capacities of a selection of carbon materials recorded

by volumetric methods

| Sample | Hydrogen Adsorption Measurement | Reference |
| --- | --- | --- |
| Type | Preparation | H2 (wt%)a | Measurement Method |  |
| CNF AC | CVD, 600 °C using C2H4-H2 | 0.01 0.005 | Volumetric direct, 25 °C, 160 bar | (Ahn et al., 1998) |
| CNF | CVD, 550-750 °C using C2H4, CO, H2 with bi-metallic catalysts | 67 (20 hrs) | Volumetric direct, 100-300 mg, 25 °C, 121 bar | (Chambers et al., 1998) |
| CNF | CVD, 550-750 °C using hydrocarbon, CO, H2 with bimetallic transition metal catalysts | 40 | Volumetric direct 500-1000 mg, 25 °C, 110 bar | (Park et al., 1999) |
| CNF (∅ ~90 nm) Demineralised | CVD floating catalyst, 1200 °C using benzene with ferrocene and sulphur | ~13 (4 hrs | Volumetric direct, 200-600 mg, 25 °C, 110 bar | (Fan et al., 1999) |
| SWNT 50 % (∅ ~1.85 nm) | Semi-continuous arc discharge with Ni, Co and Fe Catalysts, Vacuum treated, 500 °C | 4.2 (5 hrs) | 500 mg, 100 bar | (Cheng et al., 2000; Liu et al., 1999) |
| MWNT° ° MWNT | CVD, 700 °C from C2H4 with Ni Annealed to 2200 °C under Ar CVD Floating catalyst from benzene with ferrocene Annealed to 2200 °C under Ar | °0.8° ° °4° | Volumetric direct, 100 mg, 25 °C, 100 bar | (Jia et al., 1999; Li et al., 2001) |
| Aligned MWNT | CVD, 800 °C from xylene with ferrocene | 2.4 | Volumetric direct, 100 mg, 17 °C, 100 bar | (Cao et al., 2001a; Cao et al., 2001b) |
| CNF | From Demco Untreated 300 0C | 0.7 | Volumetric direct, <1000 mg, RT, 120 bar | (Tibbetts et al., 2001) |

Summary of hydrogen storage capacities of a selection of carbon materials recorded

by volumetric methods

| Sample | Hydrogen Adsorption Measurement | Reference |
| --- | --- | --- |
| Type | Preparation | H2 (wt%)a | Measurement Method |  |
| CNF | CVD, 600 °C, Ni-Cu (98:2) catalyst, C2H4 | 15 | Volumetric direct, ~1g, 120 bar, measurement taken on the desorb | (Gupta et al., 2001) |
| CNF (∅ 30-260 nm | CVD, 600 °C from ethylene and Cu5Fe85Ni10 | 6.5(2h) | Volumetric Differential 100 mg, 25 °C, 120 bar | (Browning et al., 2002) |
| CNF (∅ 300 nm) | CVD, 1000 °C using ethylene with nickel catalyst | 4 (3 h) | Volumetric direct, <500 mg, 25 °C, 30-90 bar | (Zhu et al., 2002) |
| CNF (∅ ~90 nm) Demineralised | CVD, 650 °C using CH4 with Ni0.4Mg0.6O, Heat treated, under N2 12000C | 1.4 (40min) | Volumetric direct 500 mg, 25 °C, 120 bar | (Hwang et al., 2002) |
| CNF Demineralised | CVD, 650 °C using C2H4/H2 with Ni-Pd | 0.7 | Volumetric direct, 500 mg, 25 °C, 100 bar | (Lupu et al., 2002) |
| Hydrogenated carbon nitride MWNT | Microwave enhanced plasma CVD Commercial | 0.55 0.22 | Volumetric direct, 400 mg, 27 °C, 120 bar | (Ohkawara et al., 2002) |
| CNT (∅ 10-25 nm) CNT film | Arc-discharge CVD from C2H2 using silicon support | 0.22 (35 hrs) 8.0 (60 hrs) | Volumetric direct with 167 mg, 1.1 bar 9 mg, 1.1 bar | (Wang et al., 2002) |
| Ball Milled Graphite Rods | Commercial vacuum annealed Graphite rods, Ball milled | 0.7 | Volumetric direct, 2000 mg, -196 °C, 51 bar | (Awasthi et al., 2002) |
| CNF AC MSC-30 | CVD, 600 °C using C2H4/H2 (1:1) with Cu-Fe (1:1) Maxorb Commercial | 0.27 0.057 | Volumetric direct, 500 mg, 35 ± 0.2 °C, 100 bar | (Kiyobayashi et al., 2002) |
| MWNT 70 %(∅5 nm) Demineralised | CVD Floating catalyst, 1100 °C from benzene with ferrocene annealed at 1000 °C under Ar | 6.5 | Volumetric direct, 300 mg, 23 °C, 145 bar | (Hou et al., 2002) |
| MWNT (∅ ~20-30 nm) | CVD, 750 °C, silica supported Co catalyst | 3.2 | Volumetric direct, 1 g, ~20 °C, 120 bar | (Huang et al., 2002) |

Summary of hydrogen storage capacities of a selection of carbon materials recorded

utilising TPD methods

| Sample | Hydrogen Adsorption Measurement | Reference |
| --- | --- | --- |
| Type | Preparation | H2 Adsorbed (wt%)a | Measurement Method Hydrogen adsorption conditions |  |
| Soot containing SWNT 0.2 % cobalt 20 % | Co-evaporation of graphite and cobalt in an electric arc | Projected 5-10 wt% | TPD, 1 mg, 0.4 bar, 0 °C then -140 °C (desorption peaks -123 °C) | (Dillon et al., 1997) |
| Carbon nitride nanobells | Microwave plasma CVD of CH4 /N2 on a silicon substrate | 8 | TPD, QMS, 10 mg | (Bai et al., 2001) |
| Nanostructured Graphite | Commercial graphite, ball milled under hydrogen | 8 | TPD (desorption peaks 423-727 °C) | (Orimo et al.,2001) |
| CNT bundles and peapodsb washing | Nd laser ablation, 1200 °C, using Ni/Co catalysts purified by H2O2 reflux and NaOH washing | 0.01 | TPD, 0.1 and 6 MPa (desorption peaks 77 °C) | (Shiraishi et al., 2002) |
| SWNT CNF Graphite | Arc discharge using Ni and Y catalysts (50 %wt) Ball milled under D2 CVD using ferrocene ball milled under D2 Commercial, ball milled under D2 | 1 0.5 0.3 | D2 TPD, 0.08 MPa (desorption peaks 427-527 °C) | (Hirscher et Al., 2002) |
| CNF (∅ 50-200 nm) MWNT (∅ 10-40 nm) SWNT 90 % | CVD using ethylene and Co-Fe catalyst CVD Floating catalyst using benzene and ferrocene catalyst CVD, 1050 °C using ethylene and Co-Fe catalyst on MgO thin film | 0.05 0.18 0.63 | TPD, 20 mg, 45 bar, 25 °C TPD, 20 mg, 45 bar, 25 °C TPD, 20 mg, 45 bar, 25 °C | (Ritschel et al., 2002) |

Summary of hydrogen storage capacities of a selection of carbon materials recorded

by the gravimetric methods

| Sample | Hydrogen Adsorption Measurement | Reference |
| --- | --- | --- |
| Type | Preparation | H2 (wt%)a | Measurement Method |  |
| Isothermal Temperature Gravimetric |
| CNF (∅ ~100 nm) AC | CVD (no further details) Commercial | 1.2 1.6 | Isothermal Gravimetric, <100 mg, 125 bar, 23 °C | (Strobel et al., 1999) |
| CNT (∅~50-100 nm) | Plasma assisted hot filament CVD, tube ends opened, demineralised | 13.8 | Isothermal Gravimetric ~70 mg, ~10 bar, ~20 °C (desorption peaks 120-170 °C) | (Chen et al., 2001 |
| N2 doped graphite nanoparticles | Microwave enhanced plasma CVD of CH4/H2/N2, ~1000 °C | 0.8 | Isothermal Gravimetric ~100 mg, ~2 bar, ~20 °C | (Badzian et al., 2001 |
| AC | AC From anthracite | 1.0 | Isothermal Gravimetric <100 mg, 100 bar, 20 °C | (de la Casa- Lillo et al., 2002 |
| Dynamic Temperature Gravimetric |
| CNT Li-doped (∅ 25-35 nm) CNT K-doped (∅ 25-35 nm) | CVD from CH4, demineralised, doped by solid state reaction using Li and K salts | 20 14 | Dynamic temperature Gravimetric, <100 mg, 1 bar, max H2 adsorbed at 600 °C and 27 °C for Li and K doped respectively | (Chen et al., 1999) |
| MWNT (∅ 5-25 nm) | CVD from CO or CH4 and Co-La2O3 catalyst, Demineralised with nitric acid | 0.25 | Dynamic temperature Gravimetric, <100 mg, 1 bar | (Wu et al., 2000) |
| MWNT CVD | from CH4 and Ni0.4Mg0.6 catalyst, demineralised | 0.6 | Dynamic temperature Gravimetric, 20 mg, 1 bar | (Lueking et al., 2002) |