CHAPTER – 2

Surface Analytical Techniques- An Overview

The analysis of surface starts with defining what a surface is?  Generally, it is considered that the top 4 – 5 layers or top 10 Ǻ depth is considered to be the surface since coordinative unsaturation and variations in configurations can be seen only in these layers.  It is usual to list out the available techniques in tabular form.   However, since this will not give the whole and picture, a method based on input/output probes has been adopted..  There are generally four particle beams, namely electrons, ions, neutrals and photons and there are four other fields, namely thermal, electrical, magnetic and  surface sonic waves that can be used as input probes.  When one employs any one of these eight probes, they give rise to emission or transmission or scattering of the four particle beams (except the magnetic field) namely electrons, ions, neutrals and photons.  These particles carry information of the surface to a suitable detector.  The detector assembly can be tuned to count the number of particles emitted (intensity), or it can  be tuned to identify the chemical nature of the species emitted in the case of ions and neutrals or can be made to analyse the energy or angular distribution of the particles emitted. Any or all of these four types of information on the emitted particles are used to develop better understanding of the surface under study.

The combination of the 8 different types of input probes with four different output probes on which four different types of information can be gathered give rise to the multitude of techniques. A pictorial representation of this model of generating all the techniques is given in Fig. 2.1. A listing of the possible techniques and their acronyms are given in Appendix 2.1.

It can be demonstrated that most of the surface analytical techniques can be rationalized in terms of input and output probes. Consider the case of electrons-in (electrons used as input probe) which can give rise to all the four particle beams. It is generally believed that it is always simple and easily  feasible  if the same particle is considered as the output probe.

Fig.  2.1. A pictorial representation of generating the possible techniques in terms of input and out put probes

Fig. 2.2.  Representation of the techniques based on Electrons in – electron, ion, neutral and photon out  LEED:  Low Energy Electron Diffraction;  HEED: High Energy Electron diffraction;  RHHED:  Reflected High Energy Electron Diffraction; ILEED: Ineleastic Low Energy Electron Diffraction; AES: Auger Electron Spectroscopy; EELS: Electron Energy Loss Spectroscopy; EIID: Electron Induced Ion Desorption;  SEPSMS: Electron Probe Surface Mass Spectrometry; EID: Electron Induced Desorption; SDMM: Surface Desorption Molecular Microscope; CIS: Characteristic Isochromat Spectroscopy; APS: Appearance Potential Spectroscopy.

Fig. 2.3.   Schematic representation of the techniques that can be generated from Photon- in  photon, neutral, electron or ion-out methodology.  XPS: X ray Photoelectron Spectrroscopy; ESCA: Electrons Spectroscopy for Chemical Analysis.

For a conceptual understanding a simple representation is given in Fig. 2.2 for the surface analytical techniques that are possible from using electrons as input probes and all the four particle beams as out put probes.  A similar representation is possible for other combinations as well. Some of these are pictorially shown in Fig. 2.3 and Fig. 2.4.  A simple compilation of some of the important surface analytical techniques, their basis and the type of information that can be obtained is given in Table 2.1.

The purpose of this presentation is not to consider the fundamentals of these techniques as several authoritative compilations are available on them. The  focus will be on the applications of some of these techniques in handling the problems in catalysis

Fig. 2.4.   Schematic representation of the techniques that can be generated from Ions-in  ion-, neutral-, electron- or photon-out methodology.  ISS: Ion Scattering Spectroscopy, SIMS: Secondary Ion Mass Spectrometry, INS: Ion Neutralization Spectroscopy, PIX: Proton Induced X ray emission.

It is desirable to deal in detail with the various applications of the surface and bulk analyticatechniques and show in which situation, which technique will provide the appropriate information required.   However, such an exercise will be out of reach for any single volume.   Hence in this volume only a few selected techniques are taken up for  consideration.   Even in these cases the examples chosen do not cover the entire spectrum of possibilities.

Table 2.1 Typical information that can be obtained employing surface analytical techniques and the possible limitations of these techniques

| Surface Analytical technique | Typical applications | Signal detected | Elements detected | Detection limits | Depth resolution | Imaging/ Mapping possibility | Lateral resolution (Probe size) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Auger spectroscopy | Elemental analysis, depth profiling | Atomic scale roughness | Li-U | - | 206nm | yes | 100 nm |
| Rutherford Back scattering (RBS) | Quantitative think film composition | Backscattered He atoms | Li-U | 1-10 at% (for Z<20)0.01-1 at % for X 20-70 | 2-20 nm | yes | 2 mm |
| Secondary Ion Mass Spectrometry | Dopant and impurity depth profiling, microanalysis | Secondary ions | H-U | ppb/ppm | <5 nm | yes | <5 micron imaging <30 micron depth profiling |
| X-ray Photoelectron Spectroscopy | Surface analysis both inorganic and organic | Photoelectrons | Li-U | 0.01-1 at% | 1-10 nm | yes | 10μm -2μ |
| X ray Fluorescence | Thin film thickness composition | X-rays | Na-U | 10 ppm | - | no | 100μm |
| Low Energy Electron Diffraction | Surface structure adsorbate structure | Elastic back scattering of low energy electrons | Only geometry | submonolayer | - | yes | Atomic dimensions |
| High Resolution Electron Energy Loss Spectroscopy | Structure and bonding of surface atoms and adsorbates | Vibrational excitation of surface atoms adsorbates by inelastic low energy electrons | All adsorbate molecuels | Sub monolayer | - | - | Observation of direct adsorbate-adsorbent bond |
| Infra red absorption spectroscopy | Structure and bonding of adsorbates | Vibrational excitation of surface bonds | Adsorbates internal bonds | Sub monolayer | - | - | - |
| Ion Scattering Spectroscopy | Atomic structure composition | Elastic reflection of inert gas ions | Any element mass dependent | - | possible | possible | Atomic dimensions |
| Extended X ray Absorption Fine structure | Atomic structure of surface atoms and adsorbates | Interference effects in photo-emitted electron wave function in x-ray absorption. | Mostly all species | Intermediate- coordination | - | possible | Atomic dimensions |
| Thermal Desorption Spectroscopy | Adsorption energy | Thermally induced desorption or decomposition of adsorbates | All species | Sub monolayer | Not normally done | - | No |

Appendix 2.1

Partial listing of the surface Analytic Techniques with the appropriate acronym.

| Acronym | Technique |
| --- | --- |
| AEAPS | Auger Electron Appearance Potential Spectroscopy |
| AES | Auger Electron Spectroscopy |
| AFM | Atomic Force Microscopy |
| APECS | Auger Photoelectron Coincidence Spectroscopy |
| APFIM | Atom Probe Field Ion Microscopy |
| APS | Appearance Potential Spectroscopy |
| ARPES | Angle Resolved Photoelectron Spectroscopy |
| ARUPS | Angle Resolved Ultraviolet Photoelectron Spectroscopy |
| ATR | Attenuated Total Reflection |
| BEEM | Ballistic Electron Emission Microscopy |
| BIS | Bremsstrahlung Isochromat Spectroscopy |
| CFM | Chemical Force Microscopy |
| CHA | Concentric Hemispherical Analyzer |
| CMA | Cylindrical Mirror Analyzer |
| CPD | Contact Potential Difference |
| CVD | Chemical Vapour Deposition |
| DAFS | Diffraction Anomalous Fine Structure |
| DAPS | Disappearance Potential Spectroscopy |
| DRIFT | Diffuse Reflectance Infra-Red Fourier Transform |
| EAPFS | Extended Appearance Potential Fine Structure |
| EDX | Energy Dispersive X-ray Analysis |
| EELS | Electron Energy Loss Spectroscopy |
|  | Electron induced luminescence |
|  | Ellipsometry |
| EMS | Electron Momentum Spectroscopy |
| EPMA | Electron Probe Micro-Analysis |
| ESDMS | Electron Stimulated Desorption Mass Spectrometry |
| ESCA | Electron Spectroscopy for Chemical Analysis |
| ESD | Electron Stimulated Desorption |
| ESDIAD | Electron Stimulated Desorption Ion Angle Distributions |
| EXAFS | Extended X-ray Absorption Fine Structure |
| FEM | Field Emission Microscopy |
| FIM | Field Ion Microscopy |
| FTIR | Fourier Transform Infra Red |
| FTRA-IR | Fourier Transform Reflectance-Absorbtion Infra Red |
| HAS | Helium Atom Scattering |
| HDA | Hemispherical Deflection Analyser |
| HEIS | High Energy Ion Scattering |
| HREELS | High Resolution Electron Energy Loss Spectroscopy |
| IETS | Inelastic electron tunnelling spectroscopy |
| KRIPES | k-Resolved Inverse Photoemission Spectroscopy |
| ILS | Ionisation Loss Spectroscopy |
| INS | Ion Neutralisation Spectroscopy |
| IPES | Inverse Photoemission Spectroscopy |
| IRAS | Infra-Red Absorption Spectroscopy |
|  | Ion Excited Auger Electron Spectroscopy |
| ISS | Ion Scattering Spectroscopy |
| LEED | Low Energy Electron Diffraction |
| LEEM | Low Energy Electron Microscopy |
| LEIS | Low Energy Ion Scattering |
| LFM | Lateral Force Microscopy |
| MBE | Molecular Beam Epitaxy |
| MBS | Molecular Beam Scattering |
| MCXD | Magnetic Circular X-ray Dichroism |
| MEIS | Medium Energy Ion Scattering |
| MFM | Magnetic Force Microscopy |
| MIES | Metastable Impact Electron Spectroscopy |
| MIR | Multiple Internal Reflection |
| MOCVD | Metal Organic Chemical Vapour Deposition |
| MOKE | Magneto-Optic Kerr Effect |
| NEOM | Near Field Optical Microscopy |
| NIXSW | Normal Incidence X-ray Standing Wave |
| NEXAFS | Near-Edge X-ray Absorption Fine Structure |
| NSOM | Near Field Scanning Optical Microscopy |
| PAES | Positron annihilation Auger Electron Spectroscopy |
| PECVD | Plasma Enhanced Chemical Vapour Deposition |
| PEEM | Photo Emission Electron Microscopy |
| PhD | Photoelectron Diffraction |
|  | Photon Excited Auger Electron Spectroscopy |
| PIXE | Proton Induced X-ray Emission |
|  | Raman Spectroscopy |
| PSD | Photon Stimulated Desorption |
| RAIRS | Reflection Absorbtion Infra-Red Spectroscopy |
| RAS | Reflectance Anisotropy Spectroscopy |
| RBS | Rutherford Back Scattering |
| RDS | Reflectance Difference Spectroscopy |
| REFLEXAFS | Reflection Extended X-ray Absorption Fine Structure |
| RFA | Retarding Field Analyser |
| RHEED | Reflection High Energy Electron Diffraction |
| RIFS | Reflectometric Interference Spectroscopy |
| SAM | Scanning Auger Microscopy |
| SEM | Scanning Electron Microscopy |
| SEMPA | Scanning Electron Microscopy with Polarization Analysis |
| SERS | Surface Enhanced Raman Scattering |
| SEXAFS | Surface Extended X-ray Absorption Spectroscopy |
| SHG | Second Harmonic Generation |
| SH-MOKE | Second Harmonic Magneto-Optic Kerr Effect |
| SIMS | Secondary Ion Mass Spectrometry |
| SKS | Scanning Kinetic Spectroscopy |
| SMOKE | Surface Magneto-Optic Kerr Effect |
| SNMS | Sputtered Neutral Mass Spectrometry |
| SNOM | Scanning Near Field Optical Microscopy |
| SPIPES | Spin Polarised Inverse Photoemission Spectroscopy |
| SPEELS | Spin Polarised Electron Energy Loss Spectroscopy |
| SPLEED | Spin Polarised Low Energy Electron Diffraction |
| SPM | Scanning Probe Microscopy |
| SPR | Surface Plasmon Resonance |
| SPURS | Spin Polarised Ultraviolet Photoelectron Spectroscopy |
| SPXPS | Spin Polarised X-ray Photoelectron Spectroscopy |
| STM | Scanning Tunnelling Microscopy |
| SXAPS | Soft X-ray Appearance Potential Spectroscopy |
| SXRD | Surface X-ray Diffraction |
|  | Synchrotron Radiation Photoelectron Spectroscopy |
| TDS | Thermal Desorption Spectroscopy |
| TEAS | Thermal Energy Atom Scattering |
| TIRF | Total Internal Reflectance Fluorescence |
| TPD | Temperature Programmed Desorption |
| TPO | Temperature Programmed Oxidation |
| TPRS | Temperature Programmed Reaction Spectroscopy |
| TPS | Temperature Programmed sulphidation |
| TXRF | Total Reflection X-ray Fluorescence |
| UHV | Ultra High Vacuum |
| UPS | Ultraviolet Photoemission Spectroscopy |
| XANES | X-ray Absorption Near-Edge Structure |
| XAES | X-ray Induced Auger Electron Spectroscopy |
| XPD | X-ray Photoelectron Diffraction |
| XPS | X-ray Photoemission Spectroscopy |
| XRR | X-ray Reflectometry |
| XSW | X-ray Standing Wave |

This compilation is mostly reproduced from http://www.uksaf.org/tech/list.html.