## Slide 1
1D compounds of Mo/W for electrochemcial applications

## Slide 2
Y. Wang et al., Applied Energy 88 (2011) 981-1007
Fuel Cell Cost Breakdown
2015 DOE target for Pt loading, ~ 0.2 mg/cm2 , with a performance of 650W/L
High cost and durability – barriers for commercialization

## Slide 3
Fuel Cell Cost Breakdown
Rajesh K. Ahluwalia and X. Wang, J. Power Sources 177 (2008) 167-176

## Slide 4
Objective: Development of low cost, high performance
electrode materials for methanol oxidation, oxygen reduction
reaction, hydrogen evolution reaction and
electrochemical capacitors
Approach: Low cost nanomaterials are synthesized from
simple synthetic procedures
Objective: It is preliminary requisite to understand the
fundamental properties of the catalysts before employing
them in a realistic environments such as fuel cell and
capacitor devices
Approach: To achieve this, half cell reactions are performed.
Conduct fundamental studies of the developed nanomaterials
Catalyst activities for methanol oxidation, ORR, etc..
Objectives and Approaches

## Slide 5
Work at National Centre for Catalysis Research, India
Syntheses of Nanomaterials
Nanorods of WO3, MoO2 and MoxVyOz
MoS2 nanotube and WS2 nanomaterial
Fuel Cell - Methanol oxidation and
Oxygen reduction reaction
WO3 nanorod as supports for PGM electrocatalyst
Reduce the loading of PGM
Prevent carbon corrosion in fuel cell conditions
Diagnostics
TEM
SEM
XRD
Electrochemical Studies
Energy Storage –
Electrochemical capacitors
Chronopotentiometry and CV
WO3 nanorods and MoO2 nanorods
Hydrogen Evolution Reaction
WO3 nanorods
MoS2 nanotubes

## Slide 6
Approach: Nanorod Synthesis
Method: Thermal decomposition of tetrabutylammonium
salts of metal oxides
Precursor method: Preparation methods from literature
Precursors: ((C4H9)4)N)4W10O32, ((C4H9)4)N)2Mo6O19,
((C4H9)4)N)4PMo10V2O40
Metal oxide nanorods: WO3, MoO2 and MoxVyOz
Metal Sulfide nanotube and nanomaterial: WS2 and MoS2
A. Chemseddine, C. Sanchez, J. Livage, P. Launay, M. Fournier, Inorg. Chem. 23 (1984) 2609.
M. Che, M. Fournier, J.P. Launay, J. Chem. Phys. 71 (1979) 1954.

## Slide 7
Approach: WO3Nanorod Synthesis
5 nm
Tungsten oxide nanorods
Precursor, ((C4H9)4)N)4W10O32
XRD of Tungsten oxide nanorods

## Slide 8
5 nm
Approach: MoO2 Nanorod Synthesis
Width : 20- 50 nm; Length : 5-10 m
Interplanar spacing :0.17 nm corresponds to (022) plane of monoclinic MoO2

## Slide 9
Approach: MoxVyOz Nanorod Synthesis
Precursor: ((C4H9)4)N)4PMo10V2O40
Orthorhombic MoO3 (JCPDS: 89-5108)
Tetragonal VO2 (JCPDS: 76-0678)

## Slide 10
Approach: MoS2 Nanotube Synthesis
Treatment of MoO2 nanorods with H2S
Diameter of the nanotube: ~ 60 nm, Inner diameter: 15 nm; Length: ~ 550 nm to 1 m

## Slide 11
Approach: WS2 Nanotube Synthesis
Short nanorods: 20-40 nm length and
8-20 nm width
Irregular shaped nanoparticles
Interplanar spacing: 0.61 nm - (003) plane
of WS2

## Slide 12
Approach: Methanol Oxidation Electrocatalysts
Catalyst: Platinum (H2PtCl6 precursor)
Catalyst supports: WO3 nanorods (represented as WO3NR), WO3NR-CNT,
WO3NR-C (vulcan XC) and WO3B (commercial WO3)
Method for metal reduction: Hydrogen reduction at 450 C
50 nm
Pt/WO3(NR)
Pt/WO3(NR)-CNT
Pt/WO3(NR)-C

## Slide 13
Electrocatalyst | Current density (mA cm-2) | Mass activity (mA mg-1)
(a) 20%Pt/WO3(NR) | 211 | 295
(b) 20% Pt-Ru/C (J. M) | 192 | 268
(c) 20%Pt/WO3 | 35 | 49
1M CH3OH – 1M H2SO4 at a scan rate of 25mVs-1
1M CH3OH – 1M H2SO4 at 0.7 V
J. Rajeswari, B. Viswanathan, T.K. Varadarajan, Mater. Chem. Phys.106 (2007) 168
<
<
<
<
<
<
Technical Accomplishment: Electrochemical Methanol Oxidation
Improved activity for WO3 NR supported catalyst

## Slide 14
Electrocatalyst | Current density (mA cm-2) | Mass activity (mA mg-1)
20% Pt/WO3(NR)-CNT | 322 | 452
20% Pt/WO3(NR)-C | 272 | 382
20% Pt/C | 130 | 180
1M CH3OH – 1M H2SO4 at a scan rate of 25mVs-1
1M CH3OH – 1M H2SO4 at 0.7 V
<
<
<
<
<
<
Technical Accomplishment: Electrochemical Methanol Oxidation
Improved activity for WO3 NR supported catalyst

## Slide 15
Electrocatalyst | Mass activity (mAmg-1) | Specific activity (mAcm-2)
Pt/WO3(NR)-C | 3.83 | 5.45
Pt/WO3-C | 2.42 | 3.44
Pt/C | 1.91 | 2.72
0.5 M H2SO4, Scan Rate: 5 mVs-1 (solid line: O2- saturated and dashed line: Ar- saturated)
Technical Accomplishment: Oxygen Reduction Reaction
Improved activity for WO3 NR supported catalyst
Pt/WO3(NR)-C
Pt/WO3-C
Pt/C

## Slide 16
Technical Accomplishment: Hydrogen Evolution Reaction
Low cost, non noble catalyst materials
1 M H2SO4 at 5 mVs-1
(a)
(b)
(c)
Electrocatalyst | HER activity (mAcm-2)
(a) 20% Pt/WO3(NR)-C | 185
(b) 20% Pt/WO3-C | 135
(c) 20% Pt/C | 110
Current density at -0.8 V,
WO3(NR): 23 mAcm-2
commercial WO3: 15 mAcm-2
(c) bare glassy carbon electrode

## Slide 17
Material | Activity (mAcm-2) | Onset Potential (V)
MoS2 nanotubes | 37.4 | -0.22
Bulk MoS2 | 13.7 | -0.32
Technical Accomplishment: Hydrogen Evolution Reaction
Low cost non noble catalyst materials

## Slide 18
Electrochemical Capacitors-
Specific capacitance from cyclic voltammetry
WO3NR
WO3B
Specific capacitance, C = i /( x m), where i is the current density,  is the scan rate
and m is the weight of the active material
Specific capacitance for WO3NR:
2 mVs-1: 266 Fg-1
5 mVs-1 : 198 Fg-1
Specific capacitance for commercial WO3:
2 mVs-1: 36 Fg-1
5 mVs-1: 28 Fg-1

## Slide 19
Potential range (V) | Specific capacitance of WO3 (Fg-1) | Specific capacitance of WO3(NR) (Fg-1)
-0.5 to + 0.2 | 56 | 435
-0.4 to + 0.3 | 35 | 292
-0.3 to + 0.4 | 14 | 190
-0.2 to + 0.5 | 10 | 98
J. Rajeswari, B. Viswanathan, T. K. Varadarajan, Indian Pat. Appl. (2007) 1488 CHE
Electrochemical Capacitors- WO3 nanorods
Specific capacitance from galvanostatic charge-discharge studies
Current density (mAcm-2) | Specific capacitance (Fg-1)
3 | 56
5 | 29
7 | 20

## Slide 20
Mo4+  Mo6+ ~ 0.2 V vs. Ag/AgCl
H. Zhang, Y. Wang, E.R. Fachini, C.R. Cabrera, Electrochem. Solid-state Lett. 2 (1999) 437
Current density (mAcm-2) | Specific capacitance (Fg-1)
1 | 140
3 | 115
5 | 30
Electrolyte: 1M H2SO4; scan rate: 5 mVs-1
Electrolyte: 1M H2SO4
Electrochemical Capacitors- MoO2 nanorods

## Slide 21
Summary and Overview
Relevance: Focussed on overcoming the most significant barrier for
commercialization – high cost of PGM catalysts and electrodes for
fuel cells and electrochemical capacitors
Approach: Development of simple method to synthesize low cost metal
oxides and metal sulfides nanomaterials such as nanorods, nanotubes, etc..
Conducted fundamental electrochemical studies in a half cell reaction mode
to understand the catalyst properties for above mentioned applications
Accomplishments: Electrochemical activity, in terms of mass, showed the
potential to reduce Pt loading for methanol oxidation and ORR and
Possibility to use non PGM electrode materials for HER and
electrochemical supercapacitors
Future work: Catalysts have to be tested in a single cell fuel cell