## Slide 1
Photo-electrochemical decomposition of water and storage of hydrogen
B. Viswanathan
National Centre for Catalysis Research
Indian Institute of Technology Madras,
Chennai-600 036
One of the programs of NCCR – funded by Government agencies like DST, MNRE and private agencies like Tata Chemicals -Our grateful thanks to these agencies

## Slide 2: Some Other Areas of Research
Electro-catalytic reduction of carbon dioxide (in cooperation with chemical Engineering Department)
Electrode materials for fuel cell especially for ORR ( in cooperation with laboratories in South Korea)
Solar Hydrogen ( with a consortium of laboratories like IITK, BARC, Dayalbagh, (Agra) CECRI and IIT, Rajesthan).
Encapsulation of active sites in Zeolites ( with University of Madras)
and so on……………….!

## Slide 3: Situation and Questions
Production, storage and application - challenges of hydrogen economy
Solid state storage – remarkable but not reproducible
6.5 wt% - desired level (DOE)
Demands consistent and innovative practice
(i) How to select appropriate materials for PEC of water!
Are the carbon materials appropriate for solid state hydrogen storage?
If this were to be true, what type of carbon materials or what type of treatments for the existing carbon materials are suitable to achieve desirable levels of solid state hydrogen storage?
What are the stumbling blocks in achieving the desirable solid state hydrogen storage?
Where does the lacuna lie? Is it in our theoretical foundation of the postulate or is it in our inability to experimentally realize the desired levels of storage?

## Slide 4
Small band gap – to absorb up to 600 nm
Ability to work without sacrificial agents
Low cost
High quantum yields
High efficiency without expensive co-catalysts such as Pt, Ru
Long term stability
Compounds with environmentally friendly elements
Direct band gap i.e. better light absorption
Desired properties of an ideal semiconductor photocatalyst

## Slide 5
Distribution of scientific publications focusing on materials for photo-catalytic H2 production
J. Zhu, M. Zach, Curr. Opin. Colloid. In., 14 (2009) 260
Percent contribution of various materials for water splitting

## Slide 6
Choice of constituent metal ions present in materials as photocatalysts
Materials containing elements in d0 or d10 configuration
J. Zhu, M. Zach, Curr. Opin. Colloid. In., 14 (2009) 260
Elements with d0 and d10 metal ions- suitable as photo-catalysts
Partially filled d-orbitals - higher recombination
Materials with d10 ions - smaller band gaps

## Slide 7
Binary oxide photo-catalysts
Catalyst | Pros | Cons
TiO2 | Highly active and stable | Works only in UV light
ZnO | Considerably active | Suffers photo-corrosion ; works only in UV light
CeO2 | Works in visible light | Considerably less active than TiO2
WO3 | None | Cannot evolve H2 ; Less active than TiO2; Inactive in UV light
SnO2 | None | Less active than TiO2 ; Inactive in UV light
Fe2O3 | Works in visible light | Cannot evolve H2
Bottom of CB - d and sp orbitals metal cations
Top of VB - O 2p orbitals
O 2p orbials normally located at ~+3 V (vs NHE) or higher
Alonso et al., Energy Environ. Sci., 2 (2009) 1231

## Slide 8
Binary sulfide photo-catalysts
Catalyst | Advantages | Disadvantages
CdS | Smaller band gap; can evolve H2 | Photo-corrosion
ZnS | Can evolve H2 | Large band gap ; Photo-corrosion
AgInS2, CdInS4, SnInS4, AgIn5S8 | Small band gap; Can evolve H2 | Photo-corrosion
VB - more negative potential due to S 3p orbitals
Most sulfide conduction bands lower in energy than H2 evolution potential
Suffer from photo-corrosion
Sacrificial agents (S2-/SO32-) required to prevent photo-corrosion

## Slide 9
Comparison of band position of various sulfides and oxides
Xu and Schoonen, Am. Mineral., 85 (2000) 543
Sulfides have VB at higher energy due to S 3p
Most have smaller band gap
Most cant evolve H2
Oxides have VB at lower energy
Most have large band gap
Hence can evolve H2

## Slide 10
Ternary and quarternary metal oxides with d0 metal ions
Oxides with d0 ions - larger band gaps
Only O 2p orbitals contributing to VB top - lower energy VB
CB positions suitable to evolve H2
Most Ta, Nb and Ti oxides - larger band gaps due to d0 configuration
Catalyst | Advantages | Disadvantages | Example
Ta and Nb oxides | Evolve H2 and O2 | Large band gap | ATaO3 (A – Li, Na, K), NaTaO3, K4Nb6O17
Ti oxides | Evolve H2 and O2 | Large band gap | Sr3Ti2O7, SrTiO3, La2Ti2O7, K2La2Ti3O10
Vanadium oxides | Can absorb visible light | Cannot evolve H2 | M3V2O8 (M = Mg, Ni, Zn)

## Slide 11
Ternary and quarternary metal oxides with d10 metal ions
d10 metal ions - smaller band gaps
d10 hybridize with O 2p to form top of VB
VB top at higher energy than d0
These oxides mostly contain Bi, Ag, In and Sb
Not all evolve H2 - lower CB positions
Catalyst | H2 evolution | Visible light activity | Example
Indium oxides | Yes | Yes | InVO4
Bismuth oxides | No | Yes | BiVO4, Bi2WO6, Bi2MoO6
Zn oxides | Yes | No | ZnFe2O4, ZnCr2O4
Silver oxides | Yes | Yes | AgInW2O8, Ag2ZnGeO4

## Slide 12
Metal oxysulfides, oxynitride and nitrides
VB top contains N 2p or hybridized N 2p/S 3p and O 2p
VB higher in energy than oxides
Oxysulfides, oxynitrides and nitrides of d0 and d10 metals have shorter band gaps
Ex. TaON, Ge3N4, (Ga1−XZnX)(N1−XOX), LaTiO2N, SrTiO3-2xNx, NaTaO3xNx
Most are capable of evolving H2 using visible light
K. Maeda, K. Domen, Chem. Mater., 22 (2010) 612

## Slide 13
Generation of bands in solids from atomic orbitals of isolated atoms
Fermi level - Level where probability of an electron is ½
Instrinsic semiconductor - Fermi level lies at mid-point of band gap
n-type semiconductor - lies just below CB
p-type semiconductor - just above VB
Fermi level of semiconductor varies with applied potential
Electronic structure of materials

## Slide 14: Photo-electrochemical hydrogen production at illuminated semiconductor electrodes
Photo-electrochemical energetics of semiconductors
Dye-sensitised photovoltaic cell

## Slide 15
Photocatalysis
Conventional redox reaction
Oxidizing agent should have more positive potential
Photocatalysis - simultaneous oxidation and reduction
The redox couple capable of promoting both the reactions can act as photocatalyst
Metals, Semiconductors and Insulators
reaction assisted by photons
catalyst
15
Metals
VB
CB
VB
CB
VB
CB
H+/H2
H2O/O2
Insulators
SC
E
WHY SEMICONDUCTOR ?
Metals : No band gap
Only reduction or oxidation
Depends on the band position
Insulators : High band gap
High energy requirement

## Slide 16: Ionic character of M-O bond
Ionic solids as the ionicity of the M-O bond increases, the top of the valence band (mainly contributed by the p- orbitals of oxide ions) becomes less and less positive (since the binding energy of the p orbitals will be decreased due to negative charge on the oxide ions) and the bottom of the conduction band will be stabilized to higher binding energy values due to the positive charge on the metal ions which is not favourable for the hydrogen reduction reaction.
More ionic the M-O bond of the semiconductor is, the less suitable the material is for the photo-catalytic splitting of water. The bond polarity can be estimated from the expression
Percentage ionic character (%) =
The percentage ionic character of the M-O bond for some of the semiconductors
Semiconductor | M-O | % ionicity
TiO2 SrTiO3 Fe2­O3 ZnO WO3 CdS CdSe LaRhO3 LaRuO3 PbO ZnTe ZnAs ZnSe ZnS GaP CuSe BaTiO3 MoS2 FeTiO3­ KTaO3 MnTiO3 SnO2 Bi2O3 | Ti-O Ti-O-Sr Fe-O Zn-O W-O Cd-S Cd-S La-O-Rh La-O-Ru Pb-O Zn-Te Zn-As Zn-Se Zn-S Ga-P Cu-Se Ba-O-Ti Mo-S Fe-O-Ti K-O-Ti Mn-O-Ti Sn-O Bi-O | 59.5 68.5 47.3 55.5 57.5 17.6 16.5 53.0 53.5 26.5 5.0 6.8 18.4 19.5 3.5 10.0 70.8 4.3 53.5 72.7 59.0 42.2 39.6

## Slide 17
Photodecomposition of water
Photocatalytic formation of fuel
Photocatalysis in pollution abatement
TYPICAL PHOTOCATALYTIC PROCESS
17

## Slide 18: HYDROGEN PRODUCTION
There are various methods and technologies that have been developed and a few of them have already been practiced. These technologies can be broadly classified as:
Thermo-chemical routes for hydrogen production
Electrolytic generation of hydrogen
Photolytic means of hydrogen formation
Biochemical pathways for hydrogen evolution and
Chemical (steam ) reformation of naphtha
18

## Slide 19
Identifying and designing new semiconductor materials with considerable conversion efficiency and stability
Constructing multilayer systems or using sensitizing dyes - increase absorption of solar radiation
Formulating multi-junction systems or coupled systems - optimize and utilize the possible regions of solar radiation
Developing nanosize systems - efficiently dissociate water
THE AVAILABLE OPPORTUNITIES
19

## Slide 20: Limited success – Why?
The main reasons for this limited success in all these directions are due to:
The electronic structure of the semiconductor controls the reaction and engineering these electronic structures without deterioration of the stability of the resulting system appears to be a difficult proposition.
The most obvious thermodynamic barriers to the reaction and the thermodynamic balances that can be achieved in these processes give little scope for remarkable improvements in the efficiency of the systems as they have been conceived and operated. Totally new formulations which can still satisfy the existing thermodynamic barriers have to be devised.
The charge transfer processes at the interface, even though a well studied subject in electrochemistry has to be understood more explicitly, in terms of interfacial energetics as well as kinetics. Till such an explicit knowledge is available, designing systems will have to be based on trial and error rather than based on sound logical scientific reasoning.
20

## Slide 21
Nanocrystalline (mainly oxides like TiO2, ZnO, SnO and Nb2O5 or chalcogenides like CdSe) mesoscopic semiconductor materials with high internal surface area If a dye were to be adsorbed as a monolayer, enough can be retained on a given area of the electrode so as to absorb the entire incident light.
Since the particle sizes involved are small, there is no significant local electric field and hence the photo-response is mainly contributed by the charge transfer with the redox couple.
Two factors essentially contribute to the photo-voltage observed, namely, the contact between the nano crystalline oxide and the back contact of these materials as well as the Fermi level shift of the semiconductor as a result of electron injection from the semiconductor.
21

## Slide 22
UV –VISIBLE SPECTRA OF CdS SAMPLES
Samples | Band Gap (eV)
CdS – Z CdS – Y CdS -  Bulk CdS | 2.38 2.27 2.21 2.13
M. Sathish, B. Viswanathan, R. P. Viswanath Int. J. Hydrogen Energy (In press)
22

## Slide 23
PHOTOCATALYTIC PRODUCTION OF HYDROGEN
35ml of 0.24 M Na2S and
0.35 M Na2SO3 in Quartz cell
0.1 g CdS
400 W Hg lamp
N2 gas purged before the reaction and constant stirring
Hydrogen gas was collected over
water in the gas burette
23

## Slide 24
AMOUNT OF HYDROGEN EVOLVED BY CdS PHOTOCATALYST
24

## Slide 25
TEM IMAGE OF CdS NANOPARTICLES
Catalyst | Particle Size (nm) | Surface area (m2/g) | Rate of hydrogen production (  moles /h)
CdS - Y | 8.8 | 36 | 102
CdS - Z | 6 | 46 | 68
CdS -  | 11 | 26 | 67
CdS - Bulk | 23 | 14 | 45
CdS-Z
CdS- 
100 nm
100 nm
CdS-Z
25

## Slide 26
SCANNING ELECTRON MICROGRAPHS
26
CdS-Z
CdS-Y
CdS-
CdS- bulk

## Slide 27
Activity of the catalyst is directly proportional to work function of the metal and M-H bond strength.
PHOTOCATALYTIC HYDROGEN EVOLUTION OVER METAL LOADED CdS NANOPARTICLES
27

## Slide 28
Metal | Redox potential (E0) | Metal- hydrogen bond energy (K cal mol-1) | Work function (eV) | Hydrogen evolution rate* (µmol h-1 0.1g-1)
Pt Pd Rh Ru | 1.188 0.951 0.758 0.455 | 62.8 64.5 65.1 66.6 | 5.65 5.12 4.98 4.71 | 600 144 114 54
HYDROGEN PRODUCTION ACTIVITY OF METAL LOADED CdS PREPARED FROM H-ZSM-5
*1 wt% metal loaded on CdS-Z sample. The reaction data is presented
after 6 h under reaction condition.
M. Sathish, B. Viswanathan, R. P. Viswanath Int. J. Hydrogen Energy (In press)
28

## Slide 29
Pt, Pd & Rh show higher activity
High reduction potential.
Hydrogen over voltage is less for Pt, Pd & Rh
EFFECT OF METALS ON HYDROGEN EVOLUTION RATE
Ru
Ni
Pt
Pd
Ag
Fe
Cu
Rh
Au
10
100
1000
3 %
29

## Slide 30
EFFECT OF SUPPORT ON THE CdS PHOTOCATLYTIC ACTIVITY
2, 5,10 and 20 wt % CdS on support - by dry impregnation method
MgO support has higher photocatalytic activity - favourable band position
Alumina & Magnesia supports enhance photocatalytic activity
30

## Slide 31
Suitable band positions w.r.to the desired reactions
Compounds with layered structures. Layered structured with interconnected octahedra helps in better charge transfer e.g., perovskite structures
Absence of defect sites to prevent recombination
Compounds with high dipole moment (better charge separation)
High crystallinity and surface area
A.Kudo, Y.Miseki, Chem. Soc. Rev. 38 (2009) 253
Properties of highly active photo-catalysts

## Slide 32
Factors deciding the bandgap of the materials
Electronic configuration of the constituent ions
Percentage ionic character of the metal –anion bond
Crystal structure of the material
The bandgap increases when the percentage ionic character increases
Changes in the coordination contributes to bandgap variation
TiO2 crystal structure | Bandgap (eV)
Anatase | 3.05
Rutile | 2.98
Brookite | 3.26
Walsh et al., Chem Mater 21 (2009) 547
Di Paola et al., J. Phys. Chem. C, 113 (2009) 15166

## Slide 33
Sulfides and nitrides have VB made of S 3p- and N 2p- orbitals – small bandgap
Pb 6s in Pb2+, Bi 6s in Bi3+, and Sn 5s in Sn2+ also contribute to VB in some oxides
Materials containing elements with completely filled d-orbitals (d10) have VB edge at higher energy and hence small bandgap
Variation in bandgap with orbital contribution
Top of VB composed of d- and O 2p-orbitals
Bottom of CB composed of d- (for d0 ions) and sp-orbitals
With O 2p-orbitals only in VB , bandgap higher than 3.0 eV
Band structure of AgVO3
Band structure of NaVO3
Konta et al., Phys Chem Chem Phys 5 (2003) 3061
Dolgos et al., J. Solid State Chem., 182 (2009) 1964
Influence of electronic configuration of elements on band gap

## Slide 34
A.Kudo, Y.Miseki, Chem. Soc. Rev. 38 (2009) 253
Most mixed metal oxide photocatalysts with smaller bandgaps have d10 metal ions e.g., Ag3VO4 (2.0 eV), BiVO4 (2.4 eV), SnNb2O6 (2.3 eV), BiCu2VO6 (2.1 eV)
Role of various elements in the materials

## Slide 35
Percentage ionic character of a bond =
When the percentage ionic character increases, the CB becomes more negative and VB becomes more positive
The more the percentage ionic character of the, the larger the band gap
Semiconductor | Bond | Percentage ionic character | Band gap (eV)
SrTiO3 | Sr-O-Ti | 68.5 | 3.2
TiO2 | Ti-O | 59.5 | 3.0
WO3 | W-O | 57.5 | 2.8
Fe2O3 | Fe-O | 47.3 | 2.3
CdS | Cd-S | 17.6 | 2.4
CdSe | Cd-Se | 16.5 | 1.7
B.Viswanathan.. Bull. Catal. Soc. India, 2 (2003) 71
Influence of percentage ionic character of bonds on bandgap

## Slide 36
CdSnO3 and Cd2SnO4 are the two cadmium stannates
Both Cd2+ and Sn4+ have d10 orbitals
Cd2SnO4 exists in orthorhombic and cubic unit cells
CdSnO3 exists in orthorhombic and rhombohedral unit cells
About cadmium stannates
Cd2SnO4 is an indirect bandgap n-type semiconductor
Orthorhombic Cd2SnO4 has inverse spinel structure
O2- forms ccp array
Cd2+ occupies octahedral sites ; Sn4+ occupies tetrahedral sites
Tin
Cadmium
Oxygen
Gulino, I. Fragala, J. Mater. Chem., 9 (1999) 2837
Orthorhombic Cd2SnO4

## Slide 37
CdSnO3 has an indirect bandgap
Rhombohedral CdSnO3 has Ilmenite type structure
Both Cd2+ and Sn4+ occupy the octahedral sites in an hcp array of oxygen atoms
Cadmium
Tin
Oxygen
Has direct bandgap
Has the distorted orthorhombic distorted perovskite type structure
n-type semiconductor
Sn4+ occupies the octahedral sites
G. Natu, Y. Wu, J. Phys. Chem. C, 114 (2010) 6802
Rhombohedral CdSnO3
Orthorhombic CdSnO3

## Slide 38
Electrical conductivity : 1.5 X 10-7 S cm-1
CdSnO3 is widely studied as a sensor for various compounds like ammonia, ethanol and chlorine
CdSnO3 is also studied as host for Li ion batteries
As photoanodes for dye sensitized solar cells
Also studied as transparent conducting oxides
Properties and applications of Cd2SnO4
Properties and applications of CdSnO3
Electrical conductivity : 3.8 X 10-2 S cm-1
Cd2SnO4 shows high conductivity due to oxygen vacancies
Widely studied as transparent conducting oxides
shows upto 90% transmission in the visible region

## Slide 39
Aqueous SnCl4.5H2O solution
Aq. 3CdSO4. 8H2O solution
Added simultaneously
Aq. NaOH solution
Stirred overnight
Washed, dried, calcined 850 oC air 6 h
Rhombohedral CdSnO3
Preparation of CdSnO3
Stirred overnight
Washed, dried, calcined 1000 oC air 6 h
Orthorhombic CdSnO3

## Slide 40
Aq. SnCl4.5H2O solution
Aq. NaOH solution
Mixed together
Sn(OH)4 precipitate
Dissolved in con. H2SO4
Washed till absence of Cl-
Mixed with aq. 3CdSO4 . 8H2O solution
Dried calcined air 900 oC
Orthorhombic Cd2SnO4
Preparation of Cd2SnO4
Precipitated with NaOH
Precipitate washed till absence of SO42-

## Slide 41
Rhombohedral (JCPDS no. 880287)
Particle size from Debye-Scherrer equation – 45 nm
XRD pattern of CdSnO3
Orthorhombic (JCPDS no. 801467)
Particle size – 47 nm
XRD pattern of Cd2SnO4

## Slide 42
Absorbance starts 415 nm
Bandgap 3.0 eV
Diffuse reflectance UV-visible spectrum of CdSnO3
Absorbance starts at 532 nm
Bandgap : 2.3 eV
Diffuse reflectance UV-visible spectrum of Cd2SnO4

## Slide 43
SEM images of Cd2SnO4
Agglomerates of oval shaped particles
SEM images of CdSnO3
Flake like particles in agglomerated state

## Slide 44
Catalyst : 50 mg
Light source : 480 W Hg lamp
Irradiation time : 90 min
Model pollutant : 50 ml 25 ppm p-chlorophenol
Visible light :  > 420 nm (HOYA L-42 filter)
Catalyst | % Degradation | 
 | UV-visible | Visible
CdSnO3 | 94.5 | 0.0
Photocatalytic degradation of p-chlorophenol – CdSnO3

## Slide 45
Catalyst | % Degradation | 
 | UV-visible | Visible
Cd2SnO4 | 75.8 | 24.9
Photocatalytic degradation of p-chlorophenol – Cd2SnO4
Catalyst : 50 mg
Light source : 480 W Hg lamp
Irradiation time : 90 min
Model pollutant : 50 ml 25 ppm p-chlorophenol
Visible light :  > 420 nm (HOYA L-42 filter)

## Slide 46
Impedance measurements
Coated on Ti plates using PVDF as binder
Frequency : 0.01 – 10000 Hz
Reference electrode : Ag/AgCl
Flat band potential : 0.15 V vs Ag/AgCl 0.35 V vs NHE
Determination of flatband potential by Mott-Schottky plot
MS plot of CdSnO3
MS plot of Cd2SnO4
Flat band potential : 0.23 V vs Ag/AgCl 0.43 V vs NHE
Counter electrode : Pt
Amplitude : 0.005 V
Electrolyte : 0.5 M Na2SO4 (adjusted to pH 7)
Potential range : 0 V to 0.9 V

## Slide 47
Both cadmium stannates cannot evolve H2
Band positions of the cadmium stannates
Ecb is approximated as equal to Efb since doping density values are not available

## Slide 48
Hydrogen evolution reaction using CdSnO3 and Cd2SnO4
Photocatalytic water splitting studies
Medium : 35 ml Water-methanol (5:1 ratio)
Catalyst : 50 mg
Light source : 480 W Hg lamp
No hydrogen evolution occurred in UV-visible and visible irradiation

## Slide 49
Rhombhohedral CdSnO3 and orthorhombic Cd2SnO4 were prepared by co-precipitation method
Diffuse reflectance measurements showed bandgaps of 3.0 and 2.3 eV for CdSnO3 and Cd2SnO4 respectively
Photocatalytic p-chlorophenol degradation measurements showed both catalyst were effective in UV-Visible radiation
Only Cd2SnO4 was found to be photoactive in visible radiation ( > 420 nm)
Mott-schottky plots showed flat band potentials of 0.35 and 0.43 V (vs. NHE) for CdSnO3 and Cd2SnO4 respectively
Water splitting studies showed no H2 evolution in accordance with measured flat band potentials
Summary

## Slide 50: TiO2 Core/Shell structure- A First principle study

## Slide 51: Introduction
The extensive exploitation of Degussa P25 (TiO2) for studies in photo-electrochemical splitting of water and photo-catalysis has to be rationalized even though, the objective of its use in reported studies is mainly for comparison purpose.
Its remarkable reproducibility has to be recognized. It is presumed that P25 is a model core-shell system with anatase and rutile (4:1 weight ratio) and possibly the relative thickness of the core and shell of this system is most appropriate for its behaviour as a photocatalyst.
It is necessary that one recognizes the relative values of surface energy of the polymorphs of TiO2 in order to recognize the type of core shell configuration this system can adopt.

## Slide 52
Core/shell model
The core shell structure possibly alters the relative electronic structure of the system so as to be facile for photo-catalytic reaction and for charge separation and transfer.
The thickness of the shell (Anatase) may be optimum so as to provide adequate amount of surface adsorption and activation sites.
There are two possible routes for the electron transfer either from anatase core conduction band to Rutile conduction band or Rutile conduction band to Anatase trap states. The correct electron transfer route has to be established..

## Slide 53: Construction of models
Anatase
Rutile
Anatase-Rutile

## Slide 54
Computational details
The geometry optimisation been carried out in the CASTEP 5.5 implemented in materials studio package 5.5. The Density functional theory electronic structure calculations were performed in Generalised Gradient Approximation (GGA) method employing the exchange correlation function of PW91, with default spin. Cluster is treated with plane wave method with the energy cut-off value 300eV and the k points of 5 × 3 × 1. For single point energy and Density of States Calculations (DOS) the self-consistent field convergence window is set to be 2.0e-6eV/atom along with 48×48×48 FFT grid with the augmentation density scaling factor of 1. The psudopotentials were treated as Ultra soft in the real space system. The calculated DOS is plotted with smearing of 0.2 eV.

## Slide 55
Total density of states for Anatase, Rutile and Anatase-Rutile
Results

## Slide 56
Total density of states for Anatase, Rutile and Anatase-Rutile

## Slide 57: Discussion & Conclusion
Pure anatase shows higher density of states at the valence band as compared to pure rutile . This will have implications for the observed photo-activity of anatase phase.
The Anatase-Rutile valance band shows the higher DOS as compare to Pure anatse.
The valence band width (~2.5 eV) appears to be greater for the rutile-anatase combination rather than the other two pure phases. This could be the reason why the combination system exhibits higher photo-activity.
This can result in higher photon absorption cross section and thus facilitate facile electron hole pair formation.

## Slide 58
Adsorbent | Temperature (K) | Pressure (MPa) | Weight % of Hydrogen | Ref
MWNT | 300 77 | 12 | 0.3 2.27 | 4,6
SWNT SWNT Acid treated ACF CNT | 77 77 303 303 | 0.1 3.1 11.5 | 0.8 1.8 0.26 <0.2 | 5 7
Wood based carbon | 303 |  | <0.3 | 8
CA800 CB850 Amorphous carbon | 77 77 299 | 2 2 1 | 3.9 5.5 0,05 | 9
Fishbone CNF Platelet CNF Ribbon CNF | 299 299 299 | 1 1 | 0.03 0.03 0.02 | 10
Nanofibres (Pd/C) |  | 0.1 to 10 | 0.04-0.33 | 11
AC CNF A-CNF | 77-303 303 303 | 2-10 10 3-10 | 0.85-5.5 0.35 0.33-1.03 | 12
ZIF templated carbon | 77 | 2 | 2.6-3.1 3.9-6.2 | 13
Table. 1. Data on Hydrogen Storage on a variety of Carbon Materials
MWNT Multiwall nanotube; SWNT- Single wall nano tube; CNT- carbon nano tube; ACF activated carbon fibre [for more extensive compilation of data please see the earlier review articles [1, 14,15]]

## Slide 59
Sample | Percentage nitrogen | SSA (m2/g) | Hydrogen absorption at 1 atm (cm2/g) |  | 
 |  |  | 77 K |  | 373 K
PDC | 7.6 | 93 | 20.4 | 0.90 | 
MEC | 4.3 | 182 | 64.5 | 2.78 | 
CNT1 | - | - | - | - | 
NCNT1 | 6.4 | 246 | 47.5 | 6.11 | 
CNT2 | - | 633 | 28.0 | 3.42 | 
NCNT2 | 2.5 | 646 | - | - | 
CNT3 | -1.8 | 49 | - | 3.0 | 
NCNT3 |  | 66 | 7.45 | 2.4 | 
Table 5 Hydrogen absorption activity of carbon nano-materials at 1 atm and at different temperatures
PDC prepared from polyvinylpyrolidone; MEC from poly acrylonitrile; NCNT1 using poly pyrrole; NCNT2
and NCNT using pyridine

## Slide 60
Sample | CDX-975 | T-CDX-975 | A-CDX-975 |  | TA-CDX-975
S S A in m2/g | 325 | 224 | 129 |  | 124
Hydrogen adsorption capacity (cm2/g) at 1 atm |  |  |  |  | 
77K | 28.1 | 27.3 | 8.2 | 10.4 | 
298K | 0.53 | - | - |  | 0.7
373K | 2.83 | 3.17 | 3.03 |  | 2.97
423K | 4.18 | 4.25 | 4.30 |  | -
Table. 4. Comparison of specific surface area (SSA) and hydrogen absorption activity of CDX and chemically modified CDX samples
T-CDX – acid treated A-CDX- amine treated TA-CDX both acid and amine treated

## Slide 61
System | Total energy (Hartrees) | H1-H2 (Å) | Dissociation energy (eV)
H2 | -1.175 | 0.708 | 4.76
C60 C60+H2 | -2286.042 -2287.211 | - 0.707 | - 4.61
NC59 NC59+H2 | -2302.653 -2303.640 | - 0.831 | - 0.36
PC59 PC59+H2 | -2589.253 -2590.276 | - 0.813 | - 0.64
SC59 SC59 + H2 | -2646.036 -2647.013 | - 0.815 | - 0.62
BC59 BC59+ H2 | -2272.764 --2273.908 | - 0.818 | - 3.92
2B C58 (adjacent) 2BC58 + H2 (adjacent) | -2259.506 -2560.567 | - 1.126 | - 1,.662
2B C58 (alternate) 2B C58 + H2 (alternate) | -2259.487 -2260.477 | - 1.016 | - 0.276
Table 3 Bond length and dissociation energy of hydrogen molecule upon interaction with fullerene –
calculated using B3LYP with 6-31g (p,d) basis set on the UFF optimized structure

## Slide 62
CNT and substituted hetero atom | Total energy (Hartrees) | Bond length H1-H2 (Å) | Dissociation energy (eV)
Hydrogen | -1.175 | 0.708 | 4.76
CNT CNT + H2 | -3686.5502 -36687.7161 | - 0.776 | - 4.51
NCNT NCNT+H2 | -3702.5908 -3703.5989 | - 0.835 | - 0.22
PCNT PCNT+H2 | -3989.1694 -3990.2550 | - 0.815 | - 2.33
SCNT S CNT + H2 | -4046.0020 -4047.0067 | - 0.817 | - 0.13
BCNT BCNT+ H2 | -3671.7254 -3672.9440 | - 0.818 | - 5.95
2B CNT (adjacent) 2B CNT(adjacent) +H2 | -3658.6666 -3659.8092 | - 0.913 | - 3.88
2B CNT (alternate) 2B CNT(alternate)+H2 | -3659.3491 -3660.3594 | - 0.928 | - 0.28
Table 2 Bond length and dissociation energy of hydrogen on CNT and heteroatom substituted
CNTs calculated using B3LYP with 6-31g(p,d) basis set on the UFF optimized structure

## Slide 63: Why carbon materials for solid state hydrogen storage?
Coordination number is variable/expandable
Promote new morphologies
Covalent character retention
Variable hybridization possible
Geometrical possibilities/size considerations
Meta-stable state
Similar to biological architectures “Haeckelites”
Boron and nitrogen doped graphitic arrangements promise important applications.

## Slide 64: Objectives
Necessity of active sites
Heteroatom containing carbon materials - appropriate candidates?
Gradation of the carbon materials containing various heteroatoms
Geometrical positions of the heteroatoms

## Slide 65: Model & Methodology
Three Single Walled Carbon nanotubes (SWNTs) of armchair type (4, 4)
Each tube having 32 carbon atoms
Tube diameter - 5.56 Å
Interface with three nanotubes – intertubular distance - 3.64 Å
Energy minimization – UFF 1.02 (Cerius2 Software)
Single point energy and bond population analysis – DFT
( B3LYP/6-31G*)

## Slide 66
Substitution | Total Energy (Hartrees) | H1-H2 (Å) | Dissociation Energy (eV)
H2 | -1.175 | 0.708 | 4.76
CNT CNT + H2 | -3686.5502 -3687.7161 | - 0.776 | - 4.51
NCNT NCNT + H2 | -3702.5908 -3703.5989 | - 0.835 | - 0.22
Bond length and dissociation energy of H2 on NCNT
HOMO (Hartrees) | % orbital contribution |  |  |  |  | 
 | C |  | N |  | H | 
 | s | p | s | p | sb | st
CNT (-0.1612) | 0 | 100 | - | - | - | -
CNT + H2 (–0.1613) | 0 | 100 | - | - | 0 | 0
NCNT (– 0.1617) | 1 | 98.30 | 0 | 0.18 | - | 0.56
NCNT + H2 ( – 0.1371) | 0.52 | 37.39 | 1.37 | 31.91 | 26.66 | 2.15
Character of HOMO
* b- bonded hydrogen to nitrogen and t- terminal hydrogen in the cluster

## Slide 67
Substitution | Total Energy (Hartrees) | H1-H2 (Å) | Dissociation Energy (eV)
H2 | -1.175 | 0.708 | 4.76
CNT CNT + H2 | -3686.5502 -3687.7161 | - 0.776 | - 4.51
PCNT PCNT + H2 | -3989.1694 -3990.2550 | - 0.815 | - 2.33
Bond length and dissociation energy of H2 on PCNT
HOMO level (Hartrees) | % of orbital contribution |  |  |  |  | 
 | C |  | P |  | H | 
Contribution | s | p | s | p | sb | st
CNT (-0.1612) | 0 | 100 | - | - | - | -
CNT + H2 (–0.1613) | 0 | 100 | - | - | 0 | 0
PCNT (– 0.1611) | 1 | 96.85 | 0 | 1.71 | - | 0.53
PCNT+ H2 ( – 0.1516) | 1 | 85.62 | 0.04 | 8.06 | 4.83 | 0.49
* b- bonded hydrogen to phosphorus and t- terminal hydrogen in the cluster
Character of HOMO

## Slide 68
Substitution | Total Energy (Hartrees) | H1-H2 (Å) | Dissociation Energy (eV)
H2 | -1.175 | 0.708 | 4.76
CNT CNT + H2 | -3686.5502 -3687.7161 | - 0.776 | - 4.51
SCNT SCNT + H2 | -4046.0020 -4047.0067 | - 0.817 | - 0.13
Bond length and dissociation energy of H2 on SCNT
HOMO level (Hartrees) | % of orbital contribution |  |  |  |  | 
 | C |  | S |  | H | 
 | s | p | s | p | sb | st
CNT (-0.1612) | 0 | 100 | - | - | - | -
CNT + H2 (–0.1613) | 0 | 100 | - | - | 0 | 0
SCNT (– 0.1375) | 1 | 76.87 | 0 | 21.17 | - | 1.16
SCNT + H2 ( – 0.1207) | 0.45 | 41.80 | 0.35 | 41.65 | 14.87 | 0.88
* b- bonded hydrogen to sulphur and t- terminal hydrogen in the cluster
Character of HOMO

## Slide 69
Energy profile for hydrogen interaction with heteroatom substituted CNT clusters
Reaction coordinate
Substitution | Ea I (eV) | Ea II (eV) | H1-H2 (Å) | X-H (Å) | C-H1* (Å) | C-H2* (Å)
CNT | 10.02 | - | 0.71 | - | - | -
N CNT | 3.84 | 4.58 | 1.45 | 1.11 | 1.70 | 1.94
P CNT | 3.81 | 3.99 | 1.51 | 1.61 | 1.27 | 2.33
S CNT | 3.65 | 4.85 | 1.50 | 1.75 | 1.24 | 2.40
Ea = E (transition state) – E (reactant) * Shortest C-H bond distance

## Slide 70
Substitution | Total energy (Hartrees) | H1-H2 (Å) | Dissociation energy (eV)
H2 | -1.175 | 0.708 | 4.76
CNT CNT + H2 | -3686.5502 -3687.7161 | - 0.776 | - 4.51
B CNT B CNT + H2 | -3671.7254 -3672.9440 | - 0.818 | - 5.95
Bond length and dissociation energy of H2 on BCNT
HOMO level (Hartrees) | % of orbital contribution |  |  |  |  | 
 | C |  | B |  | H | 
Contribution | s | p | s | p | sb | st
CNT (-0.1612) | 0 | 100 | - | - | - | -
CNT + H2 (–0.1613) | 0 | 100 | - | - | 0 | 0
BCNT (–0.1576) | 1 | 94.87 | 0 | 3.59 | - | 0.5
BCNT + H2 (– 0.1534) | 1 | 96.26 | 0.10 | 1.12 | 1 | 0.54
* b- bonded hydrogen to boron and t- terminal hydrogen in the cluster
Character of HOMO

## Slide 71
Bond length and dissociation energy of H2 on BCNTs
Substitution | Total energy (Hartrees) | H1-H2 (Å) | Dissociation energy (eV)
H2 | -1.175 | 0.708 | 4.76
CNT CNT + H2 | -3686.5502 -3687.7161 | - 0.776 | - 4.51
2B CNT (adjacent) 2B CNT (adjacent) + H2 | -3658.6666 -3659.8092 | - 0.913 | - 3.88
2B CNT (alternate) 2B CNT (alternate) + H2 | -3659.3491 -3660.3594 | - 0.928 | - 0.28
Adjacent position
Alternative position

## Slide 72
Substitution | Ea I (eV) | Ea II (eV) | H1-H2 (Å) | X-H (Å) | C-H1 (Å) | C-H2* (Å)
CNT | 10.02 | - | 0.71 | - | - | -
2B CNT (adjacent) | 2.22 | 2.98 | 1.95 | 1.31 | 2.59 | 2.72
2B CNT (alternate) | 1.5 | 2.33 | 2.95 | 1.47 | 1.47 | 2.34
Ea = E (transition state) – E (reactant) * Shortest C-H bond distance
Energy profile of boron substituted CNT clusters

## Slide 73
Bond length and dissociation energy of H2
 | Total Energy (Hartrees) | (H1-H2) Å | H2 Dissociation energy (eV)
H2 | -1.175 | 0.708 | 4.74
C60 C60+H2 | -2286.042 -2287.211 | - 0.707 | - 4.61
NC59 NC59 +H2 | -2302.653 -2303.640 | - 0.831 | - 0.36
PC59 PC59 +H2 | -2589.253 -2590.276 | - 0.813 | - 0.64
SC59 SC59 +H2 | -2646.036 -2647.013 | - 0.815 | - 0.62
METHODOLOGY
Energy minimization – UFF 1.02 (Cerius2 Software)
Single point energy – DFT ( B3LYP/6-31G*)
Hydrogen activation in heteroatom substituted fullerene

## Slide 74
Substituted fullerenes
Unsubstituted fullerenes
Transition state path ways for hydrogen interaction
X= N, P & S
X
X
X
X
X
Substitution | *Ea I (eV) | Ea II (eV) | Ea III (eV) | H1-H2 Å | X-H1 Å | C1-X Å | C2-X Å | C3-X Å
Carbon | 18.49 | - | - | 0.70 | - | - | - | -
Nitrogen | 3.24 | 3.15 | 3.08 | 1.85 | 1.04 | 1.44 | 1.50 | 1.50
Phosphorus | 1.73 | 1.52 | 1.52 | 1.85 | 1.26 | 1.48 | 1.62 | 1.62
Sulphur | 2.56 | 6.48 | 1.86 | 1.13 | 1.60 | 1.70 | 1.70 | 1.70
* = E (each transition state) – E (reactant)

## Slide 75
Boron substituted fullerene
Substitution | Total energy (Hartrees) | (H-H) Å | H2 dissociation energy (eV)
H2 | -1.175 | 0.708 | 4.74
C60 | -2286.042 | - | -
C60 + H2 | -2287.211 | 0.707 | 4.61
BC59 | -2272.764 | - | -
BC59 +H2 | -2273.908 | 0.818 | 3.92
2BC58 (Adj) | -2259.506 | - | -
2BC58 (Adj) +H2 | -2560.567 | 1.126 | 1.66
2BC58 (Alt) | -2259.487 | - | -
2BC58 (Alt) +H2 | -2260.477 | 1.016 | 0.28

## Slide 76
Transition state optimized parameters and the Ea for the proposed pathway
Substitution | EaI (eV) | H1-H2 (Å) | B1-H1 (Å) | B2-H2 (Å) | C-H1* (Å) | C-H2* (Å)
Adjacent (X, 2) | 2.26 | 1.98 | 1.19 | 1.29 | 2.52 (C2) | 1.43 (C4)
Alternate (X, 3) | 0.50 | 2.95 | 1.27 | 1.23 | 1.25 (C2) | 1.97 (C5)
Ea = E (each transition state) – E (reactant) * = Shortest C-H bond distance
Outcome
Substituted heteroatom acts as an active centre for hydrogen activation
For the effective hydrogenation and hydrogen storage, the heteroatoms should be incorporated geometrically and chemically into the carbon network

## Slide 77
High Pressure adsorption apparatus
Vacuum system
Digital Pressure Indicator
Vent
Gas inlet
Furnace
PT
RC
SC
TC
NV
NV- Needle valve
RC- Reference Cell
PT- Pressure transducer
SC- Sample cell
TC- Thermocouple
Calculation:
PiVi = Pf (V1+V2+V3+ Vads)
Vads Z = Vcorrect
33.8 mL (V1)
V2 (18.64 mL)
V3 (20.72 mL).
Where Z = Compressibility factor

## Slide 78
Activated Carbon and their modifications
Activated carbon
(CALGON & CDX-975)
Metal supported on CALGON
  Nickel metal - (2, 5 & 20 wt %) - physical mixture of acetate metal precursor - reduction in hydrogen atmosphere at 450 C
Chemical treatment on CDX-975
  Chemical treatment with 1M HNO3 for acid treatment and for amine treatment tri ethylene tetra amine.
Chapter 4. Hydrogen storage capacity in activated carbon

## Slide 79
 | Calgon | Nickel/Carbon (Calgon) |  |  | CDX- 975 | T-CDX | A-CDX | TA-CDX | 
 |  | 20 wt% | 5 wt% | 2 wt% |  |  |  |  | 
Surface area (m2/g) | 931 | 616 | 750 | 1066 | 325 | 224 | 129 | 124 | 
Hydrogen absorption at 1 atm (cm3/g) |  |  |  |  |  |  |  |  | 
77K | 137.7 | 54.4 | 44.5 | 120.8 | 28.1 | 27.3 | 8.2 |  | 10.4
298K | 0.70 | 0.5 | - | - | 0.53 | - | - |  | 0.7
373K | 0.43 | 3.14 | 1.4 | 1.53 | 2.83 | 3.17 | 3.03 |  | 2.97
423K |  | 1.95 | 1.7 | 2.05 | 4.18 | 4.25 | 4.30 |  | 
473K |  |  |  |  | 5.0 | 4.60 |  |  | 
523K |  |  |  |  | 4.80 | 6.36 |  |  | 
Hydrogen absorption capacity at 1 atm pressure

## Slide 80
High pressure hydrogen absorption activity of activated carbon

## Slide 81
Carbon materials | Template | Carbon Source | Technique | Morphology
PDC | Silica | PVP | Precipitation | Rod shape
MEC | Silica | PAN | Insitu precipitation | Coiled and fibers
CNT1 & NCNT 1 (6.4 %) | Alumina membrane | PPA PPY | In-situ polymerization | Tubular
CNT2 & NCNT2 (2.5%) | Zeolite | Acetylene Acetylene + Pyridine | Chemical vapor deposition | Tubes and fibers
CNT3 & NCNT3 (1.8%) | Clay (pillared) | Acetylene Acetylene + pyridine | Chemical vapor deposition | Tubes and fibers

## Slide 82: Characterization of Carbon Nanotubes

## Slide 83
Specific surface area and amount of hydrogen absorbed at 1 atm & different temperatures
Sample | SSA (m2/g) | Hydrogen absorption at 1 atm (cm3/g) at various temperatures (K) |  | 
 |  | 77 | 298 | 373
PDC | 93.0 | 20.2 | 0.34 | 0.90
MEC | 182 | 64.4 | - | 2.78
NCNT1 | 246 | 47.5 | - | 6.11
CNT2 | 633 | 28.0 | - | 3.42
NCNT2 | 646.5 | - | - | -
CNT3 | 48.8 | - | - | 3.0
NCNT3 | 66.4 | 7.45 | - | 2.4

## Slide 84
Hydrogen storage capacity at various pressures

## Slide 85
Template | Carbon Source | Technique | Morphology
Alumina membrane (BCNT1) | Polymer (hydroborane) | In-situ polymerization | Tubular
Zeolite (BCNT2) | Hydrocarbon (Acetylene + borane gas) | Chemical vapor deposition | Tubes and Fibers
Clay (pillared) (BCNT3) | Hydrocarbon (Acetylene + borane gas) | Chemical vapor deposition | Tubes and Fibers

## Slide 86
Alumina membrane
(0.2μm pore size) in THF
Borane (BH3.THF)
Divinyl benzene
Stirred 273 K
Polymer /Alumina
Carbon / Alumina
48% HF 24h
Carbonization 1173K Ar,4h
Polymerization at RT 3h
Carbon nanotubes (BCNT1)
Boron containing carbon nanotubes prepared using alumina membrane
0C
THF solvent
N2 atm
+ BH3:THF
using hydroborane polymers

## Slide 87
Ar gas
Acetylene gas
Mass flow meter
Magnetic stirrer
Ice bath
Tubular furnace
NaBH4 + THF
Conc. H2SO4
H-Y Zeolite or pillared clay in quartz boat
Chemical vapor deposition of borane gas + acetylene mixture over template
Preparation of boron containing carbon nanomaterials using zeolite and pillared clay
After carbonization treated wit 48% HF to remove the template
BCNT 2 (Zeolite)
BCNT 3 (Clay)

## Slide 88: Characterization of Carbon Nanotubes

## Slide 89
13C & 11B CP MAS NMR of boron containing carbon nanotubes prepared by different methods
13C CP MAS NMR of BCNT1
11B CP MAS NMR of BCNT1 & BCNT2

## Slide 90: XPS of BCNT1
(a). The servey X-ray photoelectron spectrum of boron substituted carbon nanotube. (b). The deconvoluted XPS spectrum of B1s.
Confirms the presence of two different chemical environment of boron

## Slide 91
Carbon nanomaterial | Surface area (m2/g) | Amount of hydrogen absorbed (cm3/g) at 1 atm & at various temperatures (C) |  |  | 
 |  | -196 | 25 | 100 | 150
BC | 11.9 | 3.63 | 0.6 | 3.63 | 4.68
PBC | 429.9 | 73 | - | 2.90 | 3.02
BCNT1 | 523 | 127 | - | 16.5 | 14.8
BCNT2 | 62.3 | 3.22 | - | 2.38 | 4.73
BCNT3 | 32.7 | 1.09 | - | 1.7 | -
Hydrogen absorption activity of boron containing carbon nanomaterials at 1 atm

## Slide 92
Boron containing carbon nanotubes prepared with polymer precursor, show different boron chemical environments and structural morphology. This configuration has a bearing on hydrogen sorption characteristics.
Hydrogen storage capacity of boron containing carbon nanotubes

## Slide 93
THANK YOU ALL