## Slide 1
Nafion layer-enhanced photosynthetic conversion of CO2 into
Hydrocarbons on TiO2 nanoparticles
Wooyul Kim et al., Energy Environ. Sci., 5, 2012, 6066
V. Jeyalakshmi
27-04-2013

## Slide 2
Direct solar conversion of CO2 into hydrocarbons is an ideal solution to reduce the
CO2 concentration in the atmosphere with the simultaneous production of solar fuels.
The photosynthetic conversion of CO2 is limited mainly by:
(i) The highly negative one-electron reduction potential of CO2,
(ii) The strong oxidation power of photo-generated valence band holes (or OH
radicals) that can react with intermediates and products of CO2 conversion
(e.g., formate, form-aldehyde, and methanol in reactions (3)–(7)),
(iii) The low solubility of CO2 in water (33 mM@ 298 K and 1 atm),
(iv) The competition with H2 formation (reaction (1))
Introduction

## Slide 3
In this study, a Nafion (perfluorinated polymer with sulfonate groups) overlayer on Pd-TiO2 (Nf/Pd-TiO2) was employed for the photo reduction of CO2 in the absence of a sacrificial electron donor.
Nafion-coated TiO2 catalyst was selected for the artificial photosynthesis on the basis of three reasons.
Being a superacid & an excellent proton conducting medium, the Nafion layer may enhance the local activity of protons near the TiO2 surface region & the PCET reaction can be facilitated within the Nafion layer over TiO2. The proton conducting property of Nafion should facilitate the diffusion of protons onto the CO2 reduction sites.
The intermediates of CO2 reduction might be stabilized within the Nafion layer, which should help the serial electron transfers from the intermediate to the final product (Nafion layer that should prohibit the direct contact between the products and the TiO2 surface).
Being a per-fluorinated polymer, Nafion itself is stable against the photocatalytic oxidation and is inert toward the photoinduced redox reactions.

## Slide 4
Preparation of Nf/Pd-TiO2 catalyst
Photo-deposition method :
Aq. TiO2 (0.5 g/L) in methanol (e- donor, 1.25 M) + 1Wt% PdCl2
filtered & washed with distilled water
UV irradiation for 30 min (with a 200-W Hg lamp)
1Wt% Pd –TiO2 (A)
20 g of 5 wt% Nafion solution in a mixture of alcohol & water + 300 mL of DI water
Heated to 70–80°C until the volume reduced to 50ml
Repeated three times to remove aliphatic alcohols
Diluted to 100 mL by adding distilled water
Nafion Solution (B)

## Slide 5
1Wt% Pd –TiO2 (A)
Nafion Solution (B)
+
Vigorous stirring for 30 min.
Dried at 80°C for overnight
Nf/Pd-TiO2
Preparation of Nf/Pd-TiO2 catalyst

## Slide 6
(a) TEM image and (b) high-resolution TEM images of Nf/Pd-TiO2.
TEM images of Nf/Pd-TiO2

## Slide 7
(a) TEM image and (b) Line Energy Dispersive X-ray microanalysis (EDX) image
(high-angle annular dark field image) and the elemental mapping of (c) Ti, (d) O, (e) Pd, and (f) F on Nf/Pd-TiO2 sample.

## Slide 8
Nf/Pd–TiO2 micrographs showing (a) TEM and (b) HRTEM images, as well as the energy-filtered TEM (EFTEM) maps of (c) Ti and (d) F (obtained from image (a)).
EFTEM Images

## Slide 9
XPS spectra of Nf/Pd-TiO2 (blue) and Pd-TiO2
(red) powder, showing (a) Ti 2p, (b)
Pd 3d, and (b) F 1s band regions.
XPS Results

## Slide 10
Time profiles of methane production in the UV-irradiated suspension of (a) Pd-TiO2
& (b) Nf/Pd-TiO2 without pre-cleaning of the catalysts. The photo-irradiation experiments were compared between Ar - and CO2 -purged conditions.
The experimental conditions were [catalyst] = 1.5 gL-1 (with 1.0 wt% Pd), pHi = 5.3 (not adjusted), λ > 300 nm, and initially Ar or CO2 -saturated.
Surface Carbon Identification

## Slide 11
The amounts of methane and ethane generated after 5 h and 1 h of continuous
illumination, respectively, as a function of Nafion loading.
The experimental conditions were [catalysts] = 1.5 gL-1 (with 1.0 wt% Pd and 0.42 - 1.3 wt% Nafion), λ > 300 nm, and initially CO2 -saturated with adding 0.2 M sodium carbonate & subsequent acidification to pHi= 3.
Effect of Nafion loading

## Slide 12
Time profiles of (a) methane & (b) ethane production in the UV-irradiated (l> 300 nm) suspension of Pd–TiO2 and Nf/Pd–TiO2 after
the pre-cleaning process at pH 3.
Photoconversion of CO2
The experimental conditions: [catalyst]=1.5 gL-1 (with 1.0 wt% Pd and 0.83 wt% Nafion), initially CO2-saturated by adding 0.2 M sodium carbonate and subsequent acidification (pH 1 and 3).

## Slide 13
The production of methane (@ 5 h) & ethane (@ 1 h) at pH 1, 3, and 11 on Pd–TiO2 and Nf/Pd–TiO2.
The experimental conditions were [catalyst]=1.5 g L-1 (with 1.0 wt% Pd and 0.83 wt% Nafion), initially CO2-saturated by adding 0.2 M sodium carbonate & subsequent acidification (pH 1 and 3).
Effect of pH on Nf/Pd-TiO2

## Slide 14
Repeated cycles of methane production in the UV-irradiated (l> 300 nm) suspension of Nf/Pd–TiO2 after the pre-cleaning process.
The experimental conditions: [catalyst]=1.5 gL-1 (with 1.0 wt% Pd and 0.83 wt% Nafion). At the end of each cycle, the reactor was purged with CO2 gas. At the point of each arrow, [Na2CO3] of 0.2 M was newly added and then acidified to pH 3 to obtain a fresh CO2-saturated suspension.
Stability of Nafion layer on Pd-TiO2

## Slide 15
Outdoor solar tests for the photoconversion of CO2 into hydrocarbons (CH4,C2H6, and C3H8) in Nf/Pd–TiO2 suspension at pH 3 (solid line: time profile of solar light intensity).
Outdoor solar tests for the photoconversion of CO2

## Slide 16
Photosynthetic conversion of CO2 to hydro-carbons occurring on the Nf/Pd–TiO2 nanoparticle.

## Slide 17
Conclusions
Introducing a thin Nafion overlayer on Pd–TiO2 significantly increased the photosynthetic activity for CO2 reduction under UV & solar light.
The main role of the Nafion over layer seems to enhance the local proton activity within the layer to facilitate PCET reactions and to stabilize intermediates and to inhibit the re-oxidation of the CO2 reduction products.
The production of hydrocarbons such as methane, ethane, & propane was clearly higher with Nf/Pd–TiO2 than with Pd–TiO2.
The photosynthetic activity of the Nf/Pd–TiO2 catalyst was maintained through repeated cycles of photoreaction, which confirms the stability of the Nafion layer.