## Slide 1: Selective hydrogenation of cinnamaldehyde to cinnamyl alcohol
Presented by
V Surya Kumar (CA11M005)
Under the guidance of
Dr. K.R.Krishnamurthy
&
Dr. Preeti Aghalayam
National Centre for Catalysis Research
Indian Institute of Technology, Madras

## Slide 2
Reaction scheme
Carbonyl group
Olefinic group
Desired product
undesired rex
Desired rex
undesired rex
G = 118 KJ/mol
G = 80.71KJ/mol
G = 37.79 KJ/mol
G = 0.49KJ/mol
CAL=cinnamaldehyde, COL=cinnamyl alcohol, HCAL= hydrocinnamaldehyde,
HCOL=hydrocinnamyl alcohol
Notes: Antibiotic chloromyctin, cinamates(ester) in flavor and fragrance, --- HCAL – cinnamic acid – protease inhibitor for treatment of AIDS

## Slide 3
Ref. W. Yu, Y. Wang, H. Liu, and W. Zheng, J. Molec. Catal. A, 112, 105 (1996).
0.03 S-1
Reduction using Stoichiometric reagents
Sodium borohydride
MPV reduction (Meerweil-Ponndorf-Verley Reduction)
Heterogeneous catalyst : Best catalyst known from litrature

## Slide 4: Problem for Research
Ref-A. Giroir-Fendler, D. Richard, and P. Gallezot, in Heterogeneous Catalysis and Fine Chemicals (M. Guisnet, J. Barrault, C. Bouchoule, D. Duprez, C. Montassier, and G. Perot, eds.), Studies in Surface Science and Catalysis Vol.41, Elsevier, Amsterdam, 1988, p. 171.
a=Cinnamyl alcohol, b=hydrocinnamylaldehyde, c=hydrocinnamyl alcohol
T= 60oC , P = 4 MPa, cinnamaldehyde=13.2g in 37.5 ml isopropanol and 10 ml H2O, 400 mg of catalyst.)

## Slide 5: Aim and scope of the project
To design Pd based catalyst which will be selective for
Cinnamyl alcohol while retaining its high activity.
Experimental approach
To prepare, characterize and test performance of following catalysts
Shape controlled Pd/Hydrotalcite(HT) (3.6 and 1w%)
Tetrahedral Pd/HT
Octahedral Pd/HT
Spherical Pd/HT

## Slide 6
2) Pd supported on different phases of titania
1%Pd/P25
1%Pd/Anatase
1%Pd/Rutile
3) Bimetallic systems
1%Pd-Ag/P25
1%Pd-Au/P25
To compare performance of above mentioned catalysts
following catalysts were prepared, studied
1%Ag/P25
1%Au/P25
1%Pd/Al2O3
1%Pd/SiO2

## Slide 7
Step 1
Dissolve in 45mL water
0.750g(2.93 mmoles) of Mg(NO3)2 ·6H2O
0.5485g(1.46 mmoles of Al(No3)3 .9H2o
Step 2
Disolve in 5mL water
Solution B
0.01571g(0.0884 mmol) PdCl2
Step 3 mix Sol A and Sol B
1.439g(10.2mmoles) of HMT
Solution A
0.01035g(0.17 mmol) of NaCl
Transfer sol A + Sol B into 100mL autoclave and keep at 150 OC oven for 6 h.
Step 4
allow Autoclave to cool, than wash the ppt till filtrate pH=7, than dry the ppt over night at 100 OC.
Preparation of Tetrahedral Pd/HT
nPd/nMg/nAl molar ratio = 2/66/33
Notes: Hydrotalcite is a LDH support, it is highly basic in nature because of presence of large no of hydroxyl groups, Shape controlled Pd- different shapes have different edges corners hence different dispersion and different plane facets giving rise to different activity.

## Slide 8
Preparation of Octahedral Pd/HT
Same as tetrahedral Pd/HT, except for addition of CTAB1.3g(3.5mmol)
into the reaction mixture.
Preparation of Spherical Pd/HT
3.6%Pd/HT
Firstly hydrotalcite support is prepared separately followed by
impregnation of Na2PdCl4 and its reduction by formaldehyde.
1%Pd/HT
Firstly hydrotalcite support is prepared separately followed by
impregnation of H2PdCl4 and its reduction by polyol process.

## Slide 9
Mechanism (precipitation – reduction method)
Ref. J. Phys. D: Appl. Phys. 45 (2012) 385302 (6pp)
Mechanism of surfactant action in Octa-Pd/HT
Notes: Decomposition of HMT gives ammonia and formaldehyde – ammonia increases PH as a result Al+3 and mg+2 getS ppt as hydroxides, formaldehyde reduces Pd+2 ,
The shape of particle can be controlled either thermodynamically or kinetically based on the rate of reducing agent production in-situely, when decomposition of HMT is high formaldehyde production is high so reduction is high rate so kinetic control and anisotropic structures may form when rate of reduction is low than thermodynamically favotred tertahedral geometry are obtained. When CTAB is used the bromide ions adsorb to the palladium seeds and alter their surface free energy and lead to formation of octahedral morpholohy, in terahedral we see only 111 plane whereas in octahedral we see both 111 and 100 planes.
When CTAB is added the bromide ions present in CTAB adsorb on seed of Pd and alter the free energy and we get octahedral geometry.

## Slide 10
XRD comparing a) Octahedral Pd/HT b) Tetrahedral Pd/HT c) Hydrotalcite
D) Incert view(38-42. 2 theta angle)
Notes: We can see small sliver of pd 111 at angle 40, this sliver is less instance in octahedral because some pd are also present. For the selectivity 111 are important as the configuration of cinnamaldehyde is approaching end-on onto 111 which we shell see in simulation part, and it is observed in acetylene hydrogenation that from P111 is selective because ethylene gest desorbed quickly from 111 and presence of 100 is not good for selectivity because they enhance presence of subsurface hydrogen which are highly reactive and will further hydrogenate unsaturated alcohol to saturated alcohol.

## Slide 11
TEM images of Tetrahedral Pd/Hydrotalcite
EDAX FO tetrahedral Pd/HT
Crystallite size distribution of tetrahedral Pd/HT

## Slide 12
TEM image & crystallite size dist. of octahedral Pd/Hydrotalcite

## Slide 13
TEM image &crystallite size dist. of Spherical Pd/Hydrotalcite

## Slide 14
TPR of octahedral 3.6%Pd/Hydrotalcite
Consumes 6.69mmol/g of H2

## Slide 15: Preparation of 1.5%PVP Protected-Pd/TiO2-P25
Add(250mmoles) 15 ml Ethylene glycol
Dissolve (1.25μmoles) 50 milligrams of PVP
Lastly add 0.31M NaOH (1.5mL) Stir the mix for ½ h at 60 oC
followed by impregnation of Pd colloid on 1.98g of TiO2-P25
Preparation of H2Pdcl4 (in RB flask) Conc.HCl(0.608mmoles)(50μl) + PdCl2(0.282mmoles)(50mgram)
PVP/Pd molar ratio = 1:150
Eo/V= -1.65eV
Pd+2 Pd Eo/V= 0.951
Notes: PVP – importance of PVP, it helps control the size of colloid depending on temp, PH, reduction time.., it protects colloid not to get agglomerated. Ethylene glycol – acts as a solvent and reducing agent.
NaoH importance – it helps accelerate the reduction by enhancing the decomposition of ethylene glycol and control the size depending on concentration.
Green process as no need to spend energy for hearing the rex as reductoin occurs at room temp, no need of further calcinatoin.
Ethanol <=> Acetaldehyde + 2H+ + 2e- (E0' = +0.197 V) aldehyde to acetate is 0.6 pd+2 ------ pd is 0.95

## Slide 16
1%Pd/P25, 1%Pd/Anatase, 1%Pd/Rutile, were prepared as 1.5%Pd/P25 were prepared using polyol method.
Bimetallic systems
1%Pd-Ag/P25
1%Pd-Au/P25
Bimetallic catalysts were also prepared using polyol method .
Pd/Ag Molar ratio = 4:1
Pd/Au Molar ratio = 4:1

## Slide 17: Characterization
UV-VIS of Pd colloid a) before reduction b) after reduction
UV–Vis spectral analysis
Notes: Pd+2 shows d-d inter band transitions (pd+2=4s2, 4p6, 4d7, 5s1) at 325 nm and 440nm. And disappearance means reduced Pd is present. While recording one must be careful about the concentration – it should be low in the range of milimoles.

## Slide 18
TEM image and crystallite size dist. Of 1.5% Pd/ P25
EDAX

## Slide 19
TEM image and crystallite size dist. of 1% Pd/ P25

## Slide 20
TEM image and crystallite size dist. of Reduced 1%Pd/P25
Reduction: at T=300OC, Time=3h in H2 atmosphere

## Slide 21
TEM image and crystallite size dist. of 1%Pd-Ag/ P25

## Slide 22
TEM image and crystallite size dist. of 1%Pd-Au/ P25

## Slide 23
TPR of 1% Pd/TiO2 P-25
0.12mmol/g H2 consumption
70oC

## Slide 24
TRP of 1% Pd-Ag/TiO2 P-25, 1% Pd-Au/TiO2 P-25
H2 consumption
Pd-Ag = 1.061mmol/g
Pd-Au= 0.91mmol/g
286.14oC
290.20 oC

## Slide 25
TPR of 1% Pd/Anatase
H2 consumption = 3.71mmol/g

## Slide 26
XPS of 3d Pd of 1%Pd/Anatase, 1%Pd/TiO2-P25, 1%Pd-Au/TiO2-P25

## Slide 27
Catalyst | BE of Pd 3d5/2(eV) | BE of Pd 3d3/2(eV)
Pd Standard | 335 ± 0.2 | 340± 0.2
1%Pd/P25 | 335.40 | 340.43
1%Pd/Anatase | 335.33 | 340.72
1%Pd-Au/P25 | 335.02 | 340.36
1%Pd/-P25 used at 100oCC | 335.47 | 340.87
Binding energy of 3d Pd in 1%Pd/TiO2-P25, 1%Pd/Anatase, 1%Pd-Au/TiO2-P25, 1%Pd/TiO2-P25 used at 100oC

## Slide 28: Deconvolution of Pd 3d peak 1%Pd/P25
%Pd0 | %Pd+2
54 | 46
Surface % ratios of Pdo and Pd+2

## Slide 29: Deconvolution of Pd 3d peak 1%Pd/Anatase
%Pd0 | %Pd+2
50.5 | 49.5

## Slide 30: Deconvolution of Pd 3d peak 1%Pd-Au/P25
%Pd0 | %Pd+2
66 | 34

## Slide 31
UV-Vis DRS of 1%Pd/TiO2-P25, 1%Pd-Ag/TiO2-P25, 1%Ag/TiO2-P25, 1%Pd-Au/TiO2-P25 and 1%Au/TiO2-P25.

## Slide 32: Testing of Catalysts
Prepared catalysts are being tested by carrying out hydrogenation of
cinnamaldehyde in a Parr Reactor
Obtained products are analyzed using Perkin Elmer GC with
RTX 5-ms column.

## Slide 33
Mixture of reactant and products
Reactant
Calibration of GC
COL
HCAL
HCOL

## Slide 34
Optimization of reaction conditions

## Slide 35
Catalyst name | Conversion% | Selectivity% |  |  | TOF(s-1)X 10-3
 |  | HCAL | HCOL | COL | From TEM
3.6%T Pd/HT | 100 | 78.9 | 20.8 | 0.3 | 9.9
3.6%O Pd/HT | 100 | 78.3 | 21.5 | 0.2 | 9.432
3.6%S Pd/HT | 100 | 71 | 22.7 | 6.3 | 2.346
1.5%Pd/TiO2-P25 | 100 | 7.3 | 19.5 | 73.2 | 3.158
Initial reaction conditions
T=120 C, Catalyst wt. = 150g, P=10bar, time=1h, solvent(methanol)=13g
Reactant = 1.2g.

## Slide 36
Effect of reactant weight
T=100 C, Catalyst wt. = 40g, P=10bar, time=1h, solvent(methanol)=13g
Reactant = 2.4g, as-synthsised catalyst
Catalyst | Conversion% | Selectivity% |  |  | 
 |  | HCAL | HCOL | COL | ACL
1%Pd/P25(1.2g) | 96.1 | 3.9 | 11.6 | 81.1 | 3.4
1%Pd/P25(2.4g) | 69.4 | 12.7 | 5 | 57.7 | 24.6
Acetal of cinnamaldehyde

## Slide 37
Catalyst | Conversion% | Selectivity% |  |  | 
 |  | HCAL | HCOL | COL | ACL
1%Pd/P25 | 69.4 | 7 | 4.2 | 63.2 | 25.6
1%Pd/P25 reduced at 300oC | 65.4 | 22.4 | 15.9 | 29.1 | 32.6
T=100 C, Catalyst wt. = 40g, P=10bar, time=1h, solvent(methanol)=13g
Reactant = 2.4g, Reduced catalyst .
Effect of Pre-reduction

## Slide 38
T=100oC, reactant(CAL)=2.4gm, solvent(methanol)=13gm,
H2 pressure=10bar, reaction time=1h
With as-synthsized ccatalyst.
Optimized reaction condition

## Slide 39
Selectivity and conversion

## Slide 40
Catalyst | Conversion% | Selectivity% |  |  |  | TOF(s-1)
 |  | HCAL | HCOL | COL | ACL | aH2 Che
1%Pd/P25 | 69.4 | 7 | 4.2 | 63.2 | 25.6 | 0.4
1%Pd/Anatase | 100 | 10.8 | 13.9 | 75.3 | 0 | 0.77
1%Pd/Rutile | 95.1 | 21.6 | 9.5 | 65.3 | 3.5 | -
Pd supported on different phases of titania
T=100oC, P=10bar, catalyst=40mg, reactant(CAL)=2.4gm,solvant(methanol)=13gm, time=1h.

## Slide 41
C=O bond activation by electropositive Fe on Pt surface
Concept of Lewis sites
Ref: Richard, J. Ockelford, A. Giroir-Fendler, and P. Gallezot, Catal.Lett., 3,53 (1989).

## Slide 42
Catalyst | Conversion | Selectivity |  |  |  | TOF(s-1)
 |  | HCAL | HCOL | COL | ACL | aH2 Che
1%Pd/P25 | 69.4 | 7 | 4.2 | 63.2 | 25.6 | 0.4
1%Pd-Au/P25 | 70.3 | 11.6 | 3 | 47.5 | 37.9 | 0.25
1%Pd-Ag/P25 | 71.5 | 6.1 | 10.6 | 45 | 38.4 | 0.57
Pd bimetallic catalysts
T=100oC, P=10bar, catalyst=40mg, reactant(CAL)=2.4gm,solvant(methanol)=13gm, time=1h.

## Slide 43
Catalyst | Conversion% | Selectivity% |  |  |  | TOF(s-1)
 |  | HCAL | HCOL | COL | ACL | From TEM
1%Td Pd/HT | 22.9 | 42.2 | 0 | 2.6 | 55.3 | 0.065
1%Sp Pd/HT | 95.2 | 69.9 | 18.9 | 10.9 | 0.3 | -
T=100 C, Catalyst wt. = 40g, P=10bar, time=1h, solvent(methanol)=13g
Reactant = 2.4g
Pd supported on Hydrotalcite

## Slide 44
Catalyst | Conversion% | Selectivity% |  |  | 
 |  | HCAL | HCOL | COL | ACL
1%Pd/Anatase(TiO2) | 100 | 10.8 | 13.9 | 75.3 | 0
1%Pd/γ-Al2O3 | 73.5 | 16.9 | 6.5 | 62 | 14.7
1%Pd/SiO2 | 74 | 4.3 | 6.7 | 67.7 | 21.3
Sp 1%Pd/HT | 95.2 | 69.9 | 18.9 | 10.9 | 0.3
Effect of supports
T=100 C, Catalyst wt. = 40g, P=10bar, time=1h, solvent(methanol)=13g
Reactant = 2.4g

## Slide 45
Tetrahedral, octahedral Pd/Hydrotalcite catalyst show poor selectivity towards COL, whereas spherical Pd/Hydrotalcite show better conversion and selectivity towards COL, when compared to tetrahedral and octahedral Pd/HT. The low selectivity to COL is attributed to large particle size and high basic nature of hydrotalcite.
Among titania based catalyst systems, anatase based catalyst is most active with good selectivity, when compared to P25 and rutile phases. High activity is attributed to SMSI(strong metal support interactions) and high reducibility of Pd/Anatase.
Pd-Au/P25 & Pd-Ag/P25 bimetallic systems are showing similar activity and selectivity, but when compared to monometallic Pd/P25, bimetallic systems show 28% decrease in selectivity, which is attributed to formation of Pd-Ag and Pd-Au alloy.
Pd supported on γ-Al2O3 and SiO2 show similar selectivity when compared to Pd/P25. More characterization of Pd supported on γ-Al2O3 and SiO2 are needed.
Among all the catalyst prepared the best catalyst for selective hydrogenation of cinnamaldehyde to cinnamyl alcohol is 1%Pd/Anatase with TOF = 0.77s-1.
Summary