Chapter – 3

Thermal Methods

Among the various surface analytical techniques thermal field in neutrals out is the simplest.  This technique has been practiced for a long time as flash desorption; wherein the temperature of a metallic wire containing adsorbed species is suddenly increased and the desorbed gases analyzed.  The principle of thermal desorption is simple.  Gaseous molecules are adsorbed on surfaces with various binding energies.  If the solid surface temperature is low, the binding energy of the adsorbate will retain the adsorbed gas on the surface.  At room temperature, this situation will prevail for chemisorbed species while at low temperatures such as that liquid nitrogen (77 K) physisorbed species can be retained on the surface.  If the surface temperature is then increased, the adsorbed components will desorb at a rate determined by their binding energies, frequency factors, the order of the desorption process and the heating rate of the substrate.  The temperature of the surface is increased in a programmed manner either linearly (T = T0 + βt where β is the rate of increase of temperature and t is time in minutes) or exponentially.  The linear heating rate has given rise to a number of useful tools including TGA, DTA, DSC , as well as a number of temperature programmed techniques usually designated as TPD, TPO, TPR , TPRS, TPC, TPRO, TPS, TPN, and so on.

Generally, temperature programming is better than flash methods in the fact that time and temperature are interrelated in programming techniques and hence one can deduce suitable kinetic expressions for the desorption process or for the process taking place as a result of temperature programming.  This aspect will be dealt with subsequently.  Temperature programmed techniques are advantageous over isothermal methods on many counts.  For example,

- Detailed stepwise reduction of a metal ion can be examined in TPR while isothermal reduction can give only the overall reduction characteristics.

- Details of the reduction characteristics of systems containing multi component metal ions could be probed by temperature programmed technique while it is difficult to discriminate the reduction schedules of individual ions with isothermal methods.

- Surface states of metals bound differently with the support can be identified by TPR which is not possible by isothermal techniques.

- Effect of added promoters, impurities can be studied by the shifts in the reduction maximum or by the appearance of a new maximum in TPR.

- Peak maximum temperature is a measure of the reactivity or binding strength of the species held on the surface.

- The integral part of the peak is proportional to the number of species involved in reduction, desorption, reoxidation and so on.

- The shifts in the peak maximum temperature in TPD as a function of coverage are indicative of the reaction order.

- It may be deduced that if reaction products were to evolve at the same peak maximum temperature, then they must originate from the same rate determining step.

In essence, temperature programming appears to provide a handle to discriminate the various individual steps involved  in desorption, reduction or oxidation processes while isothermal methods can provide information only on the over all process taking place.

Temperature programmed techniques can be advantageously utilized for a number of studies.  Let us list some of them and demonstrate the utility of this technique with suitable examples.

- Mechanistic study of the reaction under study.

- Nature of active sites involved in the reaction.

- Influence of preparation procedures of the catalyst precursors used on the phases obtained for use subsequently as catalysts.

- Effect of the support for promoting the formation of active catalyst phase, the chemical composition of the active phase in multi- component systems, the role of promoters for the effective dispersion of the active phase.

- The interaction between the active phase and the support or between the various active phases in multi-component systems.

- To identify the binding states of adsorbed species. It is known that some of the adsorbates give rise to multiple adsorption state on the surfaces of solids.

- Surface chemical changes during transient or non-steady state conditions.

Temperature programmed methods are based on monitoring chemical changes as a function of temperature where temperature is altered linearly with respect to time.  Experimentally the system under investigation is charged inside a furnace which is connected to a processor which heats the reactor typically at 0.1 to 20 °C/min.  A thermal conductivity detector monitors the gas composition.   Typically for TPR 5 % H2 in Ar or in TPO 5% O2 in He is employed to optimize the thermal conductivity difference. Typical schematic representation of the apparatus for TPX measurement is shown in Fig. 3.1.

Fig. 3.1. Schematic representation apparatus for TPX measurements

Table 3.1     Listing of the various thermal analysis Techniques and the methods of following the changes in chemical systems.

| Acronym | Name of the technique | Method of following |
| --- | --- | --- |
| DTA DSC | Differential Thermal Analysis Differential scanning calorimetry | Temperature difference between the sample and an inert reference like alumina |
| TG | Thermogravimetry | Weight of the sample |
| DTG | Differential thermogravimetry | Weight change with temperature |
| TMA | Thermomechanical Analysis Dilatometry | Specific volume of the solid sampe |
| TMA | Thermomagnetic analysis | Magnetic properties |
| DMC | Differential microcalorimetry | Enthalpy difference between sample and reference |
| TPX | Temperature Programmed (X= Reduction, Oxidation, Desorption, Sulphidation, or Surface Reaction. | Analysis of the gas at the outlet of the unit. |

Temperature programmed desorption can be used to identify

- The nature and strength of adsorption.

- The various states of adsorption.

- The quantity of adsorption in a particular adsorption state.

- The kinetics of adsorption process, like the order of the reaction, the activation energy for the process.

- In some favourable cases it is possible to evaluate the reaction network.

The Nature of information that can be obtained by each of the temperature programmed techniques are given in Table 3.2.

Table 3.2  The nature of information that can be generated from various TPX  techniques

Temperature Programmed Desorption (TPD)

- Identification of the adsorptive properties of materials - Characterization of surface functionalities like acidity and basicity - Temperature interval where desorption takes place - The amount desorbed, adsorption capacity, metal surface determination, dispersion - Binding state of the molecules, energetics of adsorption, surface non uniformity - Mechanistic and kinetic aspects of adsorption and desorption

Temperature Programmed Reduction (TPR)

- Identification of the redox properties of solids - Temperature range of the reduction of the solid - Total quantity of the reducing agent consumed, valence state of metal ions in oxidic systems - Interaction between metal and the support - Indication of the interaction between metals, alloy formation - Mechanism and kinetics of reduction process

Temperature Programmed Oxidation (TPO)

- Characterization of the redox properties of metals and metal oxides - Characterization of coke species in deactivated catalysts as well as in hydrocarbon conversion reactions - Estimation of the coke deposited in deactivated catalysts - Mechanism and kinetics of oxidation reactions

Typical experimental conditions employed in some of these techniques are summarized in Table 3.3.

Table. 3.3  Typical experimental conditions employed in TPX experiments

|  | TPD | TPR | TPO |
| --- | --- | --- | --- |
| Gas composition | He or N2 or Ar | 5%H2/N2 | 5%O2/N2 |
| Flow rate ml/min | 15-60 | 15-30 | 30-90 |
| Heating Rate K/min | 10-60 | 4-60 | 10-60 |
| Detecting system | TCD or MS | TCD | TCD or MS |

Surface Acidity Determination:

As a first example let us consider the acidity determination of solid catalysts.  It is known that many solid acids are better catalysts than even conventional mineral acids and their acid strength is higher than that of conventional acids.  The acidities of these solid catalysts have been evaluated by a number of ways like, titration with a base, [1] (this method has limitation with respect to wettability, phobicity of the solids for the non-aqueous  medium used and above all for coloured solids identifying the colour change of the indicator and so on.  Those interested in fully knowing the limitations of this method is directed to refer [2]), adsorption of basic probe molecules like ammonia, pyridine, quinolines, use of catalytic reaction like dehydration of alcohols like cyclohexanol as well as by a number of spectroscopic methods like IR, NMR and so on.  These aspects will be taken up subsequently in the chapter on acid-base property of solid

catalysts.

TPD is one of the techniques used for evaluating the acidity of solid catalyst. The most often used is the ammonia TPD since it is easy to perform.   However, ammonia adsorption may not differentiate between Bronsted and Lewis acidic sites. Strong interaction of ammonia with acidic site might result in a partial re-adsorption of NH3, resulting in  a shift of the desorption maximim of up to 150 °C.  Typical adsorption of ammonia on a variety of zeolites is shown in Fig. 3.2.

Fig. 3.2. Typical adsorption of ammonia on various zeolites and other zeolitic substances, (a) Mordenite, (b) ZXM-5, (c) SAPO-11, (d) ALPO-11

The next set of probe molecules are alkyl amines other than methyl amine. They (alkyl amines other than methyl amine) can determine Bronsted acid sites.  By Hoffman elimination they also yield  olefins and ammonia as products thus the results have to be carefully interpreted.

HRNH2 + H-O-Zeol à HRNH3+…-O-zeol à R+ NH3 + H-O-Zeol

Typical amine adsorption TPD is shown in Fig.3.3.

Fig. 3.3.  TPD-TGA curves for isopropylamine from an H-ZSM-5 catalyst containing approximately 500 μmol/g/ of Bronsted-acid sites. A mass spectrometer was used to determine the products.

The thermal desorption spectra obtained for desorption of n-propyl amine and n-butyl amine is shown in Fig.3.2 In this figure the x-axis represents time instead of temperature and in temperature programmed techniques, time and temperature are related to each other through the heating rate that is T = [T0 + βt)]  where To is the starting temperature, β is the heating rate in degrees per minute and ‘t’ is time in minutes.

It is seen that the desorption spectra for n-propyl amine  and n-butyl amine shown in Fig. 3.2 is similar in shape with two identifiable adsorption states, in both cases, marked α and β, however there are distinctive differences.  It is seen that in the case of n-propyl amine, the low temperature desorption peak is of equal magnitude as that of the high temperature desorption peak probably indicating that there are two different types of acid sites with different strengths, but the number of sites in each category is almost the same as that of the other where as in the case of n-butyl amine the number of weak acids appear to be quite small while the total number of strong acid sites is quite high.  However, the total number of acid sites available on the surface appears to be the same.  The points that emerge from this example are:

- HY zeolite does possess acid sites probable by organic amines.

- There are different kinds of acid sites with different strength.

- The probe molecules depending on their basicities do not discriminate exactly the different acid strengths.

Study of the mass spectral analysis of the desorption products showed the presence of butanes, higher olefins, dienes and aromatics.   These products could have been formed during the temperature sweep or could have resulted from the adsorption of the amines.   The point one can derive from this observation is that the desorption of these type of products take place either as a result of temperature sweep or due to surface reaction, implying that acidity measurements using amines as probe molecules has to be treated with caution.   However the data given in Table 3.4 show that there is consistency in the surface acidity of HZSM-5 determined by ammonia/ethylamine adsorption.   Therefore, there is still hope to rely on acidity determination from the measurement of adsorption of basic probe molecules.

Table 3.4. Comparison of acidity data for HZSM-5 measured by different methods

| Sample SiO2/Al2O3 | Carrier gas | adsorbate | Adsor-ption Temp. (K) | Acid amount |  | Acid strength |  | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Mole/g | Sites X 1020 per g | Peak 1 | Peak 2 |  |
| 53 | N2 | NH3 | 423 | 0.7304 | 4.4 | 476 | 698 | 1 |
|  |  |  |  | 0.6928 | 4.17 | 475 | 649 | 1 |
|  |  |  |  | 0.7016 | 4.27 | 474 | 689 | 1 |
| 48 | He | C2H5NH2 | 423 | 0.7248 | 4.38 | 498 | 698 | 2 |
| 52 | He | NH3 | 423 | 0.7706 | 4.64 | 503 | 708 | 3 |
| 47.3 | He | NH3 | 423 | 0.7505 | 4.52 | 467 | 678 | 4 |
| 49.5 | He | NH3 | 343 | 0.7803 | 4.70 | 473 | 753 | 5 |

[1] D.C.Zhang and Z.J.Da, Thermochim.Acta, 233 (1994) 87.

[2] J.X.Liu, Q.X.Wang, and L.X.Yang, J.Catal., (Chi Hua Xue Bao) 8 (1987) 203.

[3] S.Y.Li, G.Y.Gai, Q.W.Wang, X.B.Zhang and G.Q.Che, J.Catal., (Chi Hua Xue Bao)

8 (1987) 47.

[4] D.W.Zhov, Q.X.Cao and Q.Z.Li, J Fuel Chem.Technology, 11(1983) 64

[5] J.G.Post and J.H.C.Van Hooff, Zeolites, 4 (1984) 9.

Preparation of catalysts – Application of Temperature Programmed Methods

Preparation of catalysts involves many unit operations like (i) precipitation, (ii) decomposition, (iii) reduction and (iv) impregnation and so on.

In addition to this, these unit operations are also carried out under various operating conditions, like temperature, pH, nature or precipitating agent, nature of the gaseous atmosphere, reducing gas used and its partial pressure, flow rate of the gases used for pretreatment, moisture content and duration of pretreatment, nature of support, promoters impurities present will all have profound effect on the nature and texture of the materials that are produced as the final catalytic phase.   The effect of some of these parameters will be considered from the point of view of how these techniques provide information on these effects.   For example TPR can provide under favourable circumstances, information on the stepwise reduction of the metal ion precursors employed for the preparation of metallic catalysts, multi-metallic systems. The reduction behaviour of metals can also be elucidated by TPR.   The binding of the metal ions with the support if it were to be a variable parameter can be elucidated by TPR.   The effect of added promoters, impurities can also be examined from the shift in the position of the reduction signals or appearances of new signals in the TPR traces.

Table 3.2. Some of the probe molecules that have been used in conjunction with TPD for surface acidity/ basicity determination.

| Probe molecule | Type of sites normally probed | Some remarks on suitability |
| --- | --- | --- |
| Ammonia | The type (Bronsted and Lewis) and concentration of acid sites | Molecular size of ammonia is small, so micro-porous substances can be probed. |
| Aliphatic amines | The type of acid sites and their concentration | Intra molecular reactions are possible various products can be identified by TPX techniques |
| Pyridine | The type of acid sites and their concentration | Due to size restrictions only some of the pores are accessible.10 member or higher channels alone are accessible. Availability of molar absorption coefficient value enables quantitative measurements |
| Substituted Pyridines | The type of acid sites and their concentration | Accessibility of the sites is restricted; sites near pore openings can be probed. |
| Benzene, Toluene and Xylenes | Acid strength and accessibility of sites | These molecules can undergo reactions especially isomerization reactions on strong acid sites, Some time slow uptake of the bulky molecules |
| Alkanes | Acid strength and accessibility of sites | They may be used to probe sites where hydrocarbon conversion reactions preferentially takes place |
| Pyrrole | The type of basic sites and their concentration | Intra molecular reactions can take place hence interpretation has to be careful. |
| Carbon-dioxide | The type of basic sites and their concentration | Formation of carbonates can vitiate the conclusions |
| Nitriles | The type of acid sites and their concentration | Surface reactions can occur and hence interpretation is difficult |
| Carbon monoxide | Metal centres and the type of acid sites and their concentration | Low temperatures are necessary; multiple bonded species may also be present |
| NO and NO2 | Metal centres (especially ionic sites) and the type of acid sites and their concentration | Nitrate formation on the surface can vitiate the results obtained. |

The various applications of TPR technique has been compiled by Hurst et al [3]. Jenkins and coworkers [4] have examined Pt/SiO2 catalysts using TPR technique.   They have found that the catalyst prepared by ion exchange method gave better dispersion of Pt as compared to the catalyst prepared by impregnation with chloro-platinic acid.   The TPR pattern of the two catalysts are shown in Fig.3.3, wherein it is noticed that the catalyst prepared by ion exchange gets reduced at a higher temperature, perhaps due to the strong interaction of the Platinum species with the support silica.

Fig. 3.3.

It is also possible to use TPR to establish the effect of temperature of calcination on the reduction of metallic species. A typical example is shown in Fig. 3.4.

Fig. 3.4. The influence of calcinations temperature on Pt/Al2O3 catalysts

TPR technique can also provide information of the type of interaction that can occur in multi-component catalytic systems.   First let us consider the example of bimetallic systems wherein the alloy formation is an important aspect.   The alloy formation can occur in any of the four unit operations like impregnation, drying, calcination or reduction stages of the catalyst preparation.   In Fig. 3.5, the TPR traces of the Pt-Pd system is shown wherein one can easily see that the TPR traces of the physical mixture is different from that of the impregnated system.   It is seen that Pt associated with Pd is also get reduced at lower temperatures wherein essentially reduction of the palladium predominates. This part of the Pt perhaps associated with Pd in the form of the alloy is also reduced as easily as Pd.  Another example would be Pt-Ge/Al2O3 system. It is seen that Pt associated with Pd is also get reduced at lower temperatures wherein essentially reduction of the palladium predominates. This part of the Pt perhaps associated with Pd in the form of the alloy is also reduced as easily as Pd.

Fig.3.5. Alloy formation in supported catalysts

Another example would be Pt-Ge/Al2O3 system.  The data relevant to this system are shown in Fig.3.6.   The Pt and Ge when impregnated on alumina exist as two different species on the support as seen from the TPR profiles shown in Fig.3.6.   The reduction peaks of these two metallic ions are distinct and easily discriminated.

Fig.3.6. Fresh impregnated catalyst

However, after the reduction if this system were to get re-oxidized and reduced, the TPR profile shown in Fig.3.7  indicate that part of the Ge gets reduced with Pt at low temperatures, indicating these two metallic ions on reduction could give rise to an alloy formation on the surface.

Fig.3.7. Alloy formation during reduction

Senzi Li et al [5] have examined promoted iron catalysts for Fischer Tropsch synthesis.   They have compared the reduction and carbonization behaviour of Fe-Zn-K oxides promoted by Ru or Cu.   The oxygen removal rates of these two promoted systems (TPR traces) with that of the impregnated systems are shown in Fig. 3.8.

Fig.3.8.Oxygen removal rates for Fe–Zn–K–Cu(Ru) oxides in H2. (a) Fe–Zn–K2, (b) Fe–Zn–K2–Cu1, and (c) Fe–Zn–K2–Ru1. (0.2 g sample; K/Fe=0.02, Cu(Ru)/Fe=0.01; 0.167 K/s ramping rate; 20% H2/Ar, 0.268 mol/h flow rate).

The reduction sequence that is Fe2O3 → Fe3O4 → FeO→ Fe is followed in all the three catalytic systems.   The addition of Cu to Fe-Zn-K system reduced the temperature of reduction of Fe2O3 by 130 K from around 620 K to nearly 490 K; this reduction in temperatures has been attributed to the formation of hydrogen dissociation sites generated by the reduction of CuO to Cu metal at low temperatures.   Ru in the mixture had a similar effect on the temperature required for this reduction of Fe2O3 but to a greater extent than that observed with copper.   In the case of ruthenium, the metal dispersion appears to be better and hence yields more dissociated hydrogen for easy reduction of Fe2O3.   Similar conclusions can be drawn from the TPR traces for oxygen removal by CO and carbon introduction rates on these systems as shown in Fig.3.9.

Fig. 3.9.

It must be realized that the promoter action or role has to be identified in many ways. They can be listed as follows:

- Generation of suitable activation centres for the reducing agent.

- They can also induce segregation of the reducing component of the multi-component systems.

- The entropy change resulting from this chemical reaction may be favourable in the presence of the promoter.

- The promoter species could also function as effective heat transferring medium or sink or source so as to facilitate the facile reduction of the precursor species.

Fig. 3.10.

Fig. 3.11. (A) Oxygen removal and (B) carbon introduction rates for Fe–Zn–K–Cu(Ru) samples in CO. (a) Fe–Zn–K2, (b) Fe–Zn–K2–Cu1, and (c) Fe–Zn–K2–Ru1. (0.05 g sample; K/Fe=0.02, Cu(Ru)/Fe=0.01; 0.167 K/s ramping rate; 20% CO/Ar, 0.268 mol/h flow rate).

Studies on the Phase composition – TPR studies

TPR technique can also be utilized to distinguish the reduction behaviour of two phases of the same substance.   For example NiO can crystallize in cubic as well as rhombohedral forms.   The TPR traces of Ni (OH)2 prepared by urea hydrolysis is shown in Fig.3.10.   This shows a simple reduction peak. But if the same hydroxide is calcined at 673 K and then a TPR trace is recorded one can easily distinguish the reduction peaks of both the phases of NiO.   This could have arisen since while the hydroxide is decomposed both the crystalline forms of NiO could have formed.   Another aspect to be noted is that the rhombohedral form is easier to get reduced as compared to the cubic form.

The TPR traces for the hydroxide of nickel prepared by different impregnation methods are shown in Fig.3.10.   There are distinguishable nickel reduction stages that can be identified in these traces.   They are possibly free NiO in rhombohedral and cubic forms, NiO that is reduced by an autocatalytic process and a bound state of NiO which gets reduced at higher temperatures.   Thus we can see finer details of interaction of the metallic species with the support from the TPR traces.   TPR studies of zeolite systems especially metal exchanged systems have been particularly interesting since it could identify the exact site wherein the metal ions are exchanged, how the metal ions migrate over the zeolite surface on re-oxidation and thus it provides information on sub surface mobility and diffusion. [8 ]

Let us consider a few examples of the application of the Temperature programmed Reaction Spectroscopy (TPRS).

The decomposition of deteurated formic acid on Ni (110) surface has been investigated by Madix et al [9].   The desorption pattern obtained by them is shown in Fig.3.11.  One can see there are two distinct CO desorption peaks, indicating the desorption of CO is taking place from two reaction steps probably one coming out of the direct decomposition of the adsorbed formic acid molecule and the high temperature one from the adsorbed CO.

The overall reaction sequence as postulated by them is

2DCOOH           →  [DCO + DCOO] + H2O

DCO                   →  CO  + D

DCOO                 →  CO2  + D

[CO  + DCOO]ads  →   COads + CO2  + D

This type of detailed reaction steps could be elucidated from the analysis of the products evolving from the surface as a function of temperature programming.

One of the problems which require information is the reaction of oxygen with ethylene for the formation of ethylene oxide.  The questions to be answered are:

(i) Which oxygen species is involved in the formation of the desired product namely the ethylene oxide.

(ii) How does the adsorbed oxygen species involved in the reaction?

Van Santen et al [10] have performed the following studies to establish these points. The observations made by them are:

1. No reaction was observed if both oxygen and ethylene were co-adsorbed at 113K.

2. Adsorption of oxygen at 300 K followed by reaction with ethylene produced only carbon dioxide.

3. Adsorption of oxygen at 470 K followed by a TPRS with ethylene produced ethylene oxide.

These results are shown pictorially in Fig.3.12.  These studies have revealed that ethylene oxide formation has been possible only when the oxygen pre-adsorption temperature are high enough to form subsurface oxygen apart from chemisorbed oxygen. Probably for selective oxidation both subsurface and chemisorbed oxygen are essential.

Another example is the reaction between CO and hydrogen on potassium promoted ruthenium catalysts has been studied using TPRS technique using IR as the detection mode.   The TPRS trace obtained by Gonzalez and Miura [11] is shown in Fig 3.13.  It can be seen that the CO which shows absorption band around 2020 cm-1 is not reactive to produce methane while the CO showing IR absorption band around 1950 cm-1 is reactive and form methane. From these studies it may be concluded that only the linearly adsorbed CO is not participating in the reaction while the CO adsorbed in the bridged mode is reactive for the hydrogenation reaction.

The carbon deposition in hydrocarbon reactions is an important step and various attempts have been made to identify the nature of carbon that is formed on the catalyst surface.  The results obtained on the surface of Ni/Al2O3 during the hydrogenation of CO are shown in Fig 3.14.   It is seen that the surface carbon deposited by adsorption of CO is more reactive towards hydrogenation as compared to the free adsorbed CO.  Secondly the nature of the carbon deposited from the adsorption of CO is different from the carbon deposited by the adsorption of ethylene in terms of reactivity towards hydrogenation (See Fig.3.15.In fact more than one form of carbon has been identified by the adsorption of ethylene and their reactivity towards hydrogenation also differ. (Refer to Fig.3.16.)  The formation and nature of coke formed can also be probed by temperature programmed oxidation.  Parera et al [] have investigated the combustion of carbon deposited on Pt/Al2O3 catalysts.  Their results are shown in Fig.3.17.  It is seen that the coke on the metal (Pt) is oxidized at a lower temperature (553 K) while the coke on the support is oxidized only at 763 K. Another observation worth noting is that the temperature of combustion of the coke decreases with increase in the metal loading. Similar observations have been recorded by others as well [].

Many of the partial oxidation catalysts like molybdates, vanadates, tungstates and antimonates are amenable for easy reduction and oxidation, and the ease of reduction is a measure of their activity and the re-oxidation capability is a measure of the life of the catalyst.   Miura et al [] have studied the TPRO of  Bi2O3: MoO3  and bismuth molybdate catalyst.    The results obtained by them are shown in Fig.3.18 and 19. Depending on the extent of reduction, re-oxidation of Bi and Mo take place at 443 K and 693 K in single or multiple steps.   However for the bismuth molybdate, two re-oxidation peaks at 593 K and 673 K are obtained.   Phosphorus promoted bismuth molybdate however shows the re-oxidation peak at 593 K peak increases in intensity showing phosphorus addition facilitates the re-oxidation.

Another example is Pd on alumina catalysts. The re-oxidation of the aged catalysts showed redistribution of Pd particles on the used catalyst. The results of such a study are shown in Fig.3.

Fig 3. Oxygen TPD over aged (4 cycles) and fresh (3.0)Pd/alumina and upper left hand corner oxygen TPD of (3.0)Pd/alumina (3 cycles) reproduced from F.Klingstedt, H. Karhu, A.Kalantar Neyestanaki, L.E Lindfors, T.Salmi and J.Vayrynen, J.Catalysis, 206,(2002)248.

Table  Commonly employed models for describing Solid State Reactions

|  | Name of the model | f(α) | G(α) |
| --- | --- | --- | --- |
| 1 | Random Nucleation Deceleratory first order | (1-α) | -ln(1-α) |
| 2 | Generalized nth order | (1-α)n | 1/n(1-(1-α)-(n-1)) |
| 3 | 1D or 2D Avarmi-Erofeyev | 2(1-α)(-ln(1-α)1/2) | (-ln(1-α)1/2) |
| 4 | 2D or 3D Avarmi-Erofeyev | 3(1-α)(-ln(1-α)2/3) | (-ln(1-α)1/3) |
| 5 | 3D Avarmi-Erofeyev | 4(1-α)(-ln(1-α)3/4) | (-ln(1-α)1/4) |
| 6 | Generalized Avarmi-Erofeyev | n(1-α)(-ln(1-α)n-1/n) | (-ln(1-α)1/n) |
| 7 | Contracting area Sharp interface controlled reaction | (1-α)1/2 | 2(1-(1-α))1/2 |
| 8 | Contracting Volume Sharp interface controlled reaction | (1-α)1/3 | 3(1-(1-α))1/3 |
| 9 | Generalised model by Sestak | (1-α)n(-ln(1-α))p αm |  |
| 10 | Prout-Tompkins Model | (1-α) α | (ln α/(1-α)) |
| 11 | One dimensional diffusion | ½ α | (α2) |
| 12 | Two dimensional diffusion | -ln(1-α)-1 | (1-α)ln(1-α)+ (α) |
| 13 | Three dimensional diffusion Jander | 3(1-α)2/3/ (2(1-(1-α)1/3-)) | (1-(1-α)1/3)2 |
| 14 | Three dimensional diffusion Ginstling_Brounshtein | 3/2((1-α)-1/3-1) | (1-2(α)/3)-( (1-α)2/3) |

1. Benzi

2. Limitations of the titration methods

3. Hurst et al

4. Jenkins

5. Li S, Krishnamoorthy S, Li A, Meitzner GD, Iglesia E. J Catal, 2002,
206(2): 202.

6.J. A. Z. Pieterse, R. W. van den Brink, S. Booneveld and F. A. de Bruijn, Applied Catalysis, B46(2003) 239

7. Xiang Wang, Haiying Chen and W. M. H. Sachtler, Applied Catalysis, B29(2001)47; B26(2000) L227.

8. K J Leary, J.N.Michaels, and A.M.Stacy, J. Catalysis, 107(1987)393