CHAPTER 1

INTRODUCTION

1.1 Role of carbon dioxide

Presence of carbon dioxide is essential for the photo synthesis process, which forms the lifeline for all the flora and fauna that define the ecology of this earth. In fact, all other forms of life, including human beings, survive on the oxygen which is the by-product of photo synthesis. However, atmospheric CO2 level has to be within certain limits.  The optimum concentration of CO2 necessary for the bio-network on earth is 300 ppm (Ref). In earlier days, as shown in Fig. 1.1, CO2 level in the atmosphere and carbon cycle was maintained by a series of natural processes as described below.

Fig. 1.1 Carbon cycle shows the movement of carbon between land, atmosphere, and oceans in billions of tons of carbon per year. Yellow numbers are natural fluxes; red are human contributions in billions of tons of carbon per year. White numbers indicate stored carbon.(Reproduced from Ref XX)

In modern days, this delicate carbon cycle has been disturbed and atmospheric CO2 level is gradually increasing. According to the data (Ref) published by International Energy Agency (IEA), CO2 emission is exponentially increasing since 1870, (another Fig showing year-wise increase in atmospheric CO2 from IEA report to be added) mainly from the combustion of fossil fuels, in order to meet our energy requirements. Global Total Primary Energy Supply (TPES) has almost doubled, from 1971 to 2012, and 82% of TPES is derived by burning fossil fuels, emitting large quantities of CO2[1]. One ton of oil releases MT of CO2 on burning releases xx MT of CO2 (Ref). Since energy is essential for economic growth and overall development, increase in atmospheric CO2 level is expected to be high. CO2 emissions from the fossil fuels pose serious environmental issues like green-house gas effect and unusual weather patterns. Even though CO2 is the least effective green house gas per kilogram emitted, it is considered as significant green house gas due to large amount released to the atmosphere from human activities and industrial revolution [2].

Fossil fuels could continue to be our primary source of energy, possibly till the turn of 21st century. Hence globally, serious efforts are on, to keep CO2 level under control. On one hand, renewable sources of energy like solar, wind, tidal, bio-mass, and geothermal are being harnessed, though to a limited extent as of now, so to minimize the carbon foot print/ CO2 emission.

Table 1.1 Reactants and their products  with CO2  [Reproduced from Ref.3]

| Reactants | Products with CO2 |
| --- | --- |
| Alkane | Syngas, acids, esters, lactones |
| Cycloalkane | Acids, esters, lactones |
| Active-H compound | Acids, esters, lactones |
| Monoalkene | Acids, esters, lactones |
| Dienea | Acids, esters, lactonesb |
| Cycloalkene | Acids, esters, lactones, (co)polymers |
| Substituted hydrocarbonc | Acids, esters, lactones, polycarbonates |
| Alkyne | Lactones, unsaturated organic carbonates |
| Epoxide | Carbonates, (co)polymers (polycarbonates) |
| NH3 and amine | Symmetrical ureas, aminoacids, (co)polymers |
| Diamine | Ureas, carbamates, (co)polymers (polyureas) |
| Imines | Carbamates, (Co)polymers (urethane) |

aAllenes and 1,3-dienes, bwith longer C-C chain than the original monomer. cDihalogen substituted.

Simultaneously, viable means of capture, storage and sequestration of CO2 and its conversion to fuels and chemicals are being explored. The task indeed is a challenging one. Conversion of  CO2  by reaction with different organic molecules could result in variety of  highly useful products  for the fine chemicals industry, is shown in Table 1.1 [3].

However, use of CO2 as reactant by the chemical industry is only about 0.5 wt% (Ref) of the total anthropogenic CO2 emissions every year [4].  Hence, several simultaneous approaches are needed to convert CO2 to fuels and chemicals, so that atmospheric CO2 level could be maintained at near optimum levels. Such an approach would ultimately lead to the use of CO2 as sustainable source of energy as well. Considering such a dual benefits, several CO2 conversion processes, other than those for chemicals manufacture, are being studied with great interest. A list of such CO2 conversion processes to yield fuels, is presented in the following section.

1.2 Processes for CO2 conversion

CO2 is the most oxidized form of carbon and therefore, the only chemical transformation at normal energies, that would be possible, is to reduce it. A wide range of CO2 conversion/reduction techniques are under investigation [5] which include,

- Chemical Reduction by metals which occur at relatively at high temperatures

(1)

(2)

(3)

ii. Thermo-chemical Conversion

(4)

iii. Radio chemical Method

(5)

iv. Photo chemical Conversion

(6)

v. Bio-Chemical Conversion

(7)

vi. Electro-Chemical Conversion

(8)

vii. Bio Photochemical conversion

The bio part of the energy consists in catalysis and information content of an enzyme

(9)

viii. Electro photochemical conversion

(10)

Conventional catalytic reduction of CO2 to chemicals (formic acid, methanol, methane etc.) with external hydrogen is feasible [6] but hydrogen from renewable resources is to be utilized, to render the process viable and sustainable.

Amongst the processes listed above, photochemical conversion processes (direct photochemical, photo-electrochemical and photo-biochemical conversions), that utilize abundantly available solar energy, qualify as sustainable processes and hence being pursued with tremendous interest. A brief account of photo catalysis and photosynthesis, which form the basis for all types of photo catalytic conversions in general, and CO2 reduction in particular, is presented in the following section.

1.3 Photo catalysis and Photo synthesis

Photo catalysis involves an additional means of activation of molecules, besides the normal thermal and chemical catalytic action that facilitate any typical chemical reaction. In simple terms, photo catalysis refers to any reaction that requires simultaneous presence of a photo active catalyst and light energy source [7] and can be expressed as

hν, Catalyst

R                           P (ΔGR→P ˂ or ˃ 0)                            (11)

Photo-generated electrons and holes react with adsorbed reactant molecules on a photo active semiconducting catalyst surface, bringing about the reduction or oxidation of the adsorbed species. The reaction pathways in both processes according to Ravelli et al [8] are illustrated in Fig. 1.2A & B below:

Fig.1.2 Reaction path ways followed [A] in a thermal reaction (R-P) catalyzed by C via intermediate I’; [B] in a photo catalyzed reaction (the catalyst C is active only in the excited

state, but the chemical transformation of R occurs entirely on the ground state surface [Reproduced from Ref.8].

The overall reaction cycle in a typical photo catalytic conversion is depicted as shown in Scheme.1.1.

.

Scheme.1.1. Photo catalytic conversion of R to P by catalyst C [Reproduced from Ref.8]

Historically, photo catalysis has played a pivotal role in the evolution of life on earth. Photo synthesis, the process so vital for the plant life, is essentially a photo catalytic process, involving the conversion of CO2 and water to carbohydrates, with the release of oxygen into the atmosphere. Chlorophyll acts as collector of solar energy and the conversions take place with the help of a series of enzyme catalysed process steps. This phenomenon of photo synthesis marked the beginning of process of evolution of various forms of life on earth that survive on oxygen.

Both photo catalysis and photo synthesis processes utilize the sustainable source of energy,

the sunlight, available abundantly at zero cost (Scheme.1. 2).

Scheme 1. 2. Photo catalysis and Photosynthesis [Reproduced from Ref.X]

Photo catalytic reduction (PCR) of carbon dioxide by water to yield hydrocarbons, the process commonly referred to as “artificial photosynthesis”, dates back to nearly nine decades, in 1921-22 [Ref]. The process has now attained tremendous importance on global level, since it is considered as one of the means of controlling the current atmospheric carbon dioxide levels (green-house gas effect) by converting it into to fuels and chemicals and the role of CO2 as source of energy.

1.3.1 Applications of photo catalysis

In the current energy starved scenario on the earth, studies on the science and technology of photo catalytic processes that utilize sunlight, have gained tremendous importance and hence being explored for a variety of applications. Photo catalysis is an emerging as one of the possible means of providing viable solutions to the challenges related to two major issues on the global front, energy and environment. Solutions in the form of different photo catalytic conversions/ processes, mostly based on titania as the photo catalyst, are represented in Scheme.1.3.

Scheme.1.3. Major applications of photo catalysis

These applications are at various stages of development, with few of them like, self-cleaning, anti-fogging and anti-bacterial applications being practiced already on large scale.

Photo catalytic processes could be utilized for converting solar energy into other useful forms of energy like, hydrogen via splitting of water and hydrocarbons (methane, methanol etc.) which are now collectively termed as “solar fuels”, by photo catalytic reduction of CO2 with water. Besides, photo catalytic oxidation/ degradation processes help in the elimination of harmful pollutants in air/liquid/water streams in a safe manner, resulting in the conservation of environment. There has been an explosive growth of applications of photo catalysis as evidenced by the fact that from the year 2000 onwards around 1300 international patents (latest figures to be included) per year have been filed, most of them pertaining to the application of titania as photo catalyst for pollution control.

While the practical applications of photo catalysis in the area of pollution control has been demonstrated successfully, the applications on energy front, for hydrogen production by water splitting and hydrocarbons from CO2 and water are still at infant stages of development.

1.4. CO2 photo reduction with water- Process features

The CO2 reduction is a thermodynamically uphill process as illustrated by its standard free energy of formation (ΔG° = -394.359 kJ/mol) [9]. Economical CO2 fixation is possible only if renewable energy, such as solar energy is used as the energy source. Equally difficult is the reduction/ splitting of water using solar radiation to yield hydrogen and hence requires similar combination of activation steps. We can now consider two different processes for CO2 reduction namely,

- Direct photo reduction of CO2 using water as a reductant

- Photo catalytic splitting of water to generate hydrogen and further reaction of this hydrogen with carbon dioxide forming C1–C2 fuels.

The most ideal and desirable process would then be the simultaneous reduction of CO2 and water to yield hydrocarbons, which essentially works out to artificial photosynthesis. Photo catalytic process occurs via the direct absorption of photons with energy greater than or equal to the band gap of the photo catalyst, resulting in the generation of electron-hole pairs. The initial excitation and electron energy transfer to the adsorbed reactants on the photo catalyst make chemical reactions in the photo catalytic process possible.

The utilization of solar energy via chemical storage can be achieved by photo catalytic or photo-electrochemical activation of light-sensitive catalytic surfaces. When comparing the two systems, photo catalytic system is simpler, easy to construct and operate.  The primary steps involved in the photo catalytic reduction of CO2 to hydrocarbons include:

Fig. 1.3 Transformations during photo catalytic reduction CO2 with water [10] Reproduced from? (No Ref. to Fig 1.3 in the text)

- Photo generation of charge carriers by excitation

- Bulk diffusion and interfacial transfer of charge carriers to surface species

- Reduction/oxidation and further conversion of surface species to different hydrocarbons

Photo generated electrons bring out the reduction of CO2 to hydrocarbons and holes facilitate oxidation of water. While the elementary process steps/ mechanism of photo catalytic water splitting have been established to an acceptable level, there is little clarity on the reaction pathways that lead to the conversion of CO2 to hydrocarbons.

1.4.1 Thermodynamic features

Hydrogen formation from water involves a free energy change (ΔG0) of 237 kJ/ mol and an enthalpy change (ΔH0) of 285 kJ/mol; the corresponding values for CO formation from CO2 are 257 and 283 kJ/mol at 25°C (1atm). Hence, the minimum energy required for water and CO2 splitting processes are 1.229 and 1.33 eV (per photon) respectively. In theory, the band gap of a photo catalyst used for splitting/ reduction of water /CO2  should be at least 1.33 eV [11]. One, two, four, six and eight electron reduction potentials (vs. NHE) for CO2 reduction and H2O oxidation at pH 7 and at 25°C, assuming unit activities for all gaseous and aqueous species are given below [9].

Reaction E0redox V vs NHE at pH 7

-0.41		(12)

-0.82				        (13)

-1.9                    			     (14)

-0.49		      		  (15)

-0.53				        (16)

-0.48 			            (17)

-0.38                    			(18)

-0.24                   			(19)

From the above scheme it is clear that CO2 photo reduction is not a single-step reaction. Upon transfer of one electron, the structure changes from linear to bent configuration, which results in irreversible reduction [5]. Additionally, single electron transfer to CO2 is highly endergonic, because of the negative adiabatic electron affinity of CO2.

The initial step in the photo catalytic reduction of CO2 is the generation of electron-hole pairs upon absorption of photons of energy greater than or equal to the band gap of the photo catalyst. Subsequently, photoelectrons are utilized for the reduction of CO2 and hole for oxidation of water. However, electron-hole recombination process, which is two to three orders of magnitude faster, competes with the desirable redox processes. Therefore, electron-hole recombination process has to be minimized by some means, to increase the efficiency and improve the rates of CO2 photo reduction. Besides the recombination, many other factors such as incident light intensity, fraction of the incident light absorbed by the photo catalyst, the type of the catalyst and its particle size, specific surface area, structural and photo-physical properties etc. are known to influence the kinetics of CO2 photo reduction.

1.4.2 Choice of catalysts - Guiding principles

It is again essential that the photo generated electrons should possess requisite energy, as indicated by the thermodynamic criteria, to facilitate the reduction of CO2. The chemical potentials of the photo generated electrons and holes highly depend on the band edge positions of the semiconductor. This means that the conduction band bottom energy level of the photo catalyst has to be more negative with respect to the energy for CO2 reduction and the valence band top has to be more positive with respect to the energy for oxidation of water. Thus, the choice of the catalyst for CO2 photo reduction with water is determined by the relationship between energy levels of conduction and valence bands vis-a-vis the energies for CO2 reduction and water oxidation. Pioneering studies on photo electro catalytic reduction of CO2 on various semiconducting oxides has brought out the basic criteria for the catalytic activity. This guiding principle has been illustrated effectively by Inoue et al. [12] in the relationship between the energy levels of conduction and valence bands and those of the redox couples as depicted in Fig. 1.4.

Fig.1.4 Conduction band and valence band potentials for photo catalysts relative to the

Energy levels of redox couples in water [12].

Semiconductors like SiC, GaP, CdS, ZnO and TiO2, which satisfy the above criteria and are active for photo reduction of CO2 while oxides like WO3 and SnO2 whose conduction band levels are below that for CO2 reduction, have failed to perform. Energy levels of conduction and valence band Vs those for redox couple and the life time of charge carriers, prolonged by reduced recombination, are the two fundamental criteria to be considered for the selection of the efficient photo catalyst for CO2 photo reduction.

1.5 Catalysts for photo reduction of CO2 with water

A remarkable feature of PCR of CO2 is that it could emerge as a carbon neutral process [13], where in carbon emissions are recycled back as useful fuels/chemicals. The process involves two major steps; photo catalytic splitting of water to yield hydrogen, which in turn, helps in the photo reduction of carbon dioxide to different hydrocarbon products in the second step. Design of effective catalysts for such a complex process, involving multi-electron transfer steps, holds the key for the viability of the process.

Although many semiconductors have smaller band gaps and absorb in the visible range (e.g. CdS and Fe2O3 with band gap values of 2.4 and 2.3 eV, respectively), just a few of them are catalytically active because the energy levels of either the conduction or valence bands are unsuitable for CO2 reduction and/or water oxidation (Fig. 1.4). This limitation, together with poor photo-corrosion stability of many semiconductors, limits significantly the number of potential photo catalytic materials for CO2 photo reduction.

Large-band-gap semiconductors are the most suitable photo catalysts for CO2 reduction, because they provide sufficient negative and positive redox potentials in conduction bands and valence bands, respectively. The disadvantage of using wide band-gap semi-conductors is the requirement of high energy input [14-18].

1.5.1 The need for modifications in the catalysts

The photo catalytic activity of a typical semiconductor like titania is initiated by the absorption of light energy corresponding to or higher than the band gap energy, resulting in the generation of electrons and holes. The electron-hole pair, on migration to the semiconductor surface, interacts with the adsorbed reactants to facilitate reduction and oxidation process respectively. In the absence of such an energy transfer, the pairs recombine with the loss of energy. Electron-hole recombination process, which is two to three orders of magnitude faster, competes with the desirable redox processes. Therefore, the recombination process needs to be minimized by suitable modifications, to increase the efficiency. Hence modifications in wide band gap semiconductor (band gap engineering) are aimed at dealing with the two major issues, namely, extending light absorption range beyond UV region and arresting the recombination of charge carriers.

By suitable modification of the band gap, ie., reduction in band gap by creation of additional/impurity energy levels, light absorption range/wavelength could be increased. In the case of titania, light absorption range is increased to cover part of visible region [16, 17]. Arresting the recombination rate increases the life time of photo electrons and holes, thus leading to a corresponding increase in photo catalytic activity.

1.5.2 Major types of modifications in the catalysts

A number of strategies have been devised to bring about the modifications in wide band gap semiconductors, which can be broadly classified as:

- Doping with metal cations and anions

- Coupling with other semiconducting oxides

- Sensitization with light harvesting compounds/dye molecules

- Plasmon resonance induced by specific metals

Excellent and exhaustive reviews describing the changes brought about by these means in the photo-physical properties of the photo catalyst and the consequent improvements observed in the photo-catalytic properties have been compiled [5, 9, 18-29]. The main features of these modifications and the implications in the properties of semiconductors, especially for titania, are summarized in the Table. 1.2, and presented graphically Fig. 1.5

Table 1.2 Implications of different modifications in titania [20]

| Modifications | Implications/Mode of action |
| --- | --- |
| Doping of metals/metal ions | - Act as electron traps and facilitate charge carrier separation - Introduce impurity states and induce visible light absorption - Absorb visible light via surface plasmon resonance (SPR) |
| Doping of anions | - Narrowing of band gap due to mixing of p states of dopants (N, S) with O 2p states in the valance band of TiO2. - Introduce impurity states above the valence band of titania - Both states induce visible light absorption |
| Coupling with semi-conductors | - A narrow band gap semiconductor, with appropriate energy levels, absorbs visible light and transfers excited electrons into the conduction band of titania. UV light source not needed - Besides visible light activity, effective separation of charge carriers is achieved |
| Sensitization with light harvesting components /dyes | - Light absorbing components can absorb visible light and inject photo-excited electrons into the conduction band of titania. - Besides visible light activity, effective separation of charge carriers is achieved |

Fig.1.5 Implications of modifiers on the electronic structure of Titanium dioxide [20]

1.6 Influence of experimental parameters

Photo catalytic activities highly depend on the experimental conditions such as, the amount of catalyst, light intensity, lighting area, reactor volume, type of reactor, temperature and pressure etc. Intrinsic properties of semiconductor photocatalyst like,  particle/ crystallite size [30], phase composition [31], surface area, surface hydroxyls, lattice defects and the type and level of dopants (metals and non-metals), morphology (powder, nano particles, nano tubes, nano rod and hollow nano spheres), structural features and photo-physical properties influence its performance [15-29]. Photo catalytic activity and phase transition behavior of TiO2 are significantly influenced by the preparative conditions and methods [32-34]. This explains the wide variations in activity and product patterns observed for the same photo catalyst by different authors. For example, a standard/reference catalyst Degussa P-25 (TiO2) shows wide difference in efficiency in the results published by different authors during the period 1993 to 2009 as shown in Table. 1.3 (Ref?). Different experimental conditions adopted could be the other major factor that affects yield data, which shows variations in total yield as well as the product patterns. Hence, rationalization of activity and product patterns in terms of photo-physical properties has been a difficult task.

Table 1.3 CO2 photo reduction with water on P-25 TiO2 - Literature reports (Ref?)

| Sr. No | Products * | CH4 | CH3OH | Reactor type | Reactants | Light source | T (K) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | CH4, C2H6 CH3OH | 0.9 | Tr | Quartz cell | CO2 in H2O | 500W Hg > 310 nm | 278 | 35 |
| 2 | H2, CO, CH4 | 2.0 | Tr | Quartz cell | CO2 in H2O | 1000W Hg<700 nm | 343 | 36 |
| 3 | H2, CH4, CnHm | 4.74 5.68 6.42 |  | Miniaturized reactor | CO2 in H2O | 200W Hg /Xe <900 nm | 278 373 473 | 37 |
| 4 | CH4, HCOOH | 0.43 |  | SS vessel | CO2/ IPA | 4200W, Xe |  | 38 |
| 5 | CH4, CH3OH | 0.35 |  | Quartz cell | CO2: H2O 1:5 | 75W Hg 254 nm | 323 | 39 |
| 6 | CH3OH | - | 6.37 | Inner irradiator cell | CO2 in NaOH | 8W Hg 250 nm | 323 | 40 |
| 7 | CH4, CH3OH |  | 93.75 | Inner irradiator cell | CO2 in NaHCO3 | 15 W Hg 365 nm |  | 41 |
| 8 | CH3-COOH |  | 1.8 | Quartz window | Liq. CO2 | 990W Xe Arc lamp |  | 42 |
| 9 | CH4 | 0.33 | - | Quartz cell | CO2: H2O 1:5 | 100W Hg >250 nm | 323 | 43 |
| 10 | CH4 | 0.001 |  | Top illumination | CO2: H2O 1:5 | 4.8W 253.7 nm | 311 | 44 |
| 11 | CH4 | 14.6 |  | Glass plate | CO2: H2O 1:5 | 15W 365 nm | 296 | 45 |
| 12 | CH4 | 3.51 |  | Annular reactor | CO2in NaHCO3/ IPA | 450WHg | 293-298 | 31 |
| 13 | CH3OH |  | 430 | Inner irradiator cell | CO2 in NaOH | 400W halide 300-600 nm | 315 | 46 |

* Products – in micro moles per hour per gram of catalyst

1.6.1 Effect of wavelength, band gap and light intensity

Semiconductors absorb light radiation with the threshold wavelength that provides sufficient photon energy to overcome the band gap between the valence and conduction bands. This threshold wavelength, required to promote electrons to the excited state, corresponds to the minimal photon energy and depends on the band-gap energy, e.g. for TiO2 anatase with band gap energy 3.2 eV, it is about 387.5 nm. Irradiation using the light with shorter wavelength (254 nm) is significantly more effective for the CO2 reduction using TiO2 than that with the longer wavelength (350 nm) [47, 48]. The wavelength (λ) of the light used influences the yield of products as observed by Fan et.al [49] in their studies on N (4% w/w) and Ni (6% w/w) co-doped titania for CO2 reduction with water. For this catalyst formulation, Fan et al [49] observed methanol yields of  482, 253.5 and  120.5 (all in μ moles/g-cat) with radiations of wavelength 254 nm,  365 nm and 400-780 nm respectively, thus clearly bringing out the influence of the wavelength of the light used. Electrons in excited states are produced via electronic transitions the probability of which depends on the light intensity. The CO2 reduction rate increases linearly with the light intensity and at mid-range light intensities, the photo catalytic reaction rate is dependent on the square root of light intensity. At high light intensities the rate is independent of the light intensity [18].

Variations in the wavelength of radiation used can also affect the rate of formation of products as observed by Liu et al [50] on BiVO4 catalysts (Table.1.4). Monoclinic BiVO4 is found to be

Table 1.4 Rates of methanol and ethanol formation with radiations of different wavelengths [Reproduced from Ref. 50]

| BiVO4 | Production rate a/μmol h-1 | 300W Xe arc lamp with UV cut off filter | 300 W Xe arc lamp without UV cut off filter | 36W fluorescent lamp |
| --- | --- | --- | --- | --- |
| Monoclinic | Ethanol | 21.6 | 406.6 | 2.3 |
|  | Methanol | 0 | 0 | 1.8 |
| Tetragonal | Ethanol | 1.1 | 4.9 | 0.6 |
|  | Methanol | 0 | 0 | 0.6 |
| a The rate was determined on the basis of the average production rate after 80 min of irradiation |  |  |  |  |

more active than the tetragonal form. Selective formation of ethanol is observed using 300 W UV radiations, with and without UV cut-off filter. But with 36 W lamp, both alcohols are formed at nearly same.

1.6.2 Influence of reaction pressure

Mizuno et al [51] observed that CO2 photo reduction with water containing dispersed TiO2 increased with the increase in CO2 pressure. Increase in the solubility of CO2 in the liquid phase (water as well as aqueous 0.2N NaOH solution) at elevated pressure and the consequent increase in the concentration CO2 in the solution phase is responsible for the observed increase in CO2 reduction (Fig. 1.6). Similar observations on the effect of pressure have been observed by Hisao Hori et al [52].

Kaneco et al [53, 54] studied the CO2 photo reduction using TiO2 powders in liquid CO2 medium. Carbon dioxide has limited solubility in water. Also reduction of CO2 is competitive with hydrogen formation via water. To overcome this disadvantage, liquid CO2 system has been explored. The protonation reaction was performed using water after the end of illumination?. The main reduction product was exclusively formic acid. Tan et al [44, 55] studied the photo catalytic reduction of carbon dioxide using TiO2 pellets. Pellet increased the contact areas and adsorption capacity. Their yield was significant when compared to thin film coating technique.

Fig.1.6. Effect of CO2 pressure on its photo reduction (medium, purified water; irradiation time, 24 h; catalyst, TiO2): ∆- CH4, ○-C2H4, □- C2H6. [Reproduced from Ref.51]

1.6.3 Influence of titania particle size

Koci et al [30] studied the effect of TiO2 particle size on photo catalytic reduction of carbon dioxide. As the particle size decreased, higher yields of methanol and methane over the TiO2 nano particles under the illumination of light were obtained. The optimum particle size corresponding to the highest yields of both products was 14 nm (Fig. 1.7). For particles with crystallite sizes < 14 nm, conversions dropped due to a combination of electronic (increase in recombination rates) and optical properties. The observed optimum particle size was a result of competing effects of specific surface area, charge–carrier dynamics and light absorption efficiency.

Fig.1.7. A & B Dependence of product yields on particle size of titania (after 24 hrs of

irradiation) [Reproduced from Ref.30]

1.6.4 Influence of type of photo reactors and reaction media

The design of photo reactor is an important aspect in CO2 photo reduction process with water, which could significantly influence the selectivity of products and efficiency of the photo catalyst/process. As stated by O. Ola et al [56], an ideal photo reactor must have uniform light distribution throughout the entire system in order to achieve optimum results. The two parameters which determine the type of photo reactors utilized in CO2 photo reduction are the phases involved ie., multiphase, gas-solid, liquid-solid, gas-liquid-solid etc, and the mode of operation ie., batch, semi-batch or continuous flow of reactants.

Fig. 1.8. Schematic diagram for different types of photo reactors (A) slurry reactor design with top illumination, (B) optical fiber reactor design with side illumination and (C) internally illuminated reactor with top illumination. (Adapted from Ref.  56).

The photo catalyst can be used in either suspended or immobilized forms in different reactor configurations. Schematic representation of three types of reactor geometry are shown in Fig. 1.8, which are, A. Slurry reactor design with top illumination, B. optical fiber reactor design with side illumination C. internally illuminated reactor with top illumination [56].

Koci et al. [46] studied the influence of reactor geometry on photo reduction of carbon dioxide using two annular batch reactors. The dependence of product yields on the reactor diameter and on the volume of the liquid phase confirmed the fact that the requirement of perfect mixing is difficult with the annular configuration of the reactor. The highest yields of the photo catalytic reduction were achieved in a configuration where the lamp just touches the surface of the liquid in the reactor and the configuration of the reactor was not annular. As shown in Table 1.3/1.5?, different types of photo reactors and reaction medium significantly alter the product selectivity for a commercial P-25 TiO2 photo catalyst. Advantages and disadvantages of different types of photo reactors for application in CO2 photo reduction are given in Table 1.5.

( Font size is different in Table 1.5. Pl correct)

Table 1.5 Advantages and disadvantages of photo reactor systems Adapted from Ref. 56

| Reactor design | Advantages | Disadvantages | Ref. |
| --- | --- | --- | --- |
| Fluidized and slurry reactor (multiphase) | (I) Temperature gradients inside the beds can be reduced through vigorous movements caused by the solid passing through the fluids (II) Heat and mass transfer rates increase considerable due to agitated movement of solid particles. (III) High catalyst loading | (I) Filters (liquid phase) and scrubbers (gas) are needed. (II) Flooding tends to reduce the effectiveness of the catalyst. (III) Difficulty of separating the catalyst from the reaction mixture (IV) Low light utilization efficiency due to absorption and scattering of the light by the reaction medium (V) Restricted processing capacities due to mass transport limitations | 19 [57, 58] |
| Fixed bed reactor | (I) High surface area (II) Fast reaction time (III) The conversion rate per unit mass of the catalyst is high due to the flow regime close to plug flow (IV) Low operating costs due to low pressure drop Variants of fixed bed designs | (I) Temperature gradient between gas and solid surface is common | [59, 60] |
| Monolith reactor | (I) High surface to volume ratio and low pressure drop with high flow rate can be achieved. (II) Configuration can be easily modified | (I) Low light efficiency due to opacity of channels of the monolith | [61, 62] |  |
| Optical fiber reactor | (I) High surface area and light utilization efficiency. (II) Efficient processing capacities of the catalyst | (I) Maximum use of the reactor volume is not achieved. (II) Heat build-up of fibers can lead to rapid catalyst | [62, 63] |  |

Wu et.al [64-67] applied an optical fibre reactor to the photo reduction of CO2 with H2O using TiO2, Cu/TiO2, Ag/TiO2, Cu–Fe/TiO2–SiO2 and dye-sensitized Cu–Fe/P25 catalysts coated on optical fibres. Compared with a traditional packed-bed reactor, an optical fibre reactor provides a medium to transmit light uniformly throughout a reactor and hence higher conversion (Table. 1.6) is achieved. In addition, a higher processing capacity is possible because the photo catalyst can be dispersed on the optical fibers with large surface area in a given reactor volume.

Table 1.6 Production rate of methane and ethylene over TiO2 based-catalysts under artificial

light- Influence of the type of photo reactor on reaction rate [64-67]

|  | Production ratea [μmol (gcat)-1 h-1] |  |
| --- | --- | --- |
|  | Ethylene | Methane |
| Cu(0.5 wt%)-Fe(0.5 wt%)/TiO2/glass plate | 0.049 | 0.060 |
| Cu(0.5 wt%)-Fe(0.5 wt%)/TiO2/optical fiber | 0.575 | 0.914 |
| N3-dye- Cu(0.5 wt%)-Fe(0.5 wt%)/TiO2/glass plate | 0.033 | 0.148 |
| N3-dye- Cu(0.5 wt%)-Fe(0.5 wt%)/TiO2/optical fiber | 0.562 | 0.847 |
| a Production rates were determined on the basis of the average value after 4h of irradiation. The artificial light was in the wavelength range of 320-500 nm with intensity of 225 mW cm-2. |  |  |

When CO2 present in the atmosphere dissolves in water it is mostly present in the form of carbonate. Many authors have studied photo catalytic reduction of carbonate to form various chemicals. Ku et al. [41] studied the photo catalytic reduction of carbonate in aqueous solution by the UV/TiO2 process. The photo catalytic reduction of carbonate proceeded faster in acidic solutions than in alkaline solutions. The main products of the photo catalytic reduction of carbonate by the UV/TiO2 reduction process were found to be methanol and methane. A Langmuir–Hinshelwood type kinetic equation was developed for modeling the photo catalytic reduction of carbonate.

Sayama et al [68] investigated the effect of carbonate salt addition on the photo catalytic decomposition of liquid water over Pt–TiO2 catalyst. It has been found that an addition of carbonate salts to Pt-loaded suspensions led to highly efficient stoichiometric photo- catalytic decomposition of liquid water into H2 and O2. Neither the pH nor cation directly contributes to the water splitting. The presence of a high concentration of carbonate ions is essential for the catalytic photodecomposition of water. The carbonate ion affects both the Pt particles and the TiO2 surface. The Pt was covered with some titanium hydroxide compounds and therefore, the rate of the back reaction (H2O formation from H2 and O2) on the Pt was suppressed effectively in the presence of carbonate ions. On the other hand, the TiO2 surface was readily covered with several types of carbonate species. It is considered that these carbonate species aid desorption of O2 from the TiO2 surface.

In the place of pure water as the medium for dispersion of the catalysts, in some cases aqueous solution of KHCO3 [46] or NaOH has been used. Martin Reli et al [46, 69] studied different reaction media, such as, NaOH, NaOH + Na2SO3, NH4OH, NH4OH + Na2SO3 to understand the influence of reaction medium on the photo catalytic reduction of carbon dioxide. It was found that NaOH was better reaction medium than NH4OH for the yields of both gas phase [CH4, CO] and liquid phase [CH3OH] products. Some authors tried with organic reaction media like methanol, propan-2-ol which itself get oxidized during reaction and hence unfavorable for the potential separation of products from CO2 reduced products [69]. The use of NaOH as reaction medium is also beneficial since OH- ions act as hole scavengers, thereby retarding electron-hole recombination and simultaneously, alkaline solution increases solubility of CO2 vis-à-vis pure water [40]

1.6.5 Photo reduction with other reductants

Some researchers have attempted to replace water with other reductants [70]. This provides a high reaction yield and high selectivity to desired products by changing the mechanism. Liu et al. [71] conducted an experiment with CdS in various solvents including water, methanol, ethanol, and 1-propanol with dielectric constants of 80, 33, 24.3, and 20.1, respectively. The results indicated that, if low-dielectric constant solvents or low-polarity solvents are used, CO2- anion radicals can be strongly adsorbed on the surface through the carbon atom of another CO2- anion radical pre-sorbed on surface Cd sites because these radicals are not completely solvated by low-polarity solvents. Here, CO is produced as the major reduction product of CO2. If a high-dielectric-constant solvent is used (e.g., water), the CO2- anion radicals can be greatly stabilized by the solvent, resulting in weak interactions with the photo catalyst surface. Similar effects of solvents have been observed on titania embedded in SiO2 matrices [72]. Subsequently, the carbon atom of the radical tends to react with a proton to produce formic acid. Kaneco et al. [38] and later Dey [73] showed that photo catalytic reduction of CO2 using TiO2 suspension in aqueous solutions containing 2-propanol as a hole scavenger leads to the preferential formation of methane.

1.7 Classification of catalyst systems

For the sake of clarity and meaningful comparative study, the catalyst systems studied so far have been grouped in the following manner:

- Catalysts based on pure titania

- Titania catalysts modified with metals/metal oxides

- Titania catalysts modified with anions

- Titania catalysts dispersed on meso porous materials

- Titania catalysts modified with sensitizers

- Metal oxide catalysts-mono, binary & ternary oxides

Details on the application of these catalysts towards CO2 photo reduction with water have been compiled in the Tables 1.7 Table 1.14.

Table 1.7 Studies on pure titania based catalysts

Table. 1.8. Studies on metal doped titania catalysts

Table. 1.9. Studies on anion doped titania catalysts

| S. No | Photocatalyst | Type of Reactor used | Conditions |  | Light Source/ Intensity | Product formation | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Reactant | Temp. |  | µmol/g cat |  |
|  |  |  |  | (K) |  |  |  |
| 1. | S doped TiO2. | batch type reactor | CO2 + H2O | Sun light | 8 mW·cm− 2 UV lamp | CH3OH, C2H5OH | 125 |
| 2. | N doped TiO2 nanotubes | quartz reactor | CO2 in 0.1 N NaOH | 308 | 500W W-Halogen lamp | HCOOH - 12475.8±266.7, CH3OH - 1132.6±45.4, HCHO -921.6±24.1 | 126 |
| 3. | N-doped mesoporous TiO2 with cocatalyst Pt, Ag, Au | Quartz tubular reactor | CO2 + gaseous H2O | 333 | 350W Xe lamp | CH4 - 5.7 in 2 h | 127 |
| 4. | I doped TiO2 | Stainless steel with quartz window | (CO2+H2O) vapors | RT | 450W Xe lamp |  | 128 |
| 5. | N/100 | Semi batch | CO2 + H2O | RT | - | CH3OH - 23/h | 129 |
| 6. | g-C3N4–N–TiO2 (CT–70) | Gas closed circulation system | (CO2 +H2O) vapors | 303 | 300 W Xe arc lamp | CO - 14.73 | 130 |
| 7. | N–TiO2/spirulina | Slurry reactor | CO2 + H2O | RT | 13 W lamp | H2 - 144.99* CH4-0.48 C2H4 - 0.12 C2H6 - 0.17 *mmol/g | 131 |

Table. 1.10. Studies on titania supported on different materials

| S. | Catalyst | Type of | Conditions |  | Light Source | Product | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| No |  | Reactor used |  |  | /Intensity | formation |  |
|  |  |  | Reactant | Temp |  | µmol/g cat |  |
|  |  |  |  | (K) |  |  |  |
| 1. | TiO2- loaded Nafion films | Cylindrical high Press. optical cell with quartz window | 2000 psia CO2. |  | 990 W Xe | HCOOH –190, CH3OH- 280, CH3COOH –30 | 132 |
| 2. | MW-CNT supported TiO2 | SS reactor. | CO2 and H2O vapor | 308 | UV 365 nm | CH4- 58.7, HCOOH- 93.4, C2H5OH- 149.4 | 45 |
| 3. | CdSe/Pt/ TiO2 hetero structure | Custom-built photo catalysis cell | 3 Torr H2O vap. 0.3 Torr CO2 | 308 | visible light 420 nm | CH4, CH3OH, CO, H2 (CO2 conv. rate 0.8 ppm g-1 h-1) | 133 |
| 4. | Graphene - TiO2 nano Comp. |  |  |  | UV - 365 nm | CH4 – 8.5 | 134 |
| 5. | CdS–(Bi2S3), TNT | Continuous- flow reactor | CO2 in NaOH, Na2SO3 | 308 | 500 W Xe | CH3OH - TNT - 102.5, TNTs - CdS - 159.5, TNTs–Bi 2S3 - 224.6 | 135 |
| 6. | nafion coated Pd–TiO2 | Quartz reactor | CO2 in Na2CO3 | RT | 300 W Xe lamp | CH4 - 7 C2H6 - 0.7 | 136 |
| 7. | mesoporous TiO2 /graphitic carbon microspheres | Stainless steel reactor | CO2+H2O vapor | 303 | 300 W Xe lamp | CH4 - 10.3 | 137 |
| 8. | CNTs@Ni-doped TiO2 | Quartz reactor | CO2+H2O vapor | RT | visible light 400 nm | CH4 - 0.145/h | 138 |
| 9. | graphene-Ti0.9O2 hollow spheres | Cylindrical stainless steel quartz window | CO2+H2O vapor | RT | 450 W Xe lamp | CO, CH4 | 139 |
| 10. | graphene-TiO2 nanosheets | Glass reactor | CO2+H2O vapor | RT | 300 W Xe lamp | CH4 - 8 C2H6 - 16.8 | 140 |

Table. 1.11. Studies on titania dispersed on porous materials

| S. | Catalyst | Type of | Conditions |  | Light Source | Product | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| No |  | Reactor used |  |  | /Intensity | formation |  |
|  |  |  | Reactant | Temp |  | µmol/g cat |  |
|  |  |  |  | (K) |  |  |  |
| 1. | Q-TiO2 embedded in SiO2 | Quartz cell | CO2 in IPA | 308 | 500 W Hg | CO, Formate | 72 |
| 2. | Pt on (a) Ti- ionexchanged (b) Ti in MCM-48 framework | Flat bottom quartz cell. | 734Pa CO2 | 328 | 75 W Hg/λ > 280 nm | CH4 – 12, CH3OH- 2. | 141 |
| 3. | Pt/TiO2 in Zeolites | Quartz cell | CO2 in H2O | 328 | Hg/λ >280 nm. | Ti in Oh sites- CH4, Td sites- CH3OH | 142 |
| 4. | Ti- silicalite mol. sieve |  | CO2, H2O vapor |  | UV laser 266 nm | CO, HCHO, CH3CHO. | 143 |
| 5. | Fluorination of Ti- FSM-1 | Quartz cell with a flat bottom. | CO2 in H2O | 323 | 100 W Hg/λ > 250 nm | Fluorination increases selectivity towards CH3OH | 39 |
| 6. | TiO2 in porous SiO2 thin film. | - | CO2 in H2O | 323 | 100 W Hg/λ > 250 nm | CH4- 70, CH3OH-10 | 144 |
| 7. | Ti –MCM- 41 | IR vacuum cell, 3.4 ml | 0.1 MPa CO2 | 298 | 266 nm | CO, O2, H2O confirmed as a e- donor. | 145 |
| 8. | Ru/TiO2, TiO2/SiO2 | Inner irradiation type (Batch mode) | CO2 in IPA | 308 | 1000 W Hg/365 nm. | CH3OH - 250, CH4 – 75. | 146 |
| 9. | Cu, Fe substitution in TiO2– SiO2. | Packed bed, circulated reactor 216 fibers | CO2 + H2O vapor | 348 | 150 W Hg/ 320–500 nm, &500–800 nm | Cu– Fe/TiO2 favors C2H4 formation, Cu– Fe/TiO2–SiO2 favored CH4 | 147 |
| 10. | 0.5%Cu/Ti O2–SiO2 | SS wall & quartz window. (continuous- flow). | CO2 in H2O vapour | 308 | Xe arc source, λ < 650 nm | CO - 60, CH4 – 10 | 148 |
| 11. | Cu2O/SiC | XPA-II photochemical reactor | CO2 in NaOH & Na2SO3 solns. | 308 | 500W Xe/200 to 700 nm | CH3OH - 191 | 149 |
| 12. | Ti-SBA-15 | Combinatorial photo reactors. | CO2 in H2O |  | 120W Hg/280 to 650. | CH4, C2H4, C2H6. | 150 |
| 13. | Cu/TiO2-SiO2 | SS wall with quartz window (continuous flow) | (CO2 + H2O) vapour | RT | Xe arc lamp | CO - 10/h CH4 - 60/h | 151 |
| 14. | 2 wt% Cu-TiO2-SBA 15 | Inner irradiation type(continuous mode) | CO2 in NaOH + H2O | 315 | 500 W halide lamp | CH4 - 627/h | 152 |
| 15. | Kaolinite/ TiO2 | Stirred batch annular reactor | NaOH | RT | 8 W Hg lamp | CH4 - 4.5 CO - 2.5 | 153 |
| 16. | 1, 3 wt% Ce–TiO2/ SBA 15 | Stainless steel with quartz window | CO2 + H2O | RT | 450 W Xe lamp | CO - 1 | 154 |
| 17. | Ti-KIT-6/Si-Ti = 100 | Pyrex glass reactor | CO2 + H2O | RT | 300 W UV lamp | CH4 - 4.4/h H2 - 2.2/h | 155 |
| 18. | TiO2 (20%)/KIT6 | Pyrex glass reactor | (CO2 + H2O) vapor | RT | 300 W lamp | CH4 - 44.56 CH3OH - 1.09 CO - 120.54 H2 - 44.56 | 156 |
| 19. | Mesoporous g-C3 N4 flakes | Closed gas circulation system | CO2 in NaOH | RT | 300 W Xe lamp, visible light 420 nm | CH3OH, C2H5OH | 157 |
| 20. | Si/TiO2 nanosphere | Stainless steel cell with quartz window | (CO2 + H2O) vapor | RT at 50 psi | 355 nm Laser lamp | CH3OH - 197 µM/100 mL | 158 |
| 21. | Cu/TiO2 monoliths | Pyrex glass reactor | (CO2 + H2O) vapor | RT | 200 W Hg/500 W halogen lamp | H2 - 12.5, CH3OH - 4, C2H5OH - 3, CH3CHO - 3 | 159 |
| 22. | TiO2/SiO2 | Quartz reactor | (CO2 + H2O) vapor | 298 | 300 W Xe lamp | CO - 3/h | 160 |
| 23. | Cu/GO | Cylidrical reactor | (CO2 + H2O) vapor | 303 | 300 W halogen lamp | CH3OH - 3/h, CH3CHO - 4/h | 161 |
| 24. | Ag-MWCNT @ TiO2 | Quartz reactor | (CO2 + H2O) vapor | 333 | 15 W energy saving light | CH4 - 6.34, C2H6 - 0.68 | 162 |
| 25. | Au-In/TiO2 | Cylidrical stainless steel with quartz window | CO2 + H2 | RT | 200 W Hg lamp | CO - 8982/h | 163 |
| 26. | Pt-RGO/TiO2 | Quartz reactor | (CO2 + H2O) vapor | 333 | 15 W energy saving light | CH4 - 1.7 | 164 |
| 27. | Cu–TiO2/ZSM-5 | - | CO2 in NaHCO3 soln. | 298 | 254 nmUV-lamp | CH3OH - 50.05 | 165 |
| 28. | Ca/TixSi MCM-41 | Quartz reactor | CO2 + H2O (1:2) | 303 | 6 W cm-2Hg lamp | CH4 - 82/L | 166 |

Table. 1.12. Studies on different metal oxides

| S. | Catalyst | Type of | Conditions |  | Light Source | Product | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| No |  | Reactor used |  |  | /Intensity | formation |  |
|  |  |  | Reactant | Temp |  | µmol/g cat |  |
|  |  |  |  | (K) |  |  |  |
| 1. | Cu/ZrO2 | Inner irradiation quartz reactor | CO2 in NaHCO3 (pH 2.3) | 308 | 400-W Hg UV Hg | CO - 2.5 | 167 |
| 2. | TiO2 (P25), ZrO2 | Circulating Pack.bed quartz reactor | 1.1 atm CO2 | 316 | UV/365 & 254 nm. | TiO2- CH4- .21, CO-0.28, C2H6 - 0.2, ZrO2- CO- 1.24 With H2+H2O | 168 |
| 3. | Pd, Cu on Mixed oxides of MgO, ZnO Al2O3,TiO2, SiO2. | Batch reactor | CO2 in 0.5M KHCO3 (pH = 7.5) | 308 | 250 mW Hg. | C1-C3 products. Acidic supports- CH4, HCHO, HCOOH. Basic supports-C2H6, C2H5OH, Acetone | 169 |
| 4. | MgO | Closed static system | CO2 & H2 | 308 | 500 W Hg | CH4,CO. | 170 |
| 5. | Ga2O3 | Closed circulating system- Quartz | CO2: H2: (150:50 µmol). | 308 | 200W Hg–Xe. | CO – 2.1 | 171 |
| 6. | ZrO2 | Quartz reactor | CO2 : H2 or CH4 = 150:50 (µmol). | 308 | 500W Hg | CO – 9.5 | 172 |
| 7. | Meso Ga2O3 | Quartz window- closed chamber | CO2 in H2O | 300 | 300 W Xe | CH4 – 2.9 | 173 |
| 8. | WO3 nanosheets | Pyrex glass cell | CO2 + H2O vapor | RT | 300 W Xe arc, visible light 420 nm | CH4 - 16 | 174 |
| 9. | rectangular sheet-like WO3 | Stainless steel reaction chamber | CO2 + H2O vapor | RT | UV Xe lamp | CH4 - 0.34 | 175 |
| 10. | W18O49 nanowires | - | CO2 + H2O vapor | RT | visible light 420 nm | CH4 - 4000* * ppm/g | 176 |
| 11. | Porous MgO/TiO2 | Continuous flow glass reactor | CO2 + H2O vapor | 423 | 400 W Xe lamp | CO - 30/h | 177 |
| 12. | g-C3N4 nanosheet | Stainless steel with quartz window | CO2 + H2O vapor | RT | 300 W Xe lamp | CH4 - 0.5, CH3CHO - 0.05 | 178 |
| 13. | g-C3N4/ Bi2WO6 | Glass reactor with quartz window | CO2 + H2O vapor | RT | 300 W Xe lamp | CO - 5.19/h | 179 |
| 14. | CNTs–TiO2 | Quartz reactor | CO2 + H2O | RT | 15 W energy saving light bulb | CH4 - 1.2 | 180 |
| 15. | CuO nanowire/ZnO | Cylindrical stainless steel with quartz window | (CO2 + H2O)vapor | RT | 400 W Xe lamp | CO - 1980/h | 181 |
| 16. | Fe2O3/Cu2O | Cylindrical stainless steel reactor | (CO2 + H2O)vapor | RT | 300 W Xe lamp | CO - 5 | 182 |
| 17. | Rh/Cr2O3/GaN | Pyrex reaction cell | (CO2 + H2O)vapor | RT | 300 W Xe lamp | CH4 - 85, CO - 100, H2 - 3.8 | 183 |
| 18. | ZnS | Fused silica reactor | CO2 in Na2S | 288 | 1 kW high-press. Hg (Xe) arc lamp | HCOO- - 440 µM | 184 |
| 19. | g-CN | Schlenk flask | CO2 in Co- (bpy)3Cl2 and TEOA mixture | 333 | 300 W Xe lamp | CO - 10.2, H2 - 2.8 | 185 |
| 20. | ZnO/ZnTe | Quartz reactor | CO2 + H2O | - | 300 W Xe lamp | CH4 - 356.51 | 186 |

Table 1.13. Studies on mixed metal oxide catalysts

| S. | Catalyst | Type of | Conditions |  | Light Source | Product | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| No |  | Reactor used |  |  | /Intensity | formation |  |
|  |  |  | Reactant | Temp |  | µmol/g cat |  |
|  |  |  |  | (K) |  |  |  |
| 1. | SrTiO3 in aq. suspension | UHV surf. Anal. chamber -batch | CO2 + H2O | Sun light | Natural sunlight | HCOOH, HCHO, CH3OH. QE=0.011% | 16 |
| 2. | CaFe204 | Quartz beaker | CO2/0.01 M NaOH (pH 5.8) | 308 | 500-W Hg | CH3OH, HCHO. | 187 |
| 3. | Pt/ K2Ti6O13 + Fe-Cu- K/DAY | Photoreactor with quartz window | CO2 + H2O | 308 | 300W Xe & 150W Hg. | CH4 -0.014 HCOOH- 3.88 CH3OH -1.45 C2H5OH- 0.35 | 188 |
| 4. | Pt/ K2Ti6O13 with Cu/ZnO. | Photo reactor with flat quartz window. | CO2 + H2O | 308 | 300W Xe- or 150W Hg. | CH4 - 0.86, HCOOH- 43.47, CH3OH - 18.93 HCHO -10.97. | 189 |
| 5. | ATaO3 (A= Li, Na, K) | Closed circulating reactor | CO2 : H2 = 150:50 (µmol) | 303 | 200W Hg–Xe | The order of activity- LiTaO3> NaTaO3> KTaO3. CO - 0.42 on LiTaO3 | 190 |
| 6. | Bi2WO6 square nanoplates | 230 mL glass reactor | CO2 + H2O |  | 300 W Xe | CH4 - 6 | 191 |
| 7. | Pt-NaNbO3 | Pyrex glass | CO2 + H2O | 308 | 300-W Xe | CH4–653*, *ppm/h/g | 192 |
| 8. | Pt/ NaNbO3 | Closed Pyrex cell | 80 kPa CO2 in H2O. | 308 | 300 W Xe | CH4 - 0.486 | 193 |
| 9. | Pt/Meso Zn-Ge (ZGON) |  |  |  | (λ > 400 nm) | CH4 - 26.8*, *ppm/h/g | 194 |
| 10. | Ag- ALa4Ti4O15 (A = Ca, Sr, & Ba) | Inner irradiation quartz cell | CO2 flow system (15 mL min-1). |  | 400W Hg | BaLa4Ti4O15>SrLa4Ti4O15>CaLa4Ti4O15. CO, HCOOH | 195 |
| 11. | Ni@NiO on InTaO4 | Pyrex glass (continuous flow) | CO2(3 kg cm-2) in H2O | 298 | 100 mW Xe lamp | Methanol - InTaO4 < InTaO4-N<Ni@NiO/InTaO4-N. | 196 |
| 12. | NiO–InNbO4, Co3O4–InNbO4 | Pyrex glass (continuous flow) | CO2 in 0.2 M KHCO3 | 308 | 500W halogen H-500; 143µ W/cm2; λ500–900nm | CH3OH NiO-InNbO4 - 1.577 Co3O4-InNbO4 - 1.503. | 197 |
| 13. | HNb3O8 nanobelts | Quartz tubular reactor | H2O+CO2 | 318 | 350 W Xe | CH4 – 3.58 | 198 |
| 14. | Zn-Al LDH, Zn-Cu-Ga | Quartz reactor | 2.3 kPa of CO2 + 21.7 kPa of H2 | 305–313 | 500-W Xe arc lamp | CO – 0.62, CH3OH – 0.17. | 199 |
| 15. | FeTiO3/ TiO2 | Pyrex glass | CO2 in NaHCO3 | RT | 500W Xe (with cut off) | CH3OH - 0.46 | 200 |
| 16. | CuGaO2, CuGa1-x FexO2 | SS cell | CO2 in H2O | RT | 300WXe arc | CO - 9*, *ppm g-1 h-1 | 201 |
| 17. | SiO2- Pillared HNb3O8 | Quartz tubular reactor | H2O/CO2 = 0.14 | 333 | 34.8mW cm-2 Xe arc | CH4 - 2.9 | 202 |
| 18. | Pt/SrTiO3–Rh/ Pt/CuAlGaO4 WO3 | H- Twin reactor | 2 mM FeCl2/FeCl3 | RT | AM 1.5G | CH3OH - 0.52 H2 - 0.12 | 203 |
| 19. | Pt/SrTiO3–Rh/ Pt/CuAlGaO4 WO3 | H- Twin reactor | 2 mM FeCl2/FeCl3 | - | AM 1.5G | CH3OH - 8 H2 - 1 | 204 |
| 20. | Pt/self-doped SrTiO3 | - | CO2+H2O water | - | 300 W Xe lamp, visible light 400 nm | CH4 - 0.26/cm2 | 205 |
| 21. | Ag/ SrTiO3 | Batch slurry reactor | CO2 in CH3OH | 298 | Hg lamp | HCOOH | 206 |
| 22. | Au/ leaf-architectured SrTiO3 | Pyrex reaction cell | CO2+H2O vapor | RT | 300 W Xe lamp | CO, CH4 | 207 |
| 23. | Pt/Fe2V4O13 nanoribbons |  | CO2+H2O vapor |  | visible light 420 nm | CH4 | 208 |
| 24. | Pt and RuO2/ Na2 V6O16 nanoribbons | Circular glass reactor | CO2+H2O vapor |  | 300 W Xe lamp, visible light 420 nm | CH4 - 2 | 209 |
| 25. | Bi6Mo2O15 sub-microwires | - | CO2+H2O vapor | RT | UV Xe lamp | CH4 - 17* O2- 250 | 210 |
| 26. | Bi2WO6 hollow microspheres | - | (CO2+H2O) vapor | RT | visible light 420 nm | CH3OH - 33 *ppm, | 211 |
| 27. | Pt/mesoporous In(OH)3 | Gas closed circulation pump | (CO2+H2O) vapor | RT | UV Xe lamp | CH4 - 25 | 212 |
| 28. | RuO2/meso ZnGa2O4 | Glass | (CO2+H2O) vapor | RT | UV Xe lamp | CH4 - 145 ppm | 213 |
| 29. | RuO2/ZnGa2O4 nanocubes | Glass reactor | (CO2+H2O) vapor | - | UV Xe lamp | CH4 - 2, O2 - 21 | 214 |
| 30. | Pt/ ZnAl2O4 -modifi ed meso ZnGaNO | - | (CO2+H2O) vapor | - | visible light 420 nm | CH4 - 40 | 215 |
| 31. | Pt/ZIF-8/Zn2GeO4 nanorods | - | CO2 bubbled Na2SO3 | RT | UV Xe lamp | CH3OH - 3 | 216 |
| 32. | Pt &RuO2/ sheaf-like, hyperbranched Zn1.7GeN1.8O | Pyrex glass | (CO2+H2O) vapor | RT | visible light 420 nm | CH4 - 55 | 217 |
| 33. | 4.5(ZnGa2O4): (Zn2GeO4 ) | Glass reactor | (CO2+H2O) vapor | RT | UV Xe lamp | CH4 - 2.75, O2 - 17 | 218 |
| 34. | Pt/In2Ge2O7 (En) nanowires | Pyrex glass cell | (CO2+H2O) vapor | RT | 300 W Xe lamp | CO - 4, O2 | 219 |
| 35. | Pt/Zn2SnO4 | Pyrex glass cell | (CO2+H2O) vapor | RT | UV Xe lamp | CH4 - 350 | 220 |
| 36. | layered Mg-In LDH | Closed circulation system | (CO2+H2O) vapor | RT | UV Hg-Xe lamp | CO - 3, O2 | 221 |
| 37. | layered Zn– Cu–Ga LDH | Quartz reactor | (CO2+H2) vapor | RT | 500 W UV Xe lamp | CH3OH, CO | 222 |
| 38. | Ag/KTaO3 | Glass reactor | CO2+H2O | RT | 300 W Xe lamp | CO - 152.6, H2 - 1134, O2 - 499.9 | 223 |
| 39. | (MgAl)-LDO grafted TiO2 | Quartz tube reactor | (CO2+H2) vapor | 423 | 100 W He/ 450W Xe lamp | CO - 4/h | 224 |
| 40. | ZnGaNO nanorod | Glass reactor | CO2+H2O | RT | 300 W Xe lamp | CH4 - 0.19 | 225 |
| 41. | NiCo2O4 with [Ru(bpy)3]Cl2. 6H2O | Schlenk reactor | TEOA/ water/acetonitrile | 303 | 300 W Xe lamp | CO - 35, H2 - 5 | 226 |
| 42. | SnNb2O6 | Schlenk reactor | CO2+H2O | RT | 300 W Xe lamp | CH4 - 110 µL/h | 227 |
| 43. | MTaO3 (M = Li, Na, K) | Pyrex glass cell | CO2+H2O | RT | 200 W Hg–Xe arc lamp | CH4 - 1.9 nmol/h CO - 4 | 228 |
| 44. | Ag/BaZrO3 | Cylindrical quartz reactor | (CO2+H2O) vapor | RT | 300 W Xe lamp | CH4 - 4 | 229 |
| 45. | MnCo2O4 | - | CO2 in TEOA | 303 | 300W Xe lamp | CO - 27, H2 -8 | 230 |
| 46. | CuxOy-ZrOCoII SBA-15 | Stainless infrared vacuum cell | CO2 in diethylamine | RT | laser | CO | 231 |
| 47. | Cr doped SrTiO3 | - | (CO2+H2O) vapor | RT | 300W Xe lamp | CH4 - 8.8 | 232 |
| 48. | CaxTiyO3 | Quartz reactor | CO2+H2O | 303 | 6 W cm−2 , UV lamp | CH4 - 17 | 233 |
| 49. | C, N/sodium titanate | Stainless steel | (CO2+H2O) vapor | RT | 100 W Xe solar simulator | CH4 - 9.75/h | 234 |

Table .1. 14 Studies on dye sensitized photo catalysts

| S. | Catalyst | Type of | Conditions |  | Light Source | Product | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| No |  | Reactor used |  |  | /Intensity | formation |  |
|  |  |  | Reactant | Temp |  | µmol/g cat |  |
|  |  |  |  | (K) |  |  |  |
| 1. | Metal porphyrin / phthalo cyanine on Nafion | Glass cell with an optical window. | CO2 in TEA | 308 | 500 W tungsten- halogen | HCOOH. | 235 |
| 2. | Dye([Ru(B py)3]2+ perylene Di- Imide based) sensitized, Q- yield:Pt onTiO2 | Glass chamber connected to a vacuum line | 0.09 MPa CO2 inH2O | 298 | 75 W visible daylight lamp, 150 W UV | CH4 - 0.6. | 236 |
| 3. | Ruthenium dye (N3)- sensitized Cu–Fe/TiO2 | Continuous circulating Pyrex glass | CO2 + H2O (vapor) | 348 | Solar 20 mW cm-2, UV lamp 225 mW cm-2 | CH4 - 0.617 | 237 |
| 4. | CoPc/TiO2 | Pyrex glass cell (batch mode). | CO2 in 0.1N NaOH. | 308 | 500W tungsten- halogen | HCOOH - 300, CH3OH – 10, HCHO – 50. | 238 |
| 5. | 0.7 wt.% In-situ CoPc/TiO2 | Pyrex glass cell | CO2 in 0.1N NaOH. | 308 | 500W tungsten- halogen | HCOOH-1487.6 CH3OH – 93 HCHO - 134.3. | 239 |
| 6. | Ru/RuOx sensitized TiO2 | - | CO2+ H2O | - | Solar simulator | CH4 - 900 µL h-1 | 240 |
| 7. | Dye sensitized (perylene diimide derivatives) Pt impregnated on TiO2 | - | CO2 + H2O | RT | 75 W daylight lamp | CH4 - 0.74 | 241 |
| 8. | N719/TiO2 | H type reactor | CO2 + H2O/ 2 M NaOH | RT | 300 W Xe lamp | CH3OH - 178.1/cm2 HCHO - 129.2/cm2 | 242 |
| 9. | IrOx/SiGe-jn/CC/p-RuCP | Stainless steel Monolithic tablet shaped device | CO2 + H2O | RT | Simulated solar light | HCOOH - 50.2, H2 - 3.6, O2 - 26.4 | 243 |
| 10. | Zinc porphyrin/TiO2 | Pyrex glass reactor | (CO2 + H2O) vapor | RT | 300 W Xe-lamp | CO - 8.07/h CH4 - 1.01/h | 244 |

1.8 Kinetics and mechanism of CO2 photo reduction with water

CO2 reduction pathway on semiconductor surfaces is at an infant stage. However, based on

Fig. 1.9 Proposed mechanisms for the reduction of CO2 to methane: (a) formaldehyde pathway (b) carbene pathway (c) glyoxal pathway [245]

detailed experiments, researchers have put forward plausible pathways for CO2 reduction on TiO2 surfaces.

Three different reaction pathways depending on the binding mode of CO2.- radical anion on the semiconductor surface have been proposed [245], ie, i) The formaldehyde pathway, ii) The carbene pathway, iii) The glyoxal pathway shown in Fig. 1.9

In the case of Formaldehyde pathway, binding mode of CO2 through one of the oxygen atom on titanium atom/ion ? or carbon atom through surface oxygen atom of TiO2, favors the formation of .COOH radical, which further combines with .H to form formic acid. As shown in Fig. 1.9 a, final 8 e- reduction product CH4 was obtained from consecutive reduction of formic acid through HCHO and CH3OH as intermediate products. These observations find support in a recent publication by Dimitrijevic et al [246], wherein detailed low temperature ESR measurements on TiO2 nano particles dispersed in aqueous alkaline solutions, have indicated the formation of H atoms and OH radicals in addition to methyl (.CH3) and methoxy (.CH3O) radicals on the surface. However the formation of surface formate species is proposed as the initial step according to the Scheme. 4 below:

CO2 + 2e- + H+                 HCOO-                      -------------  (20)

Scheme 4 Proposed mechanism of photo catalytic transformation of CO2 to methoxy radical over TiO2 in the presence of dissociated/ bound water [246]

Ulagappan and Frei [145] carried out a mechanistic study of the reaction with methanol as electron donor on Ti silicalite using in-situ FT-IR spectroscopy and traced the reaction pathway using isotopic labelling studies with C18O2, 13CO2 and 13CH3OH. HCOOH was identified as the primary product, which on pyrolysis gives CO. In the absence of methanol, water was confirmed as the electron donor.

Koci et al. studied kinetic model for CO2 photo reduction with respect to the formaldehyde pathway [247] the result shows that the formation of methane did not correspond to the consecutive reduction of formic acid and methanol. Hence they have proposed carbene pathway for CO2 photo reduction shown in Fig. 1.9 b, in this pathway, anion radical bind through carbon on the semiconductor surface, formation of CO and O occur in the first step. Then adsorbed CO reduced with two electrons to form carbon residue on the semiconductor surface, which further combines with .H to form carbene and methyl radicals and finally CH4. Formation of different transient surface species and their transformations on TiO2 during photo catalytic reduction of CO2 by water was traced by Anpo et al [43, 248] using ESR, EXAFS and other spectroscopic techniques. Ti3+, H, C and CH3 radicals were detected by ESR studies carried out at 77K. The charge transfer excited state, (Ti3+-O-)3* with Ti in tetrahedral co-ordination, formed by absorption of light energy, was proposed as the active site on which CO2 gets reduced to CO and C, which on addition of active surface hydrogen forms hydrocarbons. Further mechanistic pathways in this case, have been elucidated in Scheme. 5.

Scheme. 5. Schematic representation of the photo catalytic reduction of CO2 with H2O on anchored titanium dioxide [43, 248]

A recent publication by Yang et al [249] on the photo catalytic reduction of CO2 using Ti-SBA-15 deals with the investigations on the effects of varying feed composition on the product patterns, with a view to understand the reaction mechanism. In particular, addition of CO, H2 in the place of H2O, methanol and formaldehyde was studied in detail. While CH4, C2H4 and C2H6 could be observed with CO + H2O with reasonable rates, with CO+H2 mixture, the reaction rates were very low. It was concluded that H2O was a more efficient reductant with CO2 or CO than H2. CH3OH was not a significant product and when added with the feed and it did not increase the reaction rate. Similarly added formic acid also did not enhance product formation. These observations rule out methanol or formic acid as intermediates in the formation of hydrocarbons on Ti-SBA-15. However, added formaldehyde underwent facile conversion to hydrocarbon products. Based on the detailed analysis of the products it was proposed that CO2 photo reduction proceeds through the formation of CO in the initial stages followed by its conversion to formaldehyde, which in turn gets converted to other hydrocarbon products. Ti-OH site, which on photo activation gets converted to [Ti (III)-O]* is considered as the active site [145].

Yang mechanism ?

Kinetic models for photo catalytic reduction of CO2 with water on titania have been reported by Lo et al. [168] and Tan et al. [250]. Both authors have applied single site Langmuir- Hinshelwood [L-H] type kinetic model to simulate the process. Lo et al.[168] could successfully validate their model with the experimental data with a pseudo first order reaction rate equation. Tan et.al [250] adopted the reaction scheme involving the formation of surface carbon radicals as proposed by Anpo et al. [43, 248] and could predict rates of formation of methane and hydrogen. Koci et al. [247] while applying the L-H model have checked the suitability of the two reaction mechanisms proposed, ie., one by Anpo [43, 248] and the other by Wu [67] and observed that their model supports Anpo’s mechanism wherein CO is proposed as the primary intermediate. Hence carbene reaction pathway is a more plausible reaction pathway for CO2 reduction.

Shkrob et al [245, 251, 252] have proposed Glyoxal reaction pathway for CO2 photo reduction  by adopting EPR study, which includes both oxidation and reduction reactions. In the previous reaction pathway authors were interested in reduction reactions (electrons), but highly oxidative holes are also present in the system. The formation of oxidized products from formaldehyde and methanol is more favorable compared to reduce product form it. Hence Shkrob et al proposed C2 complex reaction pathway shown in Fig. 1.9c, in which dimerization of formyl radical to gives glyoxal, further reduced to form acetaldehyde through vinoxyl radical. CH3CHO easily oxidized to form unstable acetyl radical which further undergoes decarbonylation to form methyl radical, and then combine with .H to form CH4.

While the formation of C1 hydrocarbons could be explained to a reasonable level of acceptability, the understanding on the pathways leading to the formation of C2 and >C2 hydrocarbons was not clear. Dimerization of surface C1 species was proposed as the possible route for the formation of C2 hydrocarbon products [253], though direct experimental evidence to this effect was lacking.

Yang et al. [249] observe that the backward reaction ie, oxidation of hydrocarbons back to CO2 and water, proceeds to a significant extent. This implies that the oxygen produced by the splitting of water, which is responsible for the backward reaction, has to be removed effectively to increase hydrocarbon yields. Means of separating physically the oxidation and reduction sites would be crucial in this respect. It is clear that the reaction mechanism is quite complex and depends on the type of the catalysts/active sites.

1.9 Deactivation of photo catalysts

In some cases [146, 89, 133, 135, 151] the catalysts reported for photo reduction of CO2 tend to get deactivated within short period, while in few cases activity beyond 20 hrs. has been reported. Transformation of photo activated CO2 to hydrocarbons proceeds through several hydrocarbon intermediates, whose identity or nature is yet to be established. Accumulation of these intermediates on the catalyst surface and blocking of the active sites is one of the major reasons for the catalyst deactivation. In the case of catalyst nano particles dispersed in liquid media, coagulation and reduction in light absorption power [146] and changes in the oxidation state of metal ions [133] may lead to catalyst deactivation. Regeneration with air helps in restoring the activity. However the phenomenon of catalyst deactivation in this process needs further study, especially when large scale applications of this process are desired.

An in-depth understanding of the reaction mechanism and the fast deactivation of the photo catalyst would be helpful in the development of superior catalysts for this process that has the potential to emerge as a sustainable route for the production of fuels and chemicals.

1.10. Future trends and research directions

Photo catalytic reduction of carbon dioxide with water to fuels/chemicals (methane, methanol, etc.,) is an emerging area of research towards utilizing the abundant sunlight. Though the process has the potential to become a viable and sustainable alternative energy source to fossil fuels, it has thrown up several tough challenges to the scientists and technologists, which are yet to be tackled, namely,

- Facilitating the activation of two thermodynamically most stable molecules, CO2 and H2O

- Conversions achieved so far are extremely small, < 1 %, occurring at very slow rate

- Catalysts tend to get deactivated over short period which needs further studies

- CO2 photo reduction process is highly complex, involving multi electron transfer and non- selective, leading to a range (C1-C3) of hydrocarbon products- reaction pathways have not been established yet

- Design of catalysts consisting of photo active phase/support and co-catalysts aided by metal ion and /or anion doping and light harvesting components/sensitizers, as a functionally integrated composite, is equally complex.

- Ideal catalysts are expected to display maximum efficiency towards solar energy absorption and possess requisite band energy level characteristics to drive the redox  reactions.

- The process involves two steps, spitting of water and reduction of carbon dioxide, which is thermodynamically more favourable. Since the second step involves multi-electron       transfer, the rates are very slow relative to the first. These two steps are to be       synchronized to achieve higher yields of hydrocarbons.

- Multiple and complex surface reaction pathways that involve several carbon containing ion radicals, render the selective formation of methane or methanol a difficult task.

- Further decomposition of the products and promotion of backward reactions also contribute towards lower yields.

- Catalyst deactivation proceeds through the formation of carbonaceous species on the surface. This implies that the metal function responsible for the hydrogenation of carbonaceous species needs to be improved though availability of hydrogen via water splitting may not be the issue.

- Titania, subjected to a wide range of modifications, in the form of titania based composites and in different morphological forms has been explored to enhance the activity for photo-catalytic reduction of CO2 with water with respect to pristine titania. Primary objectives behind the modifications, namely, promoting visible light activity, retarding the recombination of charge carriers by effective physical separation (by doping with metals, anions & cations), facilitating their transport through titania surface, isolation of titania sites by dispersion on high surface area supports and incorporation of suitable active elements to bring out required redox reactions, have been realized to a significant extent. However, the expected improvement in activity has been moderate, an increase by 2-4 times, which is too low for any possible practical applications.

- In-depth investigations on the surface reaction pathways by in-situ spectroscopic methods, supported by sound theoretical studies on the activation and surface transformations of CO2 and other aspects for investigation, as detailed in the earlier section, would be helpful in controlling deactivation and achieving higher conversions.

Nevertheless, research efforts on these fronts are being pursued with the objectives of designing of efficient catalyst systems to achieve higher yields of desired products and improving catalyst life. Efforts in future have to be towards the development of alternative catalysts, based on various semiconducting metal oxides/sulfides/nitrides/phosphides, layered titanates, binary and ternary oxides of Nb, Ta, Ga & In in conjunction with alkaline, alkaline earth and rare earth oxides and with a host of co-catalysts and sensitizers.[9, 10, 74-244, 254, 255]

Especially, the following areas/aspects are worth exploring further:

- A number of binary and ternary oxides of Bi, V, Nb & Ta with Gr IIIA elements like, Al,Ga& In are known to be efficient catalysts for photo catalytic splitting of water in the visible region [256, 257]. These systems with suitable co-catalysts like NiO could be excellent catalysts for CO2 photo reduction

- Most of these oxides are synthesized by high temperature solid state reaction with very low surface area. Soft chemistry routes could be explored to get high surface area samples. However, in such cases, the contribution due to residual carbon on the catalysts is to be accounted for.

- These compounds possess well-defined crystal structure and hence their solid state and photo- physical properties could be fine-tuned to derive maximum performance

- Performance of such photo catalysts could be improved further by forming composites with advanced materials like CNT, graphene [258-261] and Nafion [262] which facilitate free and fast transfer of charge carriers could be another way to improve performance.

- Studies on modes of adsorption and activation of CO2 on metals, metal oxides, which act as co-catalysts- experimental as well as theoretical approaches are to be pursued.

- Use of different co-catalysts, single as well as bi-component systems

- Elucidation of the mechanistic pathways for the transformation of transient surface species and formation of C2 and higher carbon number products

- Modes of deactivation of catalysts and possibilities for regeneration

It is expected that the use of photo electrochemical cells (PEC) for conversion of CO2 to methanol [263-266] would add another dimension to the process, to get improved yields of hydrocarbons. Additionally, development of novel and more efficient catalyst systems and prevention of re-oxidation of products could help in improving the efficiency of the process.

1.11 Scope of the present investigation

CO2 is one of the cheapest and most abundant carbon containing raw material in the earth. But the usage of CO2 as raw material is thermodynamically unfavorable due its stability and chemically inert nature. Hence thermodynamically uphill reactions can be solved by developing a good catalyst system. The production of fossil fuels from green house gas CO2 and abundantly available water in the presence of natural sunlight is an attractive research, because it will give remedy to both energy and environmental issues which we are facing day today life. There is some relief from green house effect by using CO2 as reactant and also getting fossil fuel (energy) from natural source such as solar light and water. The challenge is to activate thermodynamically most stable molecules CO2 and H2O. Photo catalytic reduction with water has the potential to emerge as a viable process. Since, photo catalysst can convert solar energy into chemical energy and also have the ability to promote non-spontaneous reactions (ΔG>0). Hence design of photo catalysts is an important and challenging task.

The primary objective of the present investigation is to design novel photo catalysts for CO2 reduction. Detailed literature survey on different types of catalysts investigated so far reveal that two perovskite type catalysts, NaTaO3 and Sr3Ti2O7, which display significant activity for splitting of water and possess conduction and valance band energy levels suitable for CO2 photo reduction have not been exploited so far. Both oxides, being wide band gap semi-conductors, are to be suitably modified to enable visible light absorption. Attempts have been made to modify these oxides and explore their activity for CO2 photo reduction. Besides, meso-porous character of the photo catalysts is known to improve the activity (Ref). In order to explore this aspect, a comparative study of standard titania P-25 and a lab-made mesoporous titania in pristine and doped (N,S & Fe)  forms have been investigated. Accordingly, investigations covering several other aspects, as detailed below, around these three main catalyst systems (TiO2, La-NaTaO3 and Sr3Ti2O7) have been planned:

- Studies on titania based catalysts:

- Comparison of mesoporous titanium dioxide with standard P-25 titania

- Influence of doping/co-doping with N,S & Fe

- Effect of supporting N, S &Fe co-doped TiO2 samples on sepiolite

- Studies on  La modified NaTaO3 based photo catalysts:

- Influence of different co-catalysts: Ag, Au, Pt, Pd, NiO, CuO and RuO2  and bi-metallic co-catalysts, Pt-CuO & Pt-NiO

- Effect of metal–non metal (Fe,N) co- doping

- Sensitization with Cobalt tetra phenyl porphyrin (CoTPP)

- Effect of addition of basic component, MgO

- Studies on layered perovskite type titanates based on Sr3Ti2O7 as photo catalysts:

- Comparison of strontium titanates- SrTiO3, Sr3Ti2O7 and Sr4Ti3O10

- Effect of doping/co-doping Sr3Ti2O7 with N,S & Fe

Hydrothermal and polymer complex methods have been adopted for the preparation of the tantalates and titanates. All catalysts have been subjected to comprehensive characterization studies, using XRD, DRS-UV, photo luminescence, SEM, TEM, XPS, Raman spectroscopic techniques and surface area analysis. Photo catalytic efficiency of the prepared catalysts for CO2 reduction with water has been studied in a lab-made photo reactor, with UV-visible radiation. Observed activity patterns have been rationalized in terms of structural, morphological, electronic and photo-physical properties of the catalysts, so as to arrive at a basis for the design of effective photo catalysts for this application.

1.12. Organization of the thesis

Chapter 1. Introduction

Chapter 2. Experimental methods

Chapter 3. Studies on titania based catalysts

Chapter 4. Studies on La modified sodium tantalite based catalysts

Chapter 5. Studies on strontium titanate based catalysts

Chapter 6. Summary and Conclusions

References

- International Energy Agency “CO2 emissions from fuel combustion highlights 2014”

- M. A. Wojtowicz, J. R. Pels, J. A. Moulijn, Fuel Process. Technol. 1993, 34, 1.

- R. W. Steiner, Chem. Eng. 1993, 100, 114.

- W. Wang, S. Wang, X. Ma, J. Gong, Chem. Soc. Rev., 2011, 40, 3703.

- M.A. Scibioh, B. Viswanathan, Proc. Indian National Science Academy, 2004, 70A, 407.

- S. S. Kim, G. Kishan, M. J. Choi, K. W. Lee, Appl. Catal. A. Gen., 1999, 179, 155.

- N. Serpone, E. Pelizzetti, Wiley-Interscience, New York, 1989; N. Serpone and A. V. Emeline, Int. J. Photoenergy, 2002, 4, 91.

- D. Ravelli, D. Dondi, M. Fagnoni and A. Albini, Chem. Soc. Rev., 2009, 38, 1999.

- V. P. Indrakanti, J. D. Kubickib, H. H. Schobert, Energy Environ. Sci., 2009, 2, 745.

- S. Das, W.M.A. Wan Daud, RSC Adv., 2014, 4, 20856

- V. Jeyalakshmi, K. Rajalakshmi, R. Mahalakshmy, K.R. Krishnamurthy, B.Viswanathan, Res. Chem. Intermed. 2013, 39, 2565.

- T. Inoue, A. Fujishima, K. Honda, Nature, 1979, 277, 637.

- Z. Jiang, T. Xiao, V. L. Kuznetsov, P. P. Edwards, Phil. Trans. R. Soc. A, 2010, 368, 3343.

- M. Halmann, Nature, 1978, 275, 115.

- Y. Izumi, Coord. Chem. Rev. 2013, 257, 171.

- M. Halmann, M. Ulman, B. A. Blajeni, Sol. Energy, 1983, 31, 429.

- B. A. Blajeni, M. Halmann, J. Manassen, Solar Energy, 1980, 25, 165.

- K. Koci, L. Obalova, Z. Lancy, Chem. Papers, 2008, 62, 1.

- P. Usubharatana, D. McMartin, A. Veawab, P. Tontiwachwuthikul, Ind. Eng. Chem. Res, 2006, 45, 2558.

- V. Jeyalakshmi, R. Mahalakshmy, K.R. Krishnamurthy, B. Viswanathan, Indian J. Chem., Sect. A: Inorg., Bio-inorg., phys., Theor. Anal. Chem., 2012, 51, 1263

- M. Pengfei Ji, Takeuchi and T M Cuong, J. Zhang, M. Matsuoka, M. Anpo, Res. Chem. Intermed, 2010, 36, 327.

- Y. Yang, H. Zhong, C. Tian, Res Chem. Intermed, 2011, 37, 91.

- C. M. Teh, A. R. Mohamed, J Alloys Compd, 2011, 509, 1648.

- A. Zaleska, Recent Pat Engg, 2008, 2, 157.

- A. Fujishima, X. Zhang, D.A. Tryk, Surf Sci Rep, 2008, 63, 515.

- M. Anpo and M. Takeuchi, J. Catal, 2003, 216, 505.

- M. R. Hoffmann, S.T. Martin, W. Chi and W. Detlef, Chem Rev, 1995, 95, 69.

# M. A. Malati, W. K. Wong, Surf. Tech, 1984, 22, 305.

- B. Viswanathan, K. R. Krishnamurthy International Journal of Hydrogen Energy,  2012, Article ID 269654 (10pages)

- K. Kocˇ, L. Obalova, L. Mateˇjova´, D. Placha´, Z. Lacny´, J. Jirkovsky´, O. Sˇolcova´, Appl. Catal. B: Environ. 2009, 89, 494.

- G. Li, S. Ciston, Z. V. Saponjic, L. Chen, N. M. Dimitrijevic, T. Rajh, K. A. Gray, J. Catal., 2008, 253, 105.

- M. Gopal, W. J. Moberly Chan, L. C. De Jonghe, J Mater Sci, 1997, 32, 6001.

- S. Ito, S. Inoue, H. Kawada, M. Hara, M. Iwasaki, H. Tada, J Colloid Interf.  Sci, 1999, 216, 59.

- K. Terabe, K. Kato, H. Miyazaki, S. Yamaguchi, A. Imai, Y. Iguchi, Mater Sci, 1994, 29, 1617.

- O. Ishitani, C. Inoue, Y. Suzuki, T. Ibusuki, J. Photochem. Photobiol A, 1993, 72, 269.

- F. Saladin, L. Fross, I. Kamber, J. Chem. Soc. Chem. Commun., 1995, 533.

- F. Saladin, I. Alxneit, J. Chem. Soc. Faraday Trans, 1997, 93, 4159.

- S. Kaneco , Y. Shimizu, K. Ohta, T. Mizuno, J. Photochem. Photobiol. A: Chem. 1998, 115, 223.

- K. Ikeue, H. Yamashita, M. Anpo, T. Takewaki, J Phys Chem B, 2001, 105, 8350.

- I.H. Tseng, W.C. Chang, J. C. S. Wu, Appl. Catal. B: Environ, 2002, 37, 37.

- Y. Ku, W-H Lee, W-Y Wang, J. Mol Catal. A: Chemical, 2004, 212, 191.

- P. Pathak, M. J. Meziani, L. Castillo, Y. P. Sun, Green Chem. 2005, 7, 667.

- J. Hwang, J. Chang, S. Park, K. Ikeuen, M. Anpo, Topics in Catal, 2005, 35, 311.

- S. S. Tan, L. Zou, E. Hu, Sci. Technol. Adv. Mater. 2007, 8, 89.

- X-H. Xia, Z-J. Jia, Y. Yu, Y. Liang, Z. Wang, L-L. Ma, Carbon, 2007, 45, 717.

- K. Kocí, MartinReli, O. Kozák, Z. Lacny, DanielaPlachá, PetrPraus, LucieObalov, Catal. Today (2010) doi:10.1016/j.cattod.2010.12.054

- R. W. Matthews, S. R. McEvoy, J. Photochem. Photobiol.A: Chem, 1992, 66, 355.

- K. Koˇcí, K. Zatloukalova, L. Obalova, S. Krejcikova, Z. Lacny, L. Capek, A. Hospodkova, O. Solcova, Chinese J. Catal., 2011, 32, 812.

- J. Fan, E.Z. Liu, L. Tian, X.Y. Hu, Qi He, T. Sun, Am. Soc. Civil Eng., 2010, Doi:10.1061/(ASCE)EE.1943-7870.0000311.

- Y. Liu, B. Huang, Y. Dai , X. Zhang, X. Qin ,M. Jiang, M. Whangbo, Catal. Commun, 2009, 11, 210.

- T. Mizuno, K. Adachi, K. Ohta, A. Saji, J. Photochem. Photobiol. A:                    Chem. 1996, 98, 87.

- H. Hori, K. Koike, Y. Suzuki, M. Ishizuka, J. Tanaka, K. Takeuchi, Y. Sasaki, J. Mol.Catal. A: Chem. 2002, 179, 1.

- S. Kaneco, H. Kurimoto, K. Ohta, T. Mizuno, Akira, J. Photochem. Photobiol. A: Chem., 1997, 109, 59.

- S. Kaneco, H. Kurimoto, Y. Shimizu, K. Ohta, T. Mizuno, Energy, 1999, 24, 21.

- S. S. Tan, L. Zou, E. Hu, Catal. Today, 2006, 115, 269.

- O. Ola, M. M. Maroto-Valer, J. Photochem. Photobiol. C: Photochem. Reviews, 2015, 24, 16.

- T.V. Nguyen, J.C.S. Yu, Appl. Catal. A, 2008, 335, 112.

- P. Du, J.T. Carneiro, J. A. Moulijn, G. Mul,  Appl. Catal. A. 2008, 334, 119.

- C. Perego, S. Peratello, Catal. Today, 1999, 52, 133.

- P.S. Mukherjee, Ray, Chem. Eng. Technol., 1999, 22, 253.

- T. Van Gerven, G. Mul, J. Moulijn, A. Stankiewicz, Chem. Eng. Process., 2007, 46, 781.

- H. Lin, AIChE J., 2006, 52, 2271–2280.

- R.D. Sun, A. Nakajima, I. Watanabe, T. Watanabe, K. Hashimoto, J. Photochem. Photobiol. A, 2000, 136, 111.

- J. C. S. Wu, T.H. Wu, T. Chu, H. Huang, D. Tsai, Topic in Catal., 2008, 47, 131.

- J.C.S Wu, H. M. Lin, C-H. Lai, Appl. Catal. A: Gen, 2005, 296, 194.

- J. C. S. Wu, H.M. Lin, International J. Photoenergy, 2005, 7, 115.

- J.C.S. Wu, Catal. Surv. Asia, 2009, 13, 30.

- K. Sayama, H. Arakawa, J. Chem. Soc. Faraday Trans. 1997, 93, 1647.

- M. Reli, M. Sihor, K. kočí, P. prau, O. kozák, L. obalová, Geo Science Engineering, 2012, LVIII, 34. ISSN 1802-5420.

- J. D. Graham. N. I. Hammer, Handbook of climate change mitigation pp. 1755-1780. DOI 10.1007/978-1-4419-7991-9_46,

- B. J. Liu, T. Torimoto, H. Yoneyama, J. Photochem. Photobiol. A: Chem., 1998, 113, 93.

- B.J. Liu, T. Torimoto, H. Matsumoto, H. Yoneyama, J. Photochem. Photobiol. A: Chem., 1997, 108, 187.

- G.R. Dey, J. Natural Gas Chem, 2007, 16, 217.

- G.R. Dey, A. D. Belapurkar, K. Kishore, J. Photochem. Photobiol. A: Chem, 2004, 163, 503.

- S. S. Tan, L. Zou, E. Hu, Sci. Technol. Adv. Mater. 2007, 8, 89.

- K. Rajalakshmi, V. Jeyalakshmi, R. Mahalakshmy, K.R. Krishnamurthy, B. Viswanathan, Indian J. Chem., Sect. A: Inorg., Bio-inorg., phys., Theor. Anal. Chem., 2012, 51A, 411.

- J. Pan, X. Wu, L. Wang, G. Liu, G. Qing (Max) Lu, H-M Cheng, Chem. Comm. 2011, 47, 8361.

- W-N Wang, W-J An, B. Ramalingam, S. Mukherjee, D. M. Niedzwiedzki, S. Gangopadhyay, P. Biswas, J. Am. Chem. Soc. 2012, 134, 11276.

- H. Xu, S. Ouyang, P. Li, T. Kako, J. Ye, ACS Appl. Mater. Interfaces, 2013, 5, 1348.

- T. Wang, X. Meng, P. Li, S. Ouyang, K. Chang, G. Liu, Z. Mei, J. Ye, Nano Energy, 2014, 9, 50.

- M. Halmann, E. Katzir Borgarello, J. Kiwi, Sol. Energy Mater., 1984, 10, 85.

- Z. Goren, I. Willner, A. J. Nelson, J Phys Chem, 1990, 94, 3784.

- K. Adachi, K. Ohta, T. Mizuno, Solar Energy, 1994, 53, 187.

- H. Yamashita, H. Nishigushi,N. Kamada, M. Anpo, Res Chem Interm. 1994, 20, 815-823.

- I-H. Tseng, J C S. Wu, H-Y. Chou, J. Catalysis, 2004, 221, 432.

- Slamet, H W. Nasution, E. Purnama, S. Koesla, Gunlauardi, J Catalysis Commun., 2005, 6, 313.

- T-V. Nguyen, J.C. S. Wu, Appl. Catalysis A:General 2008, 335, 112.

- O.K. Varghese, M. Paulose, T. J. Latempa, C.A.Grimes, Nano Letters, 2009, 9, 731.

- Q-H. Zhang, W-D. Han, Y-J. Hong, J-G. Yu, Catalysis Today, 2009, 148, 335.

- K. Koci, K. Mateju, L. Obalova, S. Krejcikova, Z. Lacny, D. Placha, L.Capek, A.

Hospodkova, O. Solcova, Appl. Catal. B: Environ., 2010, 96, 239.

- J. C. S. Wu, C. W. Huang, Front. Chem. Eng. China 2010, 4, 120.

- M. A. Asi, C. He, M. Su, D. Xia, L. Lin, H. Deng, Y. Xiong, R. Qui, X. Li, Catal. Today, 2011, 175, 256.

- D. Luo, Y. Bi, W. Kan, N. Zhang, and S. Hong, J. Mol. Structure,doi: .1016/j. molstruc. 2011.03.044.

- S. Qin, F. Xin, Y. Liu, X. Yin, W.Maa, J. Colloid & Surf.Sci., 2011, 356, 257.

- J-J Chen, J. C. S. Wu, P. C. Wu, D. P. Tsai, J Phys Chem C, 2011, 115, 210.

- X. Li, Z. Zongjin, W. Li, H. Pan, Appl. Catal. A: Gen. 2012, 429– 430, 31.

- A. Cybula, M. Klein, A. Zielinska-Jurek, M. janczarek, A. Zaleska, Physicochem. Probl. Miner. Process. 2012, 48, 159.

- Q. Zhang, T. Gao, J. M. Andino, Y. Li, Appl. catal. B: Environ., 2012, 123-124, 257.

- W. Jing, T. Xin, Y. Tao, Z. Lin, Appl. Mech. Mater. 2011, 55, 1506.

- L. Collado, P. Jana, B. Sierra, J.M. Coronado, P. Pizarro, D.P. Serrano, V.A. de la   Pena O’Shea, Chem. Eng. J. 2013, 224, 128.

- B. S. Kwak, K. Vignesh, N-K Park, H-J Ryu, J-I Baek, M Kang, Fuel 2015, 143, 570.

- Y. Liu, S. Zhou, J. Li, Y. Wang, G. Jiang, Z. Zhao, B. Liu, X Gong, A. Duan, J Liu, Y Wei, L. Zhang, Appl. Catal. B 2015, 168–169, 125.

- C. Tang, W. Hou, E. Liu, X. Hu, J. Fan, J. Lumin. 2014, 154, 305.

- O. Ola, M. M. Maroto-Valer, J. Catal. 2014, 309, 300.

- S. Rani, N. Bao, S.C. Roy, Appl.Surf. Sci. 2014, 289, 203.

- L. Matˇejová, K. Koˇcí, M. Reli, L. Capek, A. Hospodková, P. Peikertová, Z.

Matˇej, L. Obalová, A. Wach, P. Ku´strowski, A. Kotarba, Appl. Catal.

B:Environ.,  2014, 152-153,  172.

- Y. Wang, Q. Lai,F. Zhang, X Shen, M. Fan, Y. He, S. Ren, RSC Adv. 2014, 4

(84) 44442.

- Q. Li, L. Zong, C. Li, J. Yang, Appl. Surf. Sci. 2014, 314, 458–463.

- M. Tahir, N.S. Amin, Appl. Catal. B:Environ., 2015, 162, 98.

- G. Xi, S. Ouyang, J. Ye, Chem. Eur. J. 2011, 17, 9057.

- W. Jiao, L. Wang,G. Liu, G. Qing (Max) Lu, H-M. Cheng, ACS Catal. 2012, 2, 1854.

- Q. Zhai, S. Xie, W. Fan, Q. Zhang, Y. Wang, W. Deng, Y. Wang, Angew. Chem. Int. Ed. 2013, 52, 5776.

- D. Liu , Y. Fernandez , O. Ola , S. Mackintosh , M. Maroto-Valer, C. M. A. Parlett , A. F. Lee , J. C. S. Wu , Catal. Commun. 2012 , 25 , 78 .

- X. Meng, S. Ouyang, T. Kako, P. Li, Q. Yu, T. Wang, J. Ye Chem. Commun., 2014, 50, 11517.

- I. Rossetti, A. Villa, C. Pirola, L. Prati. G. Ramis, RSC Adv., 2014, 4, 28883.

- W. Tu, Y. Zhou, H. Li, P. Li, Z. Zou, Nanoscale, 2015, 7, 14232.

- J. Y. Do, Y. Im, B. S. Kwak, J-Y. Kim, M. Kang, Chem. Eng. J. 2015, 275, 288.

- M. Park, B. S. Kwak, S. W. Jo, M. Kang, Energy Conversion and Management., 2015, 103, 431.

- H. Abdullah, M. R. Khan, M. Pudukudy, Z. Yaakob, N. A. Ismail, Journal Of Rare Earths,  2015, 33, 1155.

- Q. Wang, P. Dong, Z. Huang, X. Zhang Chemical Physics Letters, 2015, 639, 11.

- O. Ola, M. M. Maroto-Valer, Appl. Catal. A: General, 2015, 502, 114.

- M. Manzanares, C. Fabrega, J. O. Osso, L. F. Vega, T. Andreu, J. R. Morante,   Applied Catalysis B: Environ., 2014, 150– 151, 57– 62.

- P.N. Paulino, V.M.M. Salim, N.S. Resende, Appl. Catal. B: Environ., 2015,

doi:10.1016/j.apcatb.2015.12.037

- J. Jiao, Y. Wei, Z. Zhao, W. Zhong, J. Liu, J. Li, A. Duan, G. Jiang, Catal. Today., 2015,  258, 319.

- S. T. Hussain, K. Khan & R. Hussain, J Nat. Gas Chem, 2009, 18, 383.

- Z, Zhao, J.Fan, J.Wang and R.Li, Catal. Commun., 2012, 21, 32.

- X. Li, Z. Zhuang, W. Li, H. Pan, Appl. Catal. A: General., 2012, 429– 430, 31.

- Q. Zhang, Y. Li, E. A. Ackerman, M. Gajdardziska-Josifovska, H. Li,

Appl. Catal. A: Gen., 2011, 400, 195–202.

- B. Michalkiewicz, J. Majewska, G. Ka˛dziołka, K. Bubacz, S. Mozia, A.W. Morawski, J. of CO2 Utilization 2014, 5, 47.

- S. Zhou, Y. Liu, J. Li, Y. Wang, G. Jiang, Z. Zhao, D. Wang, A. Duan, J. Liu, Y. Wei, Appl. Catal. B Environ., 2014, 158–159, 20.

- T. Phongamwong, M. Chareonpanich, J. Limtrakul, Appl. Catal. B:Environ., 2015, 168–169, 114.

- P. Pathak, M. J. Meziani, Y. Li, L.T. Cureton, Y-P Sun, Chem. Commun., 2004, 1234.

- C. Wang, R.L Thompson,J.Baltrus, C.Matranga, J. Phys. Chem. Lett. 2010, 1, 48.

- Y T. Liang, B K. Vijayan, K A. Gray, M C. Hersam, Nano Lett, 2011, 11, 2865.

- X. Li, H. Liu, D. Luo, J. Li, Y. Huang, Y. Fang, Y. Xu, L. Zhu, Chem. Engg. Journal, 2012, 180,  151-158.

- W. Kim, T. Seok, W. Choi, Energy Environ. Sci. 2012 , 5 , 6066 .

- C. L. Zhang, Q. Y. Zhang , S. F. Kang, B. Li , X. Li , Y. G. Wang , ECS Solid State Lett. 2013, 2, M49 .

- W. J. Ong, M. M. Gui, S. P. Chai, A. R. Mohamed , RSC Adv., 2013, 3, 4505 .

- L. J. Liu, H. L. Zhao, J. M. Andino , Y. Li, ACS Catal 2012, 2, 1817.

- W. G. Tu, Y. Zhou, Q. Liu, S. C. Yan, S. S. Bao, X. Y. Wang, M. Xiao, Z. G. Zou, Adv. Funct. Mater. 2013, 23, 1743 .

- M. Anpo, H. Yamashita, Y. Ichihashi, Y. Fujii, M. Honda, J Phys Chem B, 1997, 101, 2632.

- H. Yamashita, Y. Fujii, Y. Ichihashi, S. G. Zhang, K. Ikeue, D. R. Park, K. Koyano, T. Tatsumi, M. Anpo, Catal Today, 1998, 45, 221.

- N. Ulagappan, H. Frei, J. Phys. Chem. A, 2000, 104, 7834.

- K. Ikeue, S. Nozaki, M. Ogawa, M. Anpo, Catal. Lett, 2002, 111.

- Ulagappan, H. Frei, J. Phys. Chem. A, 2000, 104, 7834; W. Lin, H. Han and H. Frei, J. Phys. Chem. B 2004, 108, 18269.

- N. Sasirekha, S.J.S. Basha, K. Shanthi, Appl. Catal. B, 2006, 62, 169.

- The-Vinh Nguyen, J.C.S. Wu, Solar Energy Mat. Solar cells, 2008, 92, 864.

- Y. Li, W. Wang, Z. Zhan, M. Woo, C. Wu, P. Biswas, Appl. Catal B:Environ., 2010, 100, 386.

- H. Li, Y. Lie, Y. Huang, Y. Fang, Y. Xu, L. Zhu, Z. Li, J. Nat. Gas Chem., 2011, 20, 145.

- C-C. Yang, J. Vernimmen, V. Meynen, P. Cool and G. Mul, J. Catalysis, 2011, 284, 1.

- W. Wang, J. Park, P. Biswas, Catal Sci. Technol., 2011, 1, 593.

- H. C. Yang, H.Y. Lin, Y.S. Chien, J.C.S.Wu and H. H. Wu, Catal. Lett., 2009, 131, 381.

- K. Koˇci, V. Mateˇjka, P. Kovar, Z. Lacny, L. Obalova, Catal. Today 2011, 161, 105.

- C. Zhao, L. Liu, Q. Zhang, J. Wang, Y. Li, Catal. Sci. Technol., 2012, 2, 2558.

- P. Akhter, M. Hussain, G. Saracco, N. Russo, Nanoscale Res. Lett. 2014, 9, 1.

- M. Hussain, P. Akhter, G. Saracco, N. Russo, Appl. Catal. B: Environ., 2015, 170–171, 53.

- J. Mao , T. Peng , X. Zhang , K. Li , L. Ye , L. Zan , Catal. Sci. Technol. 2013, 3, 1253.

- Y. Liu, G. Ji, M. A. Dastageer, L. Zhu, J. Wang, B. Zhang, X. Chang, M. A. Gondal, RSC Adv., 2014, 4, 56961.

- O. Ola, M. M. Maroto-Valer, Catal. Sci. Technol., 2014, 4, 1631.

- L Yuan, C Han, M Pagliaro, Y-J Xu, J. Phys. Chem. C, DOI: 10.1021/acs.jpcc.5b08893.

- I Shown, H-C Hsu, Y-C Chang, C-H Lin, P Kumar Roy, A Ganguly, C-H Wang, J-K Chang, C-I Wu, L-C Chen, K-H Chen, Nano Lett. 2014, 14, 6097.

- M. M. Gui, W. M. Ping Wong, S-P Chai, A. R. Mohamed, Chemical Engineering Journal 2015, 278, 272.

- B. Tahir, M. Tahir, N. Saidina Amin, Appl. Surf. Sci., 2015, 338, 1.

- L. L. Tan, W-J. Ong, S-P. Chai, A.R. Mohamed, Appl. Catal. B: Environ., 2015, 166–167, 251.

- J-J Wang, Y-H. Jing, T. Ouyang, Q. Zhang, C-T Chang, Catal. Commun., 2015, 59, 69.

- S. Won Jo, B. S. Kwak, K. M. Kim, J. Y. Do, N-K. Park, S. O Ryu, H-J Ryu, J-I Baek, M. Kang,  Appl. Surf. Sci., 2015, 355, 891.

- K. Sayama, H. Arakawa, J. Phys. Chem. 1993, 97, 531.

- C.C. Lo, C.H. Hung, C.S. Yuan, J.F. Wu, Sol. Energy Mater. Sol. Cells, 2007, 91, 1765.

- M. Subrahmanyam, S. Kaneco, N. Alonso-Vante, Appl. Catal B:Environ., 1999, 23, 169.

- K. Teramura, T. Tanaka, H. Ishikawa, Y. Kohno, T. Funabiki, J. Phys. Chem. B., 2004, 108, 346.

- K. Teramura, H. Tsuneoka, T. Shishido, T. Tanaka, Chem. Phys. Lett., 2008, 467, 191.

- S. Yoshida, Y. Kohno, Catal. Surveys from Japan, 2000, 4, 107.

- H. Park, J. H. Choi, K. M. Choi, D. K. Lee, J. K. Kang, J. Mater. Chem., 2012, 22, 5304.

- X.Y. Chen, Y. Zhou, Q. Liu, Z. D. Li, J. G. Liu, Z. G. Zou, ACS Appl. Mater. Interfaces 2012, 4, 3372 .

- Y. P. Xie, G. Liu, L. C. Yin, H. M. Cheng, J. Mater. Chem. 2012 , 22 , 6746 .

- G. C. Xi, S. X. Ouyang, P. Li, J. H. Ye, Q. Ma, N. Su, H. Bai, C. Wang, Angew.

Chem. Int. Ed. 2012, 51, 2395 .

- L. Liu, C. Zhao, D. Pitts, H. Zhao, Y. Li, Catal. Sci. Technol., 2014, 4, 1539.

- P. Niu, Y. Yang, J. C. Yu, G. Liu, H-M Cheng, Chem. Commun., 2014, 50, 10837.

- M. Li, L. Zhang, X. Fan, Y. Zhou, M. Wu, J. Shi J. Mater. Chem. A, 2015, 3, 5189.

- M. M. Gui, S-P Chai, B-Q. Xu, A. R. Mohamed RSC Adv., 2014, 4, 24007.

- W-N. Wang, F. Wu, Y. Myung, D. M. Niedzwiedzki, H S Im, J Park, P Banerjee, P Biswas ACS Appl. Mater. Interfaces 2015, 7, 5685.

- J-C Wang, L Zhang, W-X Fang, J Ren, Y-Yu Li, H-C Yao, J-S Wang, Z-J Li, ACS Appl. Mater. Interfaces 2015, 7, 8631.

- B. AlOtaibi, S. Fan, D. Wang, J. Ye, Z. Mi, ACS Catal. 2015, 5, 5342.

- R. Zhou, M. I. Guzman J. Phys. Chem. C 2014, 118, 11649.

- J. Lin, Z. Pan, X. Wang, ACS Sustainable Chem. Eng. 2014, 2, 353.

- F. Ehsan, T. He, Applied Catalysis B: Environ., 2015, 166–167, 345.

- Y. Matsumoto, M. Obata, J. Hombo, J. Phy. Chem., 1994, 98, 2950.

- G. Guan, T. Kida, A. Yoshida, App. Catal., B:Environ., 2003, 41, 387.

- G. Guan,T. Kida ,T. Harada, M. Isayama, A.Yoshida, App. Catal. A: Gen. 2003, 249, 11.

- K. Teramura, H. S-I. Okuoka, H. Tsuneoka, T. Shishido, T. Tanaka, Appl. Catal. B: Environ., 2010, 96, 565.

- Y. Zhou, Z. Tian, Z. Zhao, Q. Liu, J. Kou, X. Chen, J. Gao, S. Yan, Z. Zou, ACS

Appl. Mater. Interfaces, 2011, 3, 3594.

- H. Shi, T. Wang, J. Chen, C. Zhu, J. Ye, Catal Lett, 2011, 141, 525.

- Peng Li, S. Ouyang, G. Xi, T. Kako, J. Ye, J. Phys. Chem. C, 2012, 116, 7621.

- N. Zhang, S. Ouyang, T. Kako, J. Ye, Chem. Commun., 2012, 48, 1269-1271.

- K. Iizuka, T. Wato, Y. Miseki, K. Saito, A. Kudo, J. Am. Chem. Soc. 2011, 133, 20863.

- C. W. Tsai, H. M. Chen, R. S. Liu, K. Asakura, T. S. Chan, J. Phys. Chem. C, 2011, 115, 10180.

- D.S. Lee, H. J. Chen, Y. W. Chen, J. Phys. Chem. Solids 2012, 73, 661.

- X. Li, H. Pan, W. Li, Z. Zhuang, Appl. Catal. A: Gen, 2012, 413– 414, 103.

- A. Ahmed , Y. Shibata ,T. Taniguchi T, Izumi, J. Catal. 2011, 279, 123.

- Q.D. Truong, J. Y. Liu, C. C. Chung, Y. C. Ling, Catal. Commun., 2012, 19, 85.

- J. W. Lekse, M. K. Underwood, J. P. Lewis, C. Matranga, J. Phys. Chem. C, 2012, 116, 1865.

- X. Li, W. Li, Z. Zhuang, Y. Zhong, Q. Li, L. Wang,  J. Phys. Chem. C.  DOI:10.1021/jp303365z  (2012).

- W-H Lee, C-H Liao, M-F Tsai, C-W Huang, J. C.S. Wu, Appl. Catal. B:Environ., 2013, 132, 445.

- Y-H Cheng, V-H Nguyen, H-Y Chan, J.C.S. Wu, W-H. Wang, Appl. Energy, 2015, 147, 318.

- K. Xie, N. Umezawa, N. Zhang, P. Reunchan , Y. Zhang , J. Ye, Energy Environ. Sci. 2011 , 4 , 4211.

- D. D. Sui, X. H. Yin, H. Z. Dong, S. Y. Qin, J. S. Chen, W. L. Jiang, Catal. Lett. 2012, 142, 1202 .

- H. Zhou, J. J. Guo, P. Li, T. X. Fan, D. Zhang, J. H. Ye , Sci. Rep. 2013, 3, 1667.

- P. Li, Y. Zhou, W. G. Tu, Q. Liu, S. C. Yan, Z. G. Zou, Chem Plus- Chem 2013, 78, 274 .

- S. Feng, X. Chen, Y. Zhou, W. Tu, P. Li, H. Li , Z. Zou, Nanoscale 2014, 6, 1896.

- P. Li, Y. Zhou, W. G. Tu , R. Wang, C. F. Zhang, Q. Liu, H. J. Li, Z. D. Li, H.

Dai, J. J. Wang, S. C. Yan, Z. G. Zou, Cryst. Eng. Comm., 2013 , 15 , 9855 .

- H. F. Cheng, B. B. Huang, Y. Y. Liu, Z. Y. Wang, X. Y. Qin, X. Y. Zhang, Y.

Dai, Chem. Commun., 2012 , 48 , 9729 .

- J. J. Guo, S. X. Ouyang, T. Kako, J. H. Ye, Appl. Surf. Sci. 2013 , 280 , 418 .

- S.C. Yan, S.X. Ouyang, J. Gao, M. Yang, J.Y. Feng, X.X. Fan, L.J. Wan, Z.S. Li,  J.H. Ye, Y. Zhou, Z.G. Zou, Angew. Chem. Int. Ed., 2010,  49, 6400.

- S. C. Yan, J. J. Wang, H. L. Gao, N. Y. Wang, H. Yu, Z. S. Li, Y. Zhou, Z. G. Zou, Adv. Funct. Mater. 2013, 23, 758.

- S. Yan, H. Yu, N. Wang, Z. Li, Z. Zou, Chem. Commun., 2012 , 48 , 1048

- Q. Liu, Z. X. Low, L. X. Li, A. Razmjou, K. Wang, J. F. Yao, H. T. Wang, J. Mater. Chem. A. 2013, 1, 11563 .

- Q. Liu, Y. Zhou, Z. P. Tian, X. Y. Chen, J. Gao, Z. G. Zou, J. Mater.Chem. 2012, 22, 2033 .

- 218. S. C. Yan, J. J. Wang , H. L. Gao, N. Y. Wang, H. Yu, Z. S. Li, Y. Zhou, Z. G. Zou, Adv. Funct. Mater. 2013, 23, 1839 .

- Q. Liu, Y. Zhou, Y. Ma, Z. G. Zou, RSC Adv. 2012, 2, 3247 .

- Z. D. Li, Y. Zhou, J. Y. Zhang, W. G. Tu, Q. Liu, T. Yu, Z. G. Zou, Cryst. Growth. Des. 2012, 12, 1476 .

- K. Teramura, S. Iguchi, Y. Mizuno, T. Shishido, T. Tanaka, Angew Chem. Int. Ed. 2012, 51 , 8008 .

- N. Ahmed, M. Morikawa, Y. Izumi, Catal. Today. 2012, 185, 263 .

- K. Li, A. D. Handoko, M. Khraisheh, J. Tang, Nanoscale, 2014, 6, 9767.

- C. Zhao, L. Liu, G. Rao, H. Zhao, L. Wang, J. Xua, Y. Li, Catal. Sci. Technol., 2015, 5, 3288.

- P. Zhou, S. C. Yan, Z. G. Zou, CrystEngComm, 2015, 17, 992.

- Z. Wang, M. Jiang, J. Qin, H. Zhou, Z. Ding, Phys. Chem. Chem. Phys., 2015, 17, 16040.

- S. Zhu, S. Liang, J. Bi, M. Liu, L. Zhou, L. Wu, X. Wang, Green Chem. 2015, DOI:   10.1039/C5GC02308D.

- H. Zhou, P. Li, J. Guo, R. Yan, T. Fan, D. Zhang, J. Ye, Nanoscale, 2015, 7, 113.

- X. Chen, J. Wang, C. Huang, S. Zhang, H. Zhang, Z. Li, Z. Zou, Catal. Sci. Technol., 2015, 5, 1758.

- S. Wang, Y. Hou, X. Wang ACS Appl. Mater. Interfaces 2015, 7, 4327.

- W. Kim, H. Frei, ACS Catal. 2015, 5, 5627.

- Y. Bi, M. Fahad Ehsan, Y. Huang, J. Jin, T. He, J. of CO2 Utilization, 2015, 12, 43.

- B. S. Kwak, M. Kang, Appl. Surf. Sci., 2015, 337, 138.

- S. K. Parayil, A. Razzaq, S-M. Park, H. R. Kim, C. A. Grimes, S-Il In, Appl. Catal. A: General, 2015, 498, 205.

- J. Premkumar, R. Ramaraj, J. Photochem. & Photobiol A:Chem., 1997, 110, 53.

- O. Ozcan, F. Yukruk, E.U. Akkaya, D. Uner, Applied Catalysis B: Environ., 2007, 71, 291.

- T.-V. Nguyen, J. C. S. Wu and C-H.Chiou, Catal. Commun., 2008, 9, 2073.

- Z. Zhao, J. Fan, S. Liu, Z. Wang, Chem. Eng. Journal, 2009, 151, 134.

- Z. Zhao, J. Fan, M. Xie & Z.Wang, J Cleaner Prodn, 2009, 17, 1025.

- K.R. Thampi, J. Kiwi, M. Graetzel, Nature 1987, 327 (6122), 506.

- O. Ozcan, F. Yukruk, E.U. Akkaya, D. Uner, Appl. Catal. B Environ., 2007, 71,  291.

- G. Qin, Y. Zhang, X. Ke, X. Tong, Z. Sun, M. Liang, S. Xue, Appl. Catal. B:Environ., 2013, 129, 599.

- T. Arai, S. Sato, T. Morikawa, Energy Environ. Sci., 2015, 8, 1998.

- K. Li, L. Lin, T. Peng, Y. Guo, R. Li, J. Zhang, Chem. Commun., 2015, 51, 12443.

- L. Schmidt-Mende, J. K. Stolarczyk, S. N. Habisreutinger, Angew. Chem. Int. Ed. 2013, 52, 7372.

- N.M. Dimitrijevic, B. K. Vijayan, O. G. Poluektov, T. Rajh, K. A. Gray, H. He and P. Zapol, J. Amer. Chem. Soc., 2011, 133, 3964.

- K. Kocˇ, L. Obalov, O. Sˇ olcov, Chem. Process Eng. 2010, 31, 395.

- M. Anpo, H. Yamashita, Y. Ichihashi, S. Ehara, J. Electroanal.Chem., 1995, 396, 21.

- C-C. Yang, J. Vernimmen, V. Meynen, P. Cool, G. Mul, J. Catalysis, 2011, 284, 1; C-C. Yang, Ph. D Thesis, University of Twente, Twente, The Netherlands (2011)

- S. S. Tan, L. Zou, E.Hu, Catal. Today, 2008, 131, 125.

- I. A. Shkrob, N. M. Dimitrijevic, T. W. Marin, H. He, P. Zapol, J. Phys. Chem. C 2012, 116, 9461.

- I. A. Shkrob, T.W. Marin, H. He, P. Zapol, J. Phys. Chem. C 2012, 116, 9450.

- M.R. Hoffmann, J.A. Moss, M.M. Baum, Dalton Trans. 2011, 40, 5151.

- G. Palmisano, E. Garcı´a-Lo´ pez, G. Marcı´, V.Loddo, S. Yurdakal, V. Augugliaro, L. Palmisano, Chem. Comm., 2010, 46, 7074.

- K. Li, D. Martin, J. Tang, Chinese J. Catal., 2011, 32, 879.

- J. Ye , Z. Zou, H. Arakawa, M. Oshikiri, M. Shimoda, A. Matsushita and T.  Shishido, J. Photochem. & Photobiol. A: Chemistry, 2002, 148, 79.

- W. Junhu , Z. Zhigang , Ye. Jinhua, J. Alloys and Compds., 2004, 377, 248.

- Q. Xiang, J. Yu, M. Jaroniec, Chem. Soc. Rev., 2012, 41, 782.

- M-Q Yang, Y-J. Xu, Phys. Chem. Chem. Phys., 2013, 15, 19102.

- M-Q Yang, N. Zhang, M. Pagliaro, Y-J. Xu, Chem. Soc. Rev., 2014, 43, 8240.

- X. Xie, K. Kretschmer, G. Wang, Nanoscale, 2015, 7, 13278

- W. Kim, T. Seok and W. Choi, Energy Environ. Sci., 2012, 5, 6066.

- J. Morris, G. J. Meyer and E. Fujita, Acc. Chem. Res., 2009, 42, 1983.

- G. Seshadri, C. Lin and A. B. Bocarsly, J Electroananl. Chem, 1994, 372, 145.

- Ganesh, Mater Sci. and Applns., 2011, 2, 1407.

- Y.R. Smith, V. Subramanian, B. Viswanathan,“ Photo-electrochemical and

Photocatalytic conversion of carbon dioxide, Chapter 9, in “Photo-electrochemistry and photobiology for sustainability”, 2010, 1, 217. (Eds. S. Kaneco, B. Viswanathan and H Katsumata), Bentham Science.