## Slide 1: Catalyst Characterization and Interpretation
National Centre for Catalysis Research
Indian Institute of Technology Madras
Presentation 4

## Slide 2
Course Details
Online Lecture Series 4
Catalyst Characterization and Interpretation
Online Lecture Series 1 Carbon Dioxide Conversion into Chemicals and Fuels
Online Lecture Series 2 Photo and Photo-electrochemical Water Splitting
Online Lecture Series 3 Fundamentals of Electrochemistry
Online Lecture Series 4 Catalyst Characterization and Interpretations
All these lectures will be available in YouTube
One can view them whenever they want

## Slide 3: A Site at NCCR for Catalysis
http://catalysis.eprints.iitm.ac.in/

## Slide 4
1.1. Introduction to Catalytic Phenomena
1.1.1. Emergence of Catalyst Technology: A Brief History
1.1.2. Importance of Catalysis and Catalyst Technology
1.1.3. Fundamental Catalytic Phenomena and Principles
Exercises/Assignments/Reading Materials
1.2. Catalyst Characterization and Selection
1.2.1. Principles and Objectives of Catalyst Characterization
1.2.2. Determining Physical Properties of Catalysts
1.2.3. Determining Chemical Properties of Catalysts
Exercises/Assignments/Reading Materials
Module 1

## Slide 5
2.1. Morphology and Physical Properties
2.1.1. Gas Adsorption at Low Temperatures
2.1.2. Mercury Porosimetry
2.1.3. Incipient wetness method
2.1.4. Microscopy
2.1.5.1. Electron Microscopy
2.1.5.2. Field Emission Microscopy and Ion Microscopy
Exercises/Assignments/Reading Materials
Module 2

## Slide 6
Module 3
3.1. Surface Properties
3.1.1. Volumetric, Gravimetric Adsorption Methods
3.1.2. Adsorption Calorimetry
Exercises/Assignments/Reading Materials
3.2. Spectroscopy in Catalysis
3.2.1. UV- Vis spectroscopy
3.2.2. IR spectroscopy
3.2.3. Raman Spectroscopy
3.2.4. Temperature-Programmed Techniques
3.2.4.1. Temperature-Programmed Reduction
3.2.4.2. Temperature-Programmed Sulfidation
3.2.4.3. Temperature-Programmed Reaction Spectroscopy
3.2.4.4. Temperature-Programmed Desorption
3.2.4.5. Temperature-Programmed Reaction
Spectroscopy in UHV
Exercises and Assignments/Reading Materials
Cont’d

## Slide 7
3.3. Photoemission and Auger Spectroscopy
3.3.1. X-Ray Photoelectron Spectroscopy (XPS)
3.3.2. Ultraviolet Photoelectron Spectroscopy (UPS)
3.3.3. Auger Electron Spectroscopy
Exercises and Assignments
3.4. The Ion Spectroscopies
3.4.1. Secondary Ion Mass Spectrometry (SIMS)
Exercises and Assignments
3.5. Diffraction and Extended X-Ray Absorption Fine Structure (EXAFS)
3.5.1. X-Ray Diffraction
3.5.2. Low-Energy Electron Diffraction (LEED)
3.5.3. X-Ray Absorption Fine Structure (XAFS)
Exercises and Assignments
Module 3

## Slide 8
Module 4
4.1. Bulk Properties
4.1.1. Particle Size Distribution and Mechanical Properties
4.1.2. Particles Size Analysis
4.1.3. Application to Phase Identification
4.1.4 Application to Phase Characterization:
4.1.5. X-Ray Diffraction of Catalysts in a Reactive Atmosphere
4.1.6. Small-Angle X-Ray Scattering (SAXS)
Eexercises/Assignments/Reading Materials
Module 4

## Slide 9
Introduction
Presentation 4
30th August 2017
4 pm IST
Online Lecture Series 4
Catalyst Characterization and Interpretation

## Slide 10
Importance of Catalysis and Catalyst Technology

## Slide 11
Dahl, Logadottir, Egeberg, Larsen, Chorkendorff, Törnqvist, Nørskov, Ph
Au decorates steps:
Hwang, Schroder, Gunther, Behm,
Phys. Rev. Lett. 67, 3279 (1991)
Steps Do Everything

## Slide 12
Logatottir, Rod, Nørskov, Hammer, Dahl, Jacobsen, J. Catal. 197, 229 (2001)
The Brønsted-Evans-Polanyi relation

## Slide 13: 400 C, 50 bar, H2:N2=3:1, 5% NH3
Logatottir, Rod, Nørskov, Hammer, Dahl, Jacobsen, J. Catal. 197, 229 (2001)
Calculated Ammonia Synthesis Rates

## Slide 14
Jacobsen, Dahl, Clausen, Bahn, Logadottir, Nørskov, JACS 123 (2001) 8404.
Interpolation in the Periodic Table

## Slide 15: 400 C, 50 bar, H2:N2=3:1
Jacobsen, Dahl, Clausen, Bahn, Logadottir, Nørskov, JACS 123 (2001) 8404.
Measured Ammonia Synthesis Rates

## Slide 16
High Throughput Screening
  Direct testing of many catalysts, fast, efficiently
Data Mining
  Correlating catalytic aactivity/selectivity/ durability to descriptors that can be tabulated
Data Driven Methods

## Slide 17
The Object of the Game…
Find sets of descriptors {Dik} of solid materials Mi , and a mathematical model F such that Aij being the Turn Over Frequency of Mi as catalyst for the reaction j at operationg conditions Cj one has:
Identify ranges of Dik that maximize F
Screen Databases of Materials Properties before screening real materials
Better if one descriptor is sufficient, but do not take it for granted
Much better if F has a sound physical basis
Adsorbate/substrate bond strengths should provide good descriptors according to the Sabatier principle
H. Toulhoat and P. Raybaud Workshop Catalysis from First Principles Vienna 02/02
Using DFT Calculations in the Search of Prospective Catalysts

## Slide 18
E MC @ Fm-3m carbides is rather consistent with simple chemisorption models
Onset of dissociative chemisorption as MC bond strength increases
Using DFT Calculations in the Search of Prospective Catalysts
H. Toulhoat and P. Raybaud Workshop Catalysis from First Principles Vienna 02/02

## Slide 19
The experimental alloying effects is correctly predicted
Using DFT Calculations in the Search of Prospective Catalysts
H. Toulhoat and P. Raybaud Workshop Catalysis from First Principles Vienna 02/02

## Slide 20
Structure (in situ)
Spectroscopy (in situ)
Surface thermochemistry
Calculations
There is a large need for systematic data - and for good descriptors
Getting Data/Descriptors

## Slide 21
1.5
10
0.5
0
0
1
2
3
Number of Co edge atoms
(x1020/g catalyst)
HDS activity
(x102/mol/g/h)
Topsøe, Clausen, Massoth Hydrotreating Catalysis, Science and Technology
(Anderson and Boudart (Eds.), Springer (1996).
Structure-activity Correlation
Hydrodesulphurization of Thiophene

## Slide 22
Descriptors from Spectroscopy
CO TPD shift
Core level shift
Goodman and Rodriguez, Science 279 (1992) 87

## Slide 23
Cu/MgO
Ag/MgO
Pb/MgO
Larsen, Starr, Campbell, Chem.Thermodyn. 33, 333 (2001)
Brown, Kose, King, Chem. Rev. 98, 797 (1998).
Single Crystal icrocalorimerty

## Slide 24
Pt
M
S. Gottesfeld et al.,
J. Electrochem. Soc. 148 (2001) A11.
Christoffersen, Liu, Ruban, Skriver, Nørskov, J.Catal. 199, 123 (2001)
CO tolerance of Pt alloy anodes for PEM fuel cells

## Slide 25
Calculated d band shifts:
Ruban, Hammer, Stoltze, Skriver, Nørskov, J.Mol.Catal. A 115, 421 (1997)
Over layer
Host
How can the d-band center be changed?

## Slide 26
Bengaard, Rostrup-Nielsen, Nørskov
b
Transition state for CH4 dissociation on Ni(211)
Methane activation

## Slide 27
Egeberg, Chorkendorff, Catal. Lett. 77, 207 (2001)
Methane activation on Ni/Ru

## Slide 28
Catalysis at ambient temperature and pressure
Extreme selectivity
Direct coupling of energy into the important reaction coordinate (non-thermal catalysis)
Lessons from Biology

## Slide 29
Burgess, Lowe, Chem. Rev. 96, 2983 (1996)
Schindelin, Kisker, Schlessman, Howard, Rees, Nature 387, 370 (1997)
Nitrogenase

## Slide 30
Rod, Nørskov JACS 122, 12751 (2000)
N2 Hydrogenation on FeMo Cofactor

## Slide 31
Well developed basic understanding – theory-experiment
Beginning to be able to use it directly in catalyst design
Some activity-descriptor correlations
Host of new in situ methods for catalyst characterization
New very powerful screening methods
We have a starting point which is radically different from the situation 5 or 10 years ago!
Status

## Slide 32
More basic understanding –theory-experiment
Integration of the conceptual framework for heterogeneous, homogeneous and enzyme catalysis
More systematic data (descriptors)
Better synthesis methods
Better coupling of catalyst design and process engineering
INTEGRATION
Moving Forward

## Slide 33
Synthesis
testing
characterization
Experiments, models
Theory
An integrated approach:
Promoting Development

## Slide 34: Atom-Economy, Environmental Issues, Enantiomeric Purity

## Slide 35
1.Surface-Tailored Molecular Precursors for Nanostructured Catalysts. 2. Self-Assembly and Recognition Mechanisms in Supramolecular Chemistry as Tools to Prepare New Catalysts.
Molecular and Supramolecular Chemistry in Catalysis

## Slide 36
Molecular insight in Homogeneous and
Heterogeneous Catalysts Mechanistic Comprehension of Catalytic Processes.

## Slide 37
Catalytic Reaction Engineering.
Kinetics of Molecularly Defined Heterogeneous Catalysts
Scale up Issues of Industrially Relevant Processes

## Slide 38: CHEMICAL INDUSTRY & CATALYSIS

## Slide 39: CHEMICAL INDUSTRY & CATALYSIS GLOBAL SCENERIO
Chemical/Hydrocarbon industy: $ 1.5 Trillion global enterprise
Catalysis: The key to economic & environmental viability of the industry
More than 7000 products manufactured per year using catalysts
Catalyst market: $ 10 Bill. Industry
Major segments Growth rates (%)
Refining & Petrochemicals 2
Hydroprocessing 5-7
Polymerization 7-10
Chemicals 5
Environmental 10

## Slide 40: CATALYSIS IN CHEMICAL INDUSTRY: APPLICATIONS
Catalysis
Petroleum
refining
Petro-
chemicals
Fertilizer&
Inorganic
chemicals
Pharma-
ceutical
Fine &
Agro
chemicals
Environ-
mental
protection

## Slide 41: CATALYSIS: THE KEY TO INNOVATIONS IN CHEMICAL TECHNOLOGY
Catalysis
New
processes
New
products
Feed stock
Cost of
production
Environment
Energy

## Slide 42: INCREASE IN SELECTIVITY: ECONOMIC IMPACT
Product | Selectivity improvement (%) | Global feedstock savings per year (Mill US$)
Ethylene oxide | 9 | 365
Terephthalic acid | 2 | 35
Acrylonitrile | 18 | 390
Adipic acid & Caprolactum | 7 | 215
Propylene oxide | 3 | 300
Vinyl acetate | 12 | 70
 | TOTAL | 1375

## Slide 43: DEVELOPMENT & COMMERCIALIZATION OF CATALYSTS: KEY ELEMENTS
Research & Development
Innovation/Intellectual Property Rights
Pilot scale efforts, scale up & process economics
Product & Process technology development
Process engineering / Instrumentation/Construction
Process licensing
Manufacture
Marketing
Technical services

## Slide 44: CHEMICAL INDUSTRY- CHALLENGES
Constraints in feedstock with respect to availability, quality & cost
Eco friendly processes & products: stringent emission levels
Need for conserving energy
Waste minimization/effective treatment
Catalysts with higher efficacy: activity/selectivity/ life
Process improvements: milder conditions/fewer steps
Ever-increasing demand for niche /specialty products at affordable prices
New catalysts /processes: Reduction in discovery & process development cycle time

## Slide 45: Feedstock-Alternative routes
Ethylene
Propylene

## Slide 47
Propylene : Demand- Supply gap

## Slide 48: Aletrnative routes for propylene Catalytic Dehydrogenation of Propane
Process | Catalyst | Temp ° C | Pressure (psig) | Conv. (%) | Selectivity (%) | Life (Yrs) | Reactor type
Oleflex* UOP | Pt/ Al2O3 | 600- 650 | 30 | 20-30 | 9090 | CCR | Stacked radial flow adiabatic
Catofin* Houdry | Cr2O3/ Al2O3 | 600- 650 | 30-100 | 25-30 | 95 | 1.5- 3 15 min. Regen. | Fixed bed, adiabatic, cascade mode
STAR* Phillips | Pt/ Al2O3 | 560- 620 | 30-100 | 28-40 | 89-95 | 1-2 | Fixed bed isothermal
FBD-4 | Cr2O3/ Al2O3 | - | - | - | - |  | Fluid bed
Linde- BASF | Cr2O3/ Al2O3 | - | - | - | - |  | Fixed bed Isothermal

## Slide 49: Catalyst Life-Reactor type

## Slide 51: Alternative routes for Propylene
Olefin Metathesislefin Metathesis
C2H4 + C4H8  2 C3H6
Can be a stand alone unit or integrated with cracker/FCC unit
Low investment, less energy intensive, attractive returns
High propylene/ethylene yield ratios, varying from 0.5 to 1.1
Use of low cost C4 stream
Process technologies
META-4 ® (Axens – IFP Group Technologies)
OCT ® Olefins Conversion Technology (ABB Lummus)
UOP’s process
Depends on relative costs of ethylene & propylene

## Slide 52: Metathesis- Catalysts & Process conditions

## Slide 53: Alternative routes to Propylene
Olefin Inter conversion Processes
Catalytic cracking of C4- C5 streams or the light naphtha streams in a fixed or fluidized bed reactor
Compatible with crackers and FCC units
Unlike metathesis, do not consume ethylene.
Process technologies
Olefin Cracking Process (UOP-ATOFINA)
Propylur (Lurgi)
PCC process (Exxon –Mobil)
SUPERFLEX ® (Lyondell/Kellogg)
Mobil’s Olefin Inter conversion Process (MOI)

## Slide 55: Tuning the Selectivity

## Slide 56
PARA-DISUBSTITUTED AROMATICS:USEFULNESS
para-xylene
Raw Material for polyester fiber, platiciser etc
para-ethyl toluene
Starting material for poly (para-methyl) styrene
para-diethyl benzene
Desorbent for separation of para-xylene from C8 raffinate
Raw material for variety of polymers, antioxidants, stabilizers, hydroquinones
Raw material for para-cresol, fragrances, herbicides pharmaceuticals etc
Raw material for variety of polymers, antioxidants
C2H5
H3C
CH3
H3C
C2H5
H5C2
C
H3C
CH3
CH3
para-cymene
para-diisopropyl benzene
H3C
H3C
C
C
CH3
CH3
para-ethyl phenol
OH
H5C2

## Slide 57
+ R2OH
R1
R2
R1
R1
R2
R1
R2
R2
R1
Fig.2 Selective alkylation reactions over pore size regulated zeolite

## Slide 59
H5C2
H3C
H3C
CH3
H3C
CH3
H3C
CH3
CH3
H3C
CH3
Catalyst/Process for PDEB Production
Issue of Other Aromatics in Feed

## Slide 60
H5C2
H3C
H3C
CH3
H3C
CH3
H3C
CH3
H3C
CH3
CH3
Bz, Tol. : Create hindrance, get alkylated, reduce yield of PDEB
p-X, PDEB : Create more hindrance, but does not participate in reaction
m-X, o-X, TMBs: Act only as diluent
Bhat, Das & Halgeri: Appl. Catal, A: Gen., 1994, 115, 257-267
Catalyst/Process for PDEB Production
The PDEB selectivity is not affected any way
Pore Size Engineered MFI Zeolite

## Slide 61: Asymmetric Hydrogenation

## Slide 62: Asymmetric Hydrogenation

## Slide 63
Asymmetric hydrogenation of -Phenyl acrylic acid to Hydratropic acid in 15 % ee
The Nobel Prize in Chemistry for 2001 was awarded to Prof . KB. Sharpless for Asymmetric catalytic oxidation Prof.R. Noyori & Prof. WS. Knowles for Asymmetric catalytic hydrogenation

## Slide 64: Design of Catalysts
Fluid Catalytic Cracking
Hydrotreating

## Slide 65: The Oil Industry
Oil provides the largest share (39%) of world energy
source than any other forms
Despite dwindling reserves, global oil consumption is
growing:(MBPD)
  73.15 (1997)
  80.74 (2002)
  112.8 (2020)
Modern oil refineries produce a wide range of fuels &
feed stocks through different processes

## Slide 66: Oil Refining Industry: Key Issues
Tough environmental regulations
Increasing cleanliness of fuels
Increasing yields from crudes of inferior
quality
Globalization, thin profit margins
Public scrutiny of environment,
Global warming

## Slide 67
Processes in Oil Refining |  | 
Physical | Thermal | Catalytic
Distillation | Visbreaking | Hydrotreating
Solvent extraction | Delayed coking | Catalytic Reforming
Solvent dewaxing | Flexicocking | Catalytic Cracking
Propane deasphalting |  | Catalytic dewaxing
Blending |  | Hydrocracking
 |  | Isomerization
 |  | Alkylation
 |  | Etherification
 |  | Polymerization

## Slide 68
Fluid Catalytic Cracking (FCC)
Heart of any modern refinery
One of the marvels of petroleum refining technology
Very high levels of sophistication in technology &
process efficiency
Significant value addition and up gradation of
petroleum fractions.
Accounts for 30-40% of refining capacity
Major contributor to the gasoline pool
  FCC (35%)
  Catalytic reforming(30%)
  Alkylation (20%)
  Isomerization (15%)

## Slide 69: FCC Process : Advantages
Very high flexibility different & difficult feeds
Yields a variety of valuable products:
  Light olefins, Alky feed, Oxygenates
  Gasoline, LCO, CSO
Volume gain (6 – 12 %), economically attractive
Operates at lower pressure/lower operating cost
Highly energy efficient
Alive to environmental issues
Inexpensive catalyst

## Slide 70: FCC Today More than 400 units 13 MBPD capacity Catalyst consumption 1500 TPD Largest FCC unit-RIL JN-9 MTA
FCC Future

## Slide 72: FCC : Operating conditions
Reactor temperature (C) 500-550
Regenerator temperature (C) 720-800
Catalyst/Oil (wt ratio) 5-16
Reactor space velocity (lb/hr/lb) 1.1-13.4
Catalyst requirement (lb/bbl feed) 0.15-0.25
Average contact time (Sec) 2-3
Reactor-regenerator-cycle time (min) 10
Catalyst circulation rate (MT/Sec) 1Max.
Reactor pressure psig 15-20

## Slide 74: Amorphous silica-alumina Vs Zeolite: Advantages
high activity : at least 104 times more active
high density of acid sites
Favourable distribution site strengths
Pore geometry
- longer life
- hydrothermal stability
- high gasoline/olefins yields
- low coke/ gas make
- better attrition resistance, metal passivation
2 Bill.$ savings per annum when introduced first in US

## Slide 75: FCC Catalysts Application Vs Composition
Gasoline
REHY-10 13 % RE2O3, 15-25% zeolite content with moderately active SiO2& clay matrix
Octane boosting
HSY/REHY with lower RE with active matrix of Al2O3 or SiO2-Al2O3 plus clay and ZSM-5 additive
Light olefins- PETRO-FCC
HSY/REHY with lower RE with active matrix of Al2O3 or SiO2-Al2O3 plus clay and ZSM-5 additive for olefins maximisation
Resid cracking
HSY/REHY with higher RE, 35-40% zeolite content, with large pore active matrix of Al2O3 or SiO2-Al2O3 plus modified clay plus metal passivators /traps, Sox, NOx CO combustion additives

## Slide 76: FCC Catalysts: Challenges & Design
Acidity: type, site density, strength distribution
Feed characteristics
Complex feed, many reactants, active sites
distribution
Pore modulation./accessibility
Product slate/Yield pattern
Gasoline/Octane/Olefins
Coke combustion
Metal passivation
Mechanical properties/attrition
Morphology/free flow

## Slide 81: C1Chemistry

## Slide 82: C1Chemistry
Drivers
Abundance of gas ( C1) 180 TCM, to last 70 years
Global shift towards gas based economy
Minimize flaring, pollution & energy loss
Stranded gas monetization- Viable alternaive
Technological options
Syn gas to olefins / fuels /n-paraffins via Fischer Tropsch Synthesis
Syngas to fuels/n-paraffins via GTL
Syngas to DME/ Methanol
Methanol to C2/C3 Olefins ( MTO)
Methanol to Propylene (MTP)
Methane to methanol

## Slide 83: Utilization of Natural Gas Global scenario
Consumption
Chemical feedstocks : 200 Mill.MT
Fuels and chemicals : 3,500 Mill.MT
Proven reserves : 217,000 Mill.MT
Reserves to last for 60-70 more years
Stranded gas reserves need special
attention

## Slide 86
UOP-HYDRO MTO PROCESS

## Slide 87
Methanol To Propylene- Lurgi Process

## Slide 89: ALKANE ACTIVATION

## Slide 90: ALKANE ACTIVATION: CHALLENGES
Inert molecules. Difficult to activate/convert
Lower per pass conversion for acceptable selectivity levels
Extensive recycle streams/equipments/investments
Corrosive catalysts/special & costly MOC
Reaction heat transfer/reactor design
INITIATIVES BY CSIR
New Millennium Indian Technology Leadership Initiatives (NMITLI)
NONO MATERIALS
FUNCTIONALIZATION OF ALKANES

## Slide 91: DEVELOPMENTS IN ALKANE ACTIVATION
METHANE PROPANE
Oxidative coupling Acrylonitrile
Formaldehyde Propylene*
Methanol
ETHANE BUTANE
Oxidative dehydrogenation Maleic anhydide*
Acetic acid*
Vinyl chloride
Ethylene glycol
* COMMERCIALLY SUCESSFUL PROCESS
OTHERS AT LABORATORY/PILOT SCALE

## Slide 92: ACID CATALYSED REACTIONS
Conventional catalysts
AlCl3,HF,H2SO4,H3PO4
Potential hazards in storage, handling & disposal
Generation of waste products/disposal isssues
Non-regenerable
Corrosion, Special MOC, higher investment costs
Solid acid catalysts
Ion-exchange resins
Clays
Amorphous silica-alumina
Crystalline aluminosilicates (Zeolites)

## Slide 93: SOLID ACID BASED CATALYTIC PROCESSES
Alkylate production
- ALKYLENE by UOP
- Thin layerd catalyst by ABB Lummus
- Several processes under development
Aromatics alkylation
- Cumene
- Ethyl benzene
- Linear Alkyl Benzene

## Slide 94: Clean Fuels

## Slide 95: Clean Fuels

## Slide 97: Catalysis for Environment
Process technologies for clean fuels
- Hydrogen requirement
- Loss of RON
- Heavy investments
Synsat Technology- co-current & counter current operation in a single reactor
OATS- Olefinic alkylation of thiophenic sulfur- for gasoline with <10ppm S. Heavier alkylated S compunds removed separately
Z-SORB- Adsorptive removal of sulfur
Oxidative removal of sulfur
Bio-desulfurization

## Slide 98
GTL-Block flow diagram

## Slide 99
Vision of GTL barge production facility to produce ultra clean fuel- Utilization of stranded gas field
Finished products at the wellhead. The GTL barge provides a processing platform at or near the stranded gas reserve, which allows for finished products to be produced at the source.
GTL barge is a repeatable and modular concept – much like a floating, production, storage and offloading (FPSO) vessel

## Slide 100: Reactions under Supercritical Conditions

## Slide 101: Hydrogenation with Super Critical CO2
Hydrogen is infinitely miscible with scCO2 and therefore, eliminates the mass transport problems commonly associated with traditional solvent-based processing (Batch or Buss loop).
A wide range of substrates can be hydrogenated including alkenes, aldehydes, nitro compounds, ketones and oximes.
Reaction rates with heterogeneous catalysts are especially enhanced with increased selectivity and a high diffusivity/low viscosity environment which maximises mass transport
Supercritical fluid systems combine the mass transport properties of gases with the mass density of liquids. This results in increased reaction kinetics and, hence, high throughputs from a relatively
small reactor system.
Through the appropriate choice of reaction pressure, temperature, catalyst type, residence time and stoichiometry it is possible to achieve far higher degrees of selectivity than has been observed under
traditional reaction conditions.

## Slide 102
Figure 1.
Synthesis of Ethyl Cyclohexene under SC CO2 conditions
Thomas Swan& Co,UK-Swan-SCF®

## Slide 103
1.Chemical & Engg. News, 82 (43),p12, 2004
2. Continuous hydrogenation of organic compounds in supercritical fluids, MG. Hitzler &M.Poliakoff, Chem. Commun.1997,1667

## Slide 104: DEVELOPMENT OF CATALYSTS: MODERN APPROACHES

## Slide 105: DEVELOPMENT OF CATALYSTS: MODERN APPROACHES
COMBINATORIAL CATALYSIS
Systematic preparation, processing and testing of a number of formulations
Rapid library synthesis
Evaluation by high throughput techniques
Micro fabrication
Robotics
Automation & Instrumentation
Computational chemistry
Information management
Better understanding of catalytic functions
Trends & patterns of structure-activity correlations
Faster discovery of new formulations

## Slide 106
HIGH THROUGHPUT EVALUATION OF CATALYSTS
EVALUATION OF ACTIVITY, SELECTIVITY & LIFE FOR A
NUMBER OF CATALYST FORMULATIONS
NORMAL SCREENING OF ONE FORMULATION:
ACTIVITY & SELECTIVITY : ONE DAY
STABILITY/LIFE : 30 DAYS TO 90 DAYS
ONE FORMULATION/ONE REACTOR AT A TIME
SCREENING OF PROMISING FORMULATIONS THROUGH
HIGH THROUGHPUT EVALUATION TECHNIQUE
SIMULTANEOUS EVALUATION OF SEVERAL CATALYSTS
8 OR 80 REACTORS BEING USED SIMULTANEOUSLY
FAST ANALYTICAL TECHNIQUES FOR ANALYSIS OF FEED
& PRODUCTS BY IR THERMOGRAPHY/ QMS/TOF-MS

## Slide 107: Sustainable Chemistry
SUSTAINABILITY
Meeting the needs of the present generation without compromising the ability of the future generations to meet their own demands
SUSTAINABLE DEVELOPMENT
To ensure the viability of our world in the long run and create a harmonious balance between economic development preservation of eco-systems &improve quality of life
SUSTAINABLE CHEMISTRY
The chemistry that is eco-friendly, minimises waste generation and energy use and preferentially uses renewable raw materials such as agricultural products instead of fossil resources
INDUSTRIAL BIO TECHNOLOGY- White Bio-technology
Means of achieving sustainable development
Green Bio-technology- Agriculture oriented- GM
Red Bio-technology - Medical oriented

## Slide 108: Sustainable Chemistry
INDUSTRIAL BIOTECHNOLOGY
Application of modern bio-technology for industrial production of
chemicals & bio-energy using living cells and their enzymes, leading
to inherently clean processes with minimum waste generation &
energy use
SUSTAINABLE CHEMICALS
Inherently safe,pose no risk to human health & environment, low
acute toxicity, low persistency,no bio-accumulation
SUSTAINABLE PRODUCTION & PROCESSING
Best Available Techniques (BAT) & Best Environmental Practice
(BEP) to be adopted.
Responsible care as per Integrated Pollution Prevention & Control
(IPPC) guide lines to be followed with respect to:
Emission to air,water & land
Generation of waste Prevention of accidents
Use of raw materials Risk management auditing systems
Energy efficiency
Noise

## Slide 109: Sustainable Chemistry
SUSTAINABLE PRODUCTS
Effects on long term use
Properties suitable for reuse & recycling
Low resource demand in its production & use
Life cycle assessment
Sustainable chemistry as an innovative
new branch of science
is the challenge to
Scientists & Technologists

## Slide 110: CHEMICAL INDUSTRY: 2020 GOALS
Reduce catalyst discovery & process development cycle time from 5-10 to 3-5 yrs
Speed up development & commercial availability of tools for computer aided catalysis modeling
Decrease total process costs by 50%
Reduce development cycle time for new high performance products by 50%
Reduce wastes associated with catalyst use and manufacture by 50-75%
Develop low cost manufacturing techniques for catalysts
Reduce the cost of pilot plant scale-up by 30%
Reduce the cost of production of catalyst by 50%
Reduce the process down time due to catalyst failure/regeneration by 50%
Reduce the volume and cost of catalyst used in existing processses by 35%
BETTERCHEAPERFASTER SAFERCLEANER
TOWARDS SUSTAINABLE DEVELOPMENT