## Slide 1: Oganic-Inorganic Perovskites
New generation of photoactive materials
absorber in solar cells and significant progress towards improved efficiency, fabrication and scale up process.
organic inorganic perovskite materials in photovoltaics as well as photoelectrochemical applications

## Slide 2
power-conversion efficiency (PCE) of 22% for perovskite solar cells, similar to that of commercial crystalline silicon solar cells. (2009).
crystal structure, photophysical (optical-thermal properties) and surface morphology.
First basic unit of organometal trihalide perovskites (OTP) have been explored by H.L. Wells (1893), who already synthesized alkali-metal lead and tin halides
chemical formula CsPbX3 (X = Cl, Br or I) were analyzed after 64 years by the Danish scientist Christian Møller (1958).
After two decade, Dieter Weber (1978) replaced Cesium with methylammonium cations (CH3NH3+) and generated the first three-dimensional organic–inorganic hybrid perovskites.
In the 1990s, David B. Mitzi and his co-workers focused on perovskite crystal structure methylammonium lead halide, CH3NH3PbX3

## Slide 3
tolerance factor (t) and octahedral factor (μ)
{t = (RA+ RX )/(√2(RB+ RX)
= RB/RX
μ
0.81<t<1.11 and 0.44<μ<0.90
cubic perovskite structure
symmetric tetragonal or orthorhombic structures.

## Slide 5: Developments in organometal trihalide perovskites (OTP)
Since 2006 photovoltaic's with a DSSC based on CH3NH3PbBr3 by Miyasaka and colleagues from Toin University reported an efficiency of 2.2%. In 2009, replaced 'Br' by 'I' and ceased efficiency was 3.8%, while stability was poor. In 2011, Nam-Gyu Park and co-workers from Sungkyunkwan University (SKKU) were able to achieve stability with PCE upto 6.5%. Subsequently, Park, Grätzel and other colleagues focused on demerits of electrolytes, introduced solid state hole transporting medium (HTM). A spiro MeOTAD (2,2‘,7,7‘-tetrakis(N,N-di-p-methoxyphenylamine)-9,9‘-spirobifluorene) HTM was effectively used in solid state dye cell in which HTM solute was used within nanoporous TiO2. The HTM improves the stability with increase stability in PCE 9.7%. In mid 2012, Henry Snaith and co-workers from Oxford University simultaneously exploited spiro-MeOTAD and used mixed halide in perovskite structure for better stability.

## Slide 7
'OTP is a class of materials that has quickly become the rising star of the solar cell world and would enable production of hydrogen fuel using sunlight ' as said by Sam Lemonick

## Slide 8: Extremely optical absorption small effective mass of electron and hole dominant point defects – shallow levels grain boundaries

## Slide 10
Metal −organic framework (MOF) structure of [C(NH2)3]-Mn(HCOO)3.43In order to show the relationship with the halide perovskites, the oxygen atoms are drawn as red spheres in this figure; C, N, H, and Mn are black, sky blue, light pink, and cyan spheres respectively

## Slide 11
for the semiconducting
inorganic
halide perovskite CsAuI
3
,
wherein the Au disprortionates into +1 and +3 states; that is,
the compound can more speci
fi
cally be expressed as Cs
2
Au-
(I)Au(III)I
6
.
30
,
31
Interest in the mixed-valent metal halide
perovskites further follows from the theoretical prediction
32
of
superconductivity in CsTlX
3
, which features Tl
+
(6
s
2
) and Tl
3+
(6
s
0
) ions that are isoelectronic to Bi
3+
and Bi
5+
in BaBiO
3
.Ina
recent experimental work,
33
CsTlF
3
was prepared as a light
brown powder that adopts a double cubic perovskite
Fm
3
m
structure, whereas orange crystals of CsTlCl
3
were obtained in
two di
ff
erent polymorphs, a tetragonal
I
4/
m
and a cubic
Fm
3
m
phase. In all of these phases, charge ordering between Tl
+
and
Tl
3+
was con
fi
rmed to exist. Although resistivity was found to
decrease under pressure, no evidence of a phase transition to a
Tl
2+
(i.e., delocalized charge) state, which would be required for
obtaining a superconducting phase, has been observed so far. In
comparison to these inorganic systems, there are only a few
known organic
−
inorganic mixed-valent perovskites, all featur-
ing lower-dimensional or 3-D defect crystal structures (see
section 3
).
In addition to size and charge, there are also the details of the
bonding/coordination preferences for the metal ions involved,
which can impact the structural chemistry. For example, in the
related inorganic Cs
2
Au(I)Au(III)I
6
the primary bonding
around Au(I) and Au(III) can perhaps more accurately be
described as square planar for Au
3+
and linear for Au
1+
, with
long Au
···
I contacts nominally completing octahedral coordi-
nation.
31
In another example, the lone pair
s
2
electrons on B =
Tl
+
,Ge
2+
,Sn
2+
,Pb
2+
,Sb
3+
, and Bi
3+
may sterically interfere with
BX
6
octahedral coordination, leading to structural distortions of
the perovskite framework.
22
,
34
−
37
In the perovskite structure, a
stereochemically active lone pair (or
s
-orbital hybridization)
generally gives rise to a shift of the metal atom away from the
crystallographic center of the metal halide octahedra, resulting
in alternating long and short B-X bonds and the prospects of
ferroelectricity.
34
,
36
,
38
For organic
−
inorganic perovskites, the
directional hydrogen bonding of the organic cation can also
couple through intervening halogens to the steriochemically
active
s
2
electron pair, giving rise to a coordinated structural
distortion, as has been discussed for the low temperature phase
of CH
3
NH
3
SnBr
3
.
36
On the other hand, a number of transition
metal ions are also impacted by Jahn
−
Teller and related
distortions: for example, AMnO
3
(A = Pr, Nd, Dy, Tb, Ho, Er,
Y),
39
Cs
2
Au
2
Br
6
,
40
and KCuF
3
.
41
,
42
Given the substantial size,
charge, and chemistry constraints, there are only a limited
number of
“
A
”
,
“
B
”
, and
“
X
”
chemical combinations that can
yield a 3-D organic
−
inorganic perovskite.
Note that the perovskites based on metal halide frameworks
and organic cations are often referred to as
“
organometal
”
perovskites

a terminology that is misleading, since there are
no metal
−
carbon bonds or direct linkages between metals and
organic ligands. These structures can more accurately be
referred to as
“
organic-inorganic
”
or
“
hybrid
”
perovskites.
However, organic
−
inorganic perovskites with direct bonding
between a metal and an organic ligand do exist,
43
−
45
with
prototypical examples including [C(NH
2
)
3
]M(HCOO)
3
,
where M = Mn, Fe, Co, Ni, Cu, and Zn.
43
In this example
(
Figure 3
) the guanidinium cation occupies the
“
A
+
”
site in the
ABX
3
perovskite framework and the formato anion takes the
role of the X
−
anion (this time an organic anion). Examples of
analogous structures with the guanidinium cation replaced with
other organic amines are also known.
44
,
45
This family of
compounds provides a direct link between the traditional
organic
−
inorganic perovskites based on metal halides and
metal
−
organic frameworks or
“
MOFs
”
: a widely expanding
class of compounds with potential application in catalysis, gas
storage, puri
fi
cation, and separation.
46
,
47
3. LOWER-DIMENSIONAL ORGANIC
−
INORGANIC
PEROVSKITES
While the ABX
3
structure described above has fairly rigid
structural constraints, one can explore within a broader
extended family of lower-dimensional perovskites, which then
Table 1. E
ff
ective Radii of Molecular Cations and Anions
a
Cation
E
ff
ective radius
r
A,eff
(pm)
Ammonium [NH
4
]
+
146
Hydroxylammonium [H
3
NOH]
+
216
Methylammonium [CH
3
NH
3
]
+
217
Hydrazinium [H
3
N-NH
2
]
+
217
Azetidinium [(CH
2
)
3
NH
2
]
+
250
Formamidinium [NH
2
(CH)NH
2
]
+
253
Imidazolium [C
3
N
2
H
5
]
+
258
Dimethylammonium [(CH
3
)
2
NH
2
]
+
272
3-Pyrollinium [NC
4
H
8
]
+
272
Ethylammonium [C
2
H
5
NH
3
]
+
274
Guanidinium [C(NH
2
)
3
]
+
278
Tetramethylammonium [(CH
3
)
4
N]
+
292
Thiazolium [C
3
H
4
NS]
+
320
Piperazinium [C
4
H
12
N
2
]
2+
322
b
Tropylium [C
7
H
7
]+
333
Dabconium [C
6
H
14
N
2
]
2+
339
b
Anion
E
ff
ective radius
r
X,eff
(pm)
Fluoride
129
Chloride
181
Bromide
196
Iodide I
−
220
Formate HCOO
−
136
a
Adapted from ref
22
with permission from The Royal Society of
Chemistry.
b
Radii calculated from the single crystal X-ray data.
26
Figure 3.
Metal
−
organic framework (MOF) structure of [C(NH
2
)
3
]-
Mn(HCOO)
3
.
43
In order to show the relationship with the halide
perovskites, the oxygen atoms are drawn as red spheres in this
fi
gure;
C, N, H, and Mn are black, sky blue, light pink, and cyan spheres,
respectively.
Chemical Reviews
Review
DOI:
10.1021/acs.chemrev.5b00715
Chem.Rev.
2016, 116, 4558
−
4596
4560
allows for a remarkable structural tunability, i.e., from the
parent 3-D structure, based upon corner-shared BX
6
octahedra,
all the way down to isolated, zero-dimensional (0-D) BX
6
octahedral clusters.
9
,
10
Note that the dimensionality discussed
here refers to the connectivity of the corner-sharing BX
6
octahedra in the crystal structure, as conceptually excised
from the 3-D parent compound (
Figure 4
). As the perovskite
structure is cut into slices, the size restrictions, as outlined by
the tolerance factor for the 3-D structures, are gradually lifted.
For example, in two-dimensional (2-D) layered derivatives of
the perovskite structure, there are no known restrictions for the
interlayer
“
A
”
cation length and, in the 0-D derivatives, size
restrictions are not applicable altogether, as MX
6
octahedra are
isolated and can readily shift in relative position. This structural
fl
exibility and tunability of the dimensionality provide a rich and
fertile
“
playground
”
for the preparation of interesting crystal
structures with varying physical properties.
While the size restrictions may be relaxed for the lower
dimensional perovskites, there are still other important
parameters to consider for the successful design and synthesis
of a targeted perovskite-derived structure.
10
The organic cation
“
A
”
must contain terminal functional groups that can ionically
interact with the anionic inorganic substructure, but without the
rest of the organic molecule interfering with the inorganic
components
“
B
”
and
“
X
”
. Most of the known layered (2-D)
perovskite derivatives feature mono- or diammonium cations,
yielding the general formulas of (RNH
3
)
2
BX
4
or (NH
3
RNH
3
)-
BX
4
, where here
“
R
”
represents an organic functional group.
The presence of ammonium cations leads to various hydrogen
bonding schemes with the anionic substructure, which are
important for determining the orientation and conformation of
the interlayer organic cations (see ref
10
for details).
Depending on the choice of metal, the inorganic framework
can be more or less rigid, which also in
fl
uences the hydrogen
bonding schemes. For example, perovskites containing Jahn
−
TellerionssuchasCu
2+
feature highly distorted CuX
6
octahedra that enable greater
fl
exibility for the interaction
with interlayer organic cations.
For the diverse family of 2-D perovskite frameworks,
although there is no de
fi
nitive restriction for the length of
the interlayer organic cations, there is a restriction for the
width, which must
fi
t into an area de
fi
ned by the terminal
halides from four adjacent corner-sharing octahedra. This is
important both from the perspective of hydrogen bonding and
electron counting schemes. The charge balance requirement
dictates the presence of a certain concentration of cations, and
organic molecules that are too large (in terms of their width)
may cause steric hindrance with adjacent organic molecules,
which in turn would render impossible
fi
tting this number of
cations into the targeted perovskite framework. However, if
they are too narrow

i.e., much smaller than the area provided
by the inorganic substructure

the structure can accommodate
by allowing organic molecules to tilt. In summary, both the
organic cations and the anionic inorganic framework have
templating in
fl
uence on each other, allowing a certain degree of
control over the
fi
nal structures and properties.
As mentioned above, lower-dimensional derivatives of the
perovskite structure can be obtained by making slices along
di
ff
erent crystallographic directions in the parent compounds.
The choice of the organic cation(s) and the reaction
stoichiometry are among the most in
fl
uential parameters on
the orientation of the resultant inorganic frameworks. It is
important to note that the dimensional reduction discussed
here has signi
fi
cant impact on the physical properties of the
compounds. For example, the band gap of the compounds
typically increases as the dimensionality of the structure is
lowered. This is best illustrated by the example of (C
4
H
9
NH
3
)
2
-
(CH
3
NH
3
)
n
−
1
Sn
n
I
3
n
+1
compounds, for which the parent 3-D
perovskite (
n
→
∞
)CH
3
NH
3
SnI
3
is a dopable small band gap
semiconductor (even yielding semimetallic character), whereas
the
n
= 1 compound (C
4
H
9
NH
3
)
2
SnI
4
is a large band gap
semiconductor.
48
In simple terms, this can be rationalized by
Figure 4.
Schematic representation of the derivation of the lower dimensional organic
−
inorganic perovskites (lower sections) from di
ff
erent cuts of
the 3-D perovskite structure (top sections). (a) The family of
⟨
100
⟩
-oriented layered perovskites with a general formula of (RNH
3
)
2
A
n
−
1
B
n
X
3
n
+1
are
obtained by taking
n
layers from along the
⟨
100
⟩
direction of the parent structure. (b) Cuts along the
⟨
110
⟩
direction of the 3-D perovskite structure
provide the
⟨
110
⟩
-oriented family, A
′
2
A
m
B
m
X
3
m
+2
, which includes 1-D chain (
m
= 1) and 2-D layered (
m
> 1) members. (c) The
⟨
111
⟩
-oriented
family, A
′
2
A
q
‑
1
B
q
X
3
q
+3
, is formed by excising along the
⟨
111
⟩
direction of the 3-D parent, and features 0-D isolated cluster (
q
= 1) and 2-D layered (
q
> 1) members. In each of these layered structures, the perovskite framework is separated by a layer of typically larger organic cations.
Chemical Reviews
Review
DOI:
10.1021/acs.chemrev.5b00715
Chem.Rev.
2016, 116, 4558
−
4596
4561
the fact that the dimensionality of the inorganic framework is
reduced by removing the metal
“
B
”
, which results in an increase
in purely ionic interactions between
“
A
”
and
“
X
”
,two
components with a very di
ff
erent set of electronegativities
and, consequently, leading to a larger band gap. In the following
subsections, we will review some of the recent reports on lower-
dimensional perovskite derivatives that feature di
ff
erent cuts
from the 3-D structure, including the well-known
⟨
100
⟩
-,
⟨
110
⟩
-, and
⟨
111
⟩
-oriented families as well as more exotic
possibilities.
3.1.
⟨
100
⟩
-Oriented Perovskites
The
⟨
100
⟩
-oriented perovskites are obtained by the ordered
removal of the B-component from the inorganic framework
along
⟨
100
⟩
in the ABX
3
structure. Alternatively, they can be
thought of as intergrowth compounds with a general formula of
(RNH
3
)
2
A
n
−
1
B
n
X
3
n
+1
, formed from the two end members: i.e.,
the 3-D-parent ABX
3
and 2-D-layered (RNH
3
)
2
BX
4
. The
⟨
100
⟩
-oriented perovskites currently represent the richest
subgroup of the perovskite derivative family, likely in part
because the coordination of the interlayer RNH
3
+
cations is
most readily accommodated in these structures. The inter-
actions between organic cations and the inorganic substructure
in general, and the hydrogen bonding schemes in particular, are
important in the perovskite-derivative structures. The majority
of known hybrid perovskites feature primary mono- or
diammonium cations. An interesting example involves long
chain alkyl
“
R
”
groups (
Figure 5
). Subject to the constraint of
lateral restrictions imposed by the metal halide layers, these can
provide a useful model sys
tem for the study of lipid
bilayers.
49
−
51
The advantageous feature of the hybrid perov-
skites is that, unlike free lipid bilayers, since the organic cations
are anchored to the inorganic perovskite lattice, the phase
transitions are solid-to-solid, which allows investigations of
these transitions through a variety of spectroscopic techniques.
Depending on the length of the organic chain and the nature of
the B-metal cation, the temperature and the order of the phase
transitions observed in hybrid perovskites can be di
ff
erent.
49
In
addition to the regular dynamic rotational disordering of the
ammonium functional group, the hybrid perovskites containing
long chain organic cations undergo
“
melting transitions
”
as a
function of temperature, which are characterized by an
increased conformational disorder of the methylene units of
the alkyl groups.
50
This large increase in gauche conformational
disorder results in the nonuniform distribution of the
orientation of the chains, and consequently, in the increase of
the interlayer lattice parameter.
51
Raman spectra of
(C
n
H
2
n
+1
NH
3
)
2
PbI
4
(
n
= 12, 16 and 18) above the melting
transition are noted to be similar to that of
n
-alkanes in the
molten state. These spectra support the idea that, above the
melting transition, the alkyl chains of the bilayers are liquid-like
in two dimensions between adjacent inorganic layers.
50
Molecular dynamics (MD) simulations were used to success-
fully reproduce the experimental data, except for the detailed
transition temperatures, for (C
n
H
2
n
+1
NH
3
)
2
PbI
4
(
n
= 12, 14, 16
and 18).
51
Snapshots of the simulated structures above and
below the melting transition for (C
18
H
37
NH
3
)
2
PbI
4
are
provided in
Figure 5
.
Recently, several examples of perovskites containing non-
primary ammonium cations have also been prepared. In
(C
6
H
8
N
4
)BI
4
(B = Pb, Sn),
52
for example, the inorganic
Figure 5.
Structures of the organic cation bilayers in (C
18
H
37
NH
3
)
2
PbI
4
, obtained using molecular dynamics simulations, below (142
°
C) and above
(272
°
C) the melting transition of
T
m
= 182
°
C.
51
Reprinted with permission from ref
51
. Copyright 2010 American Chemical Society.
Figure 6.
Combined skeletal (top) and polyhedral (bottom, shaded) representation of the crystal structure of (C
6
H
8
N
4
)PbI
4
, which features
[PbI
4
]
2
−
sheets that are separated by a monolayer of aromatic biimidazolium (C
6
H
8
N
4
)
2+
dications.
52
In the right half of the
fi
gure, the structure of a
single inorganic [PbI
4
]
2
−
sheet is shown, viewed along the
c
-axis (i.e., top down), with the organic cations removed for clarity. The inorganic layers
are remarkably
fl
at, with a Pb
−
I
−
Pb angle of
β
= 174
°
, and contain regular PbI
6
octahedra with the I
−
Pb
−
I angles of 87.70
−
94.83
°
, and the out-of-
plane distortion of
α
=2
°
.
Chemical Reviews
Review
DOI:
10.1021/acs.chemrev.5b00715
Chem.Rev.
2016, 116, 4558
−
4596
4562
Schematic representation of the derivation of the lower dimensional organic−inorganic perovskites (lower sections) from different cuts of the 3-D perovskite structure (top sections). (a) The family of ⟨100⟩-oriented layered perovskites with a general formula of (RNH3)2An−1BnX3n+1 are obtained by taking n layers from along the ⟨100⟩ direction of the parent structure. (b) Cuts along the ⟨110⟩ direction of the 3-D perovskite structure provide the ⟨110⟩-oriented family, A′2AmBmX3m+2, which includes 1-D chain (m = 1) and 2-D layered (m > 1) members. (c) The ⟨111⟩-oriented family, A′2Aq‑1BqX3q+3, is formed by excising along the ⟨111⟩ direction of the 3-D parent, and features 0-D isolated cluster (q = 1) and 2-D layered (q > 1) members. In each of these layered structures, the perovskite framework is separated by a layer of typically larger organic cations.

## Slide 12
Structures of the organic cation bilayers in (C18H37NH3)2PbI4, obtained using molecular dynamics simulations, below (142 °C) and above (272 °C) the melting transition of Tm = 182 °C.51 Reprinted with permission from ref 51

## Slide 15
(a) Electronic band structure of MAPbI3 , adopted from density-functional theory calculations presented in References 40 and 45. Colored upward-pointing arrows represent allowed photoinduced electronic transitions. The lowest CB (CB1) is the spin-orbit SO band, whereas the higher-lying CB2 comprises HE and LE states, according to References 40 and 45. The dashed blue arrows indicate the partly dipole-allowed transitions VB2 → CB1 and VB1 → CB2 at the R point. (b) Absorption spectrum showing that a continuum of electronic transitions between the R and M valleys leads to strong absorption across the visible range (46). Relaxation toward the R valley gives rise to a photoluminescence peak near 1.6 eV arising from CBM1 → VBM1 transitions at the R point. Abbreviations: CB, conduction band; CBM, conduction band minimum; HE, heavy electron; LE, light electron; SO, split-off; VB, valence band; VBM, valence band maximum.

## Slide 16
Schematic diagram indicating recombination mechanisms active in organic-inorganic metal halide perovskites. (a) Trap-assisted recombination is a monomolecular process involving the capture of either an electron (as shown) or a hole in a specific trap state (e.g., defect). (b) Bimolecular recombination may occur between electrons and holes, from either the relaxed state (CBM → VBM) or states higher in the band. (c) Auger recombination is a higher-order process involving at least three particles. The energy of an electron (or hole) is here transferred to another electron (or hole) to allow nonradiative recombination with a hole (or electron). As indicated, all processes have to satisfy energy and momentum conservation. Abbreviations: CB, conduction band; CBM, conduction band minimum; VB, valence band; VBM, valence band maximum.

## Slide 18
SUMMARY POINTS
1.Hybrid organic-inorganic metal halide perovskites exhibit interesting structure-property relationships deriving from their propensity to undergo structural transformations with relative ease.
2.The exciton binding energy Eb appears to be a function of temperature as a result of the strong temperature dependence of the dielectric function. At room temperature, Eb is in the range of a few milli-electron volts to at most a few tens of milli-electron volts, in accordance with the presence of a free-charge-carrier population.
3.Charge-carrier relaxation dynamics within the first few picoseconds after excitation are marked by thermalization, cooling, and many-body effects. It remains to be explored whether extended hot charge-carrier phases can be utilized in photovoltaic devices that exceed the Shockley-Queisser limit.
4.Trap-assisted (monomolecular) charge-carrier recombination is mostly nonradiative and highly specific to material processing, yielding associated lifetimes from nano- to microseconds. Traps in hybrid lead halide perovskites appear to be mostly shallow (approximately tens of milli-electron volts), arising, for example, from elemental metal, halide, or organic vacancies, and may be present in higher density near interfaces and grain boundaries.
5.Bimolecular charge-carrier recombination is predominantly radiative and exhibits rate constants that defy the Langevin limit by many orders of magnitude.
6.Nonradiative Auger recombination is significant for charge-carrier densities corresponding to the threshold for amplified spontaneous emission. Rate constants show a strong specificity to crystal structure, opening the possibility for the design of materials with low Auger rates from first-principles calculations.

## Slide 19
In summary, organic-inorganic metal halide perovskites have proven to be a fascinating material system to investigate. Few materials show such inherent flexibility in terms of compositional and structural modification, yet allow for excellent optoelectronic properties, including high charge-carrier mobilities, strong optical absorption, and low trap-assisted recombination rates. Whether perovskite photovoltaic cells will become competitors to current silicon technology, the lessons learned from investigating their photophysics will serve as highly valuable guidelines on how to design effective light-harvesting and light-emitting materials.

## Slide 20
Reproduced from Chem.Soc., 2025,6,3430

## Slide 21
Reproduced from Chem.Soc., 2025,6,3430

## Slide 22
Reproduced from Chem.Soc., 2025,6,3430;supplement

## Slide 26
Figure 2 Electronic structure and closely related physical properties of HOIPs
Brenner. et al. (2016) Hybrid organic–inorganic perovskites: low-cost semiconductors with intriguing charge-transport properties
Nat. Rev. Mater. doi:10.1038/natrevmats.2015.7
Panel b adapted with permission from REF. 49, American Chemical Society. Panel c from REF. 63, Nature Publishing Group. Panel d adapted with permission from REF. 31, Royal Society of Chemistry. Panel e adapted with permission from REF. 74, American Chemical Society. Panel f adapted with permission from REF. 76, American Chemical Society