## Slide 1
Manoj M
Division for Research in Advanced Materials Department of Physics
Cochin University of Science and Technology
Supervising guide: Prof S Jayalekshmi
Pre-Synopsis seminar on
Investigations on carbonaceous materials as electrodes for the next generation electrochemical energy storage device applications.

## Slide 2: Contents
1
Introduction
2
Characterization tools and techniques
3
Biomass-derived, activated carbon-sulfur composite cathode with a bifunctional interlayer of functionalized carbon nanotubes for lithium-sulfur cells.
4
Sulfur-polyaniline coated mesoporous carbon composite in combination with carbon nanotubes interlayer as a superior cathode assembly for high capacity lithium-sulfur cells.
5
Polyaniline–graphene oxide based ordered nanocomposite electrodes for high-performance supercapacitor applications.
6
Mn3O4-mesoporous carbon composite as an improved anode material for rechargeable lithium ion cells.
7
A Li-ion full cell using LiFePO4 cathode and Mn3O4-mesoporous carbon anode
8
Conclusions and future outlook
9
Acknowledgements

## Slide 3
Chart: 
| Renewables 3% | Hydroelectric 7% | Nuclear Plants 4% | Fossil Fuels 86%
Global Energy Consumption | 3 | 7 | 4 | 86
Transportation
Industry
Commercial and Residential
Electricity
Energy Consumption
by Sectors
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 4
Greenhouse gas emissions
Land pollution and waste generation
Acid Rain
Oil Spills
Adverse Effects of Non-Renewable Resources
Motivation
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 5: Why Energy Storage?
Need of cleaner and renewable energy sources
Move Fast
Renewable energy output is intermittent since it is affected by weather conditions.
It makes the development of advanced energy storage systems mandatory.
Store energy when it is available in excess and release back to grid on demand.
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: The amount of wind power around the world has grown by an astounding 10x over the last 11 years
In 2016 world consumed 3x more wind energy than in 2010
The solar market has exploded, surging by an incredible 100x in just 13 years
10x more solar energy in 2016 than in 2010

## Slide 6
BATTERY and SUPERCAPACITOR
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 7: History of batteries
The commercialization of Li-ion battery in 1991 by Sony
Leclanche ́ cell
Lead-acid cell
Nickel-Cadmium Cell
The invention of Alessendro Volta cell in 1800
Stack of zinc and copper discs separated
by cardboard soaked in salt water (Electrolyte)
The price of Li-ion battery dropped by roughly a factor of 10 between 1991 and 2005
Li-ion battery market is expected to reach 68.97 Billion USD, globally, by 2022
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: The history of batteries run from the invention of Alessendro Volta cell
in 1800 to the commercialization of Li-ion battery in 1992, via the well-known
Leclanche ́ cell, lead-acid battery, nickel-cadmium accumulator and numerous other
systems.
The price of small lithium-ion batteries dropped by roughly a factor of 10 between 1991 and 2005

## Slide 8
Portable Electronics
Transportation
Applications of Li ion batteries
Batteries comparison
Coin cells
AA
AAA
C
D
9V
Laptop
Powerbank
Trimmer
Can be charged faster
Last longer
High energy density
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: Dominating portable electronic market owing to its lightweight and compactness
Compared with traditional battery technology, lithium-ion batteries charge faster, last longer and have a higher power density for more battery life in a lighter package.

## Slide 9
Anode (Negative Electrode)
Graphite, Silicon
Cathode (Positive Electrode)
LiCoO2, LiMn2O4, LiFePO4
Electrolyte: Example: Lithium hexafluorophosphate
Main components of batteries
Transport ions from the anode to the cathode or vice-versa
Porous membrane which is a good electronic insulator
Keeps positive and negative electrodes apart to prevent electrical short circuits.
Separator: Example: Polypropylene (Celgard)
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: Keep positive and negative electrodes apart to prevent electrical short circuits and, at the same time allow rapid transport of ionic charge
Commercially available Li-ion cells use polyolefin as a separator. This material has excellent mechanical properties, good chemical stability and is low-cost. A polyolefin is a class of polymer that is produced from olefin by polymerizing olefin ethylene. Ethylene comes from a petrochemical source; polyolefin is made from polyethylene, polypropylene or laminates of both materials. The Li-ion separator must be permeable and the pore size ranges from 30 to 100nm.

## Slide 10
Working of Li ion batteries
Imagine a never ending rally
Lithium ion is as light as a shuttle cork
Both electrodes allow lithium ions to move in and out of their structures
Intercalation
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: Both electrodes allow lithium ions to move in and out of their structures with a process called insertion (intercalation)

## Slide 11: New Energy Storage Systems
The Li-ion technology, though highly advanced, faces limitations when applied to electric vehicles
Comparison of theoretical gravimetric/volumetric energy densities of Li-ion (Graphite/LiCoO2) and Li-S batteries
Theoretical energy density 5 times greater than Li-ion
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: Li-ion battery dominated the portable electronics market
The conventional graphite/LiCoO2 even fully developed still far behind the requirement of electric vehicles.

## Slide 12: Advantages of Li-S batteries
Eco-friendly
Lightweight
Cost Effectiveness
Full discharge
Maintenance free
Temperature and Pressure tolerance
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 13: Working of Li-S batteries
S
Li
Li
Sulfur can host two ions of lithium
Co
Li
Compared to one in Li-ion technology
Lithium interacts directly with sulfur
Discharge
Charge
Anode : Li Li+ + e-
Cathode : S8 + 16Li+ + 16e- 8Li2S
Anode : Li+ + e- Li+
Cathode : 8Li2S S8 + 16Li+ + 16e-
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 14: Mechanism
Charge/Discharge process is more complicated
Sulfur becomes lithiated during discharge process to form polysulfide species
Long-chain lithium polysulfides
S8 Li2S8 Li2S6 Li2S4 Li2S2 Li2S
Short-chain lithium polysulfides
Contributes 25% of the theoretical capacity of S
Contributes 75% of the theoretical capacity of S
The opposite process occurs during charging , although the intermediate species might be different.
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 15: Major challenges
Dissolution of intermediate lithium polysulfide species in the electrolyte
Long-chain lithium polysulfide species (Li2S4 to Li2S8) dissolve readily in the electrolyte. This leads to continuous loss of the active material,sulfur.
Low conductivity of sulfur and lithium sulfide
The insulating nature of sulfur and lithium sulfide, both electronically and ionically, results in poor utilization of the active material.
Polysulfide shuttle effect
The higher-order polysulfides migrate towards the anode, react with the lithium metal, get reduced to lower-order polysulfides, migrate back to the cathode, form higher-order polysulfides again, and so on.
How do they have adverse effects?
Internal shorting
Self-discharging
Low Coulombic efficiency
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 16: Supercapacitors
Supercapacitors (SC’s) are energy storage systems having similarities with both batteries and conventional capacitors.
EDLC
Pseudo-capacitor
Electrochemical capacitors
Electrochemical double layer capacitors (EDLC)
(non-Faradaic)
Pseudo–capacitors
(Faradaic)
Hybrid capacitors
EDLC+Pseudo–capacitors
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 17
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 18
Carbon
C
Amorphous carbon
Diamond
Graphite
Graphene
Carbon nanotube
Fullerene
Carbon is the basic building block of the cells in the body.
Carbon forms about 18% of the human body constituents
Tunable electrical and optical properties
Economically viable
Environmentally benign
They have transformed the electronics industry and revolutionized the energy scenario
Graphene Oxide
Mesoporous Carbon
Activated Carbon
Carbon nanotubes
Carbonaceous materials
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: Transformed the electronics industry and energy storage devices.

## Slide 19: Chapter 2
Characterization tools and techniques
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 20: Characterization Tools
Structural, morphological and thermal characterizations
XRD (X-ray diffraction)
Micro-Raman Spectroscopy
FTIR (Fourier Transform Infra-red) Spectroscopy
FE-SEM (Scanning Electron Microscopy)
HR-TEM (High Resolution Transmission Electron Microscopy)
EDX (Energy Dispersive X-ray) analysis.
TGA (Thermo Gravimetric Analysis)
Electrochemical Analysis
Cyclic Voltammetry
Galvanometric charge - discharge studies
Impedance spectroscopy
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 21
Manufacturing Process
Material
Electrode Manufacturing
Slurry Mixing
Coating
Drying
Cutting
Active Material (80%)
Conductive Agent (10%)
Solvents
Binder (10%)
Al foil/Cu foil
Solvents
Cell Manufacturing Process
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
10-16 mm

## Slide 22
Manufacturing Process
Material
Cell Assembly
Stacking
Sealing
Electrolyte
Separator
Cell Manufacturing Process
Cell testing
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: Test cells were assembled in a glove box with moisture content less than 5ppm, using Li metal as anode and LiPF6 in organic solvents as the electrolyte.

## Slide 23: Terminology used in electrochemical technology
Specific capacitance :
C-rate :
Coulombic efficiency :
Specific charge :
The charge obtained in one discharge cycle from unit mass of the active material of the cell. Specific charge capacity is expressed in mA h g-1
The ability of a supercapacitor cell to store electric charge for a unit mass of the active material and is expressed in F g-1
The duration of one full charge or discharge of a cell and expressed in h-1.
Ratio of energy output on discharge to the input energy upon charging of a rechargeable cell.
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 24: Chapter 3
Biomass-derived, activated carbon-sulfur composite cathode with a bifunctional interlayer of functionalized carbon nanotubes for lithium-sulfur cells.
Under review in Journal of Colloids and Interface Science
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 25: Introduction
  Promising candidate for high performance Li-S cells.
  Low-cost and the availability of easy processing techniques (biomass sources such as jackfruit, coconut shell, sugarcane and rice husk).
  Adjustable surface properties.
The coconut shell derived carbons dominate the field due to their natural abundance and the desirable electrochemical properties.
The activation processes also play a crucial role in determining the performance of the electro active carbon materials.
Activated carbon (AC).
Activated carbon sulfur composite (ACS)-Cathode
Acid functionalized CNTs interlayer
Li-S cells with good performance characteristics
High theoretical specific capacity of 1675 mA h g-1
Low electrical conductivity.
Sulfur.
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 26: Synthesis
Coconut shell derived steam activated carbon (CSC)
Washed with 5 vol % NaOH, distilled water and dried at 110 ℃ for 12 hours.
Washed with HF (1.2 M) and then with distilled water until a neutral pH was obtained and dried at 110 ℃ for 12 hours.
Washed with distilled water and dried overnight at 110 ºC.
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 27: Synthesis of free-standing and flexible film of acid-functionalized carbon nanotubes (CNTF interlayer).
Synthesis of acid washed activated carbon-sulfur (ACS) composite.
PVDF in NMP solution
Ultra-sonicated for 2 hours
Pristine CNTs
H2SO4 : HNO3 (6M)
in 3:1 volume ratio
Refluxed at 120 ℃ for 12 hours
Acid-functionalized CNTs
Dried at 60 ℃ in vacuum oven
Ultra-sonicated for 3 hours
Sulfur
Activated carbon
+
Dispersed in acetone
Ultra-sonicated (3 hrs) in an ice bath and then stirred (3 hrs)
Solvothermal process at 120 ℃ for 4 hours
ACS composite
Sulfur : AC
80 : 20
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
0.2 mm
Notes: The commercially obtained sulfur and the synthesized activated carbon were mixed in a weight ratio of 8:2 in 30 ml of acetone
Explain why IL?

## Slide 28: Structural and morphological characterization
X- Ray diffraction patterns of AC, Sulfur and ACS composite
Micro Raman spectra of pristine and functionalized CNTs
Characteristics Raman peaks of CNTs: D band: 1346 cm-1, G band: 1574 cm-1, and G' band : 2689 cm-1.
After functionalization, the intensity ratio ID/IG is found to increase to 0.82 from 0.62
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
(222)
(222)
(313)
Notes: The dominant peak at 23.1 corresponds to the 222 plane of orthorhombic fddd phase of sulfur.
After functionalization, the intensity ratio ID/IG is found to increase to 0.82 from 0.62 which implies that the acid functionalization brings about structural distortions in the CNTs network [53]. The acid treatment also facilitates the good dispersion of the CNTs in NMP solution with reduced agglomeration [54].

## Slide 29
Peaks at 153 cm-1, 219 cm-1, and 473 cm-1 correspond to those of orthorhombic sulfur.
  In ACS composite, slight shift in D and G bands is also observed
Micro Raman spectra of sulfur, AC and ACS composite
  ID/IG: 1.16
  ID/IG: 1.11
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
153 cm-1
219 cm-1
473 cm-1
Notes: The 153 cm-1 peak is assigned to E2 symmetry interactions, and the 219 cm-1 and 473 cm-1 peaks are assigned to A1 vibration modes
There are two typical Raman peaks in the spectrum of AC shown in figure 5(b), located at 1340 cm-1 and 1590 cm-1 which are related to the D-band and G-band respectively and the intensity ratio ID/IG of AC is observed to be 1.16. The D band corresponds to the defects in the carbon structure and the G band is linked to the vibration of sp2 carbon atoms [56].
The Raman spectrum of the ACS composite (figure 5(c)) displays the significant peaks of sulfur, while those of AC are not visible because of the presence of the high-intensity sulfur peaks in the composite. The distinct scan of the ACS composite in the range 1000-2000 cm-1 as depicted in figure 5(d) reveals the characteristics peaks of AC.
After the reaction of AC with sulfur the intensity ratio ID/IG is found to decrease to 1.11, and slight changes in the positions of D and G bands are also observed in the spectrum of the composite which can be associated with the interaction of sulfur with carbon during the solvothermal process

## Slide 30
S~80 wt.%
FESEM images of AC (a-b) and ACS (c-d)
EDX of ACS composite
TGA of ACS composite
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: The XRD pattern of AC shows no crystalline peaks which is an indication of its amorphous nature
After functionalization, the intensity ratio ID/IG is found to increase to 0.82 from 0.62 which implies that the acid functionalization brings about structural distortions in the CNTs network [53]. The acid treatment also facilitates the good dispersion of the CNTs in NMP solution with reduced agglomeration [54].

## Slide 31: Cell fabrication
Li-S test cells : Swagelok type.
Cathode : ACS composite,
Anode : Li foil,
Separator : Celgard
Electrolyte : 1M lithium perchlorate in a mixed solvent of 1, 3 dioxolane (DOL) and 1, 2 dimethoxymethane (DME) at a volume ratio of 1:1 including 0.5 M LiNO3 .
Voltage window : 1.5 V – 3 V
Sulfur loading ~1.3 mg cm-2.
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: The ACS composite cathode electrodes for Li-S cells were prepared from the slurry containing 80 wt. % ACS composite, 10 wt. % of acetylene black and 10 wt. % of polyvinylidene difluoride (PVDF) in N-methyl pyrrolidinone (NMP) solvent as explained earlier. The homogeneous slurry was then spray coated on an aluminium foil and after drying at 60 °C under vacuum for 12 hours, the cathode electrodes were cut into circular disks of 10 mm in diameter with a sulfur loading of approximately 1.3 mg cm-2. Using stainless steel Swagelok cells, Li-S cells were assembled by stacking ACS composite as the cathode active material, Li foil as the anode and Celgard as the separator in an argon-filled glove box,with 1 M lithium perchlorate in a mixed solvent of 1, 3-dioxolane (DOL) and 1, 2-dimethoxymethane (DME) at a volume ratio of 1:1 including 0.5 M LiNO3 as an electrolyte additive, as the electrolyte[42,43]. The synthesized CNTF interlayer was placed between the separator and the ACS cathode and the amount of electrolyte added to each cell was 70 μl. The cyclic voltammetry (CV) test was carried out at a scan rate of 0.1 mV s-1 in the voltage window of 1.5-3 V and the electrochemical impedance spectroscopy (EIS) studies in the frequency range between 1 MHz and 10 mHz, using Bio-Logic SP300 workstation. The test cells were charge-discharge cycled between 1.5 and 3 V at various C-rates (1C=1650 mA g-1) using the 8 channel battery analyzer (MTI Corporation-USA) at room temperature

## Slide 32: Electrochemical studies
Cyclic voltammograms (a) With out CNT interlayer (b) With CNT interlayer at 0.1mV S-1
Anodic peak
~2.50 V
:Conversion of Li2S2/Li2S to polysulfides and sulfur
Cathodic peak
~2.3 V
: Reduction of sulfur to soluble higher order lithium polysulfides (Li2Sn, 4 ≤ n ≤8)
~2.0 V
: Reduction of the higher order lithium polysulfides to the lower order insoluble Li2S2 and ultimately to Li2S
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: The ACS composite cathode electrodes for Li-S cells were prepared from the slurry containing 80 wt. % ACS composite, 10 wt. % of acetylene black and 10 wt. % of polyvinylidene difluoride (PVDF) in N-methyl pyrrolidinone (NMP) solvent as explained earlier. The homogeneous slurry was then spray coated on an aluminium foil and after drying at 60 °C under vacuum for 12 hours, the cathode electrodes were cut into circular disks of 10 mm in diameter with a sulfur loading of approximately 1.3 mg cm-2. Using stainless steel Swagelok cells, Li-S cells were assembled by stacking ACS composite as the cathode active material, Li foil as the anode and Celgard as the separator in an argon-filled glove box,with 1 M lithium perchlorate in a mixed solvent of 1, 3-dioxolane (DOL) and 1, 2-dimethoxymethane (DME) at a volume ratio of 1:1 including 0.5 M LiNO3 as an electrolyte additive, as the electrolyte[42,43]. The synthesized CNTF interlayer was placed between the separator and the ACS cathode and the amount of electrolyte added to each cell was 70 μl. The cyclic voltammetry (CV) test was carried out at a scan rate of 0.1 mV s-1 in the voltage window of 1.5-3 V and the electrochemical impedance spectroscopy (EIS) studies in the frequency range between 1 MHz and 10 mHz, using Bio-Logic SP300 workstation. The test cells were charge-discharge cycled between 1.5 and 3 V at various C-rates (1C=1650 mA g-1) using the 8 channel battery analyzer (MTI Corporation-USA) at room temperature

## Slide 33
Initial Charge-Discharge profiles of Li-S cells (a) With out CNTF interlayer (b) With CNTF interlayer
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: The ACS composite cathode electrodes for Li-S cells were prepared from the slurry containing 80 wt. % ACS composite, 10 wt. % of acetylene black and 10 wt. % of polyvinylidene difluoride (PVDF) in N-methyl pyrrolidinone (NMP) solvent as explained earlier. The homogeneous slurry was then spray coated on an aluminium foil and after drying at 60 °C under vacuum for 12 hours, the cathode electrodes were cut into circular disks of 10 mm in diameter with a sulfur loading of approximately 1.3 mg cm-2. Using stainless steel Swagelok cells, Li-S cells were assembled by stacking ACS composite as the cathode active material, Li foil as the anode and Celgard as the separator in an argon-filled glove box,with 1 M lithium perchlorate in a mixed solvent of 1, 3-dioxolane (DOL) and 1, 2-dimethoxymethane (DME) at a volume ratio of 1:1 including 0.5 M LiNO3 as an electrolyte additive, as the electrolyte[42,43]. The synthesized CNTF interlayer was placed between the separator and the ACS cathode and the amount of electrolyte added to each cell was 70 μl. The cyclic voltammetry (CV) test was carried out at a scan rate of 0.1 mV s-1 in the voltage window of 1.5-3 V and the electrochemical impedance spectroscopy (EIS) studies in the frequency range between 1 MHz and 10 mHz, using Bio-Logic SP300 workstation. The test cells were charge-discharge cycled between 1.5 and 3 V at various C-rates (1C=1650 mA g-1) using the 8 channel battery analyzer (MTI Corporation-USA) at room temperature

## Slide 34
Specific capacity : 384 mA h g-1 at 1 C after 200 cycles.
Capacity retention : 71% at 1 C
Coulombic efficiency : 97% at 1 C
Rate capability of the Li-S cells: Capacity of 976 mA h g-1 was obtained after the C-rate was reverted back to 0.1 C from 1 C.
Li-S cells with the interlayer
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 35: Role of CNTF interlayer
Before cycling
After cycling
(a) Conventional and (b) modified structure of Li-S cell
Trapped Polysulfides
Importance of the porosity of CNTF interlayer.
Helps in the localization of polysulfides and acts as a pseudo current collector.
Facilitates the penetration of the electrolyte for the electrochemical reaction.
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: Figure 15. FE-SEM images of the CNTF interlayer (a) before cycling (inset: enlarged image), (b) after 200 cycles at 1 C rate (inset: enlarged image).
Figure 16. The EDAX spectrum of the CNTF interlayer after 200 cycles at 1 C rate.
The image of the free standing and flexible CNTF interlayer displays interconnected carbon nanotubes which are randomly aligned with a porous 25 | P a g e
structure. The porous nature of interlayer is beneficial in two different ways. It allows an easy pathway for the electrolyte to permeate through the layer. The porous CNTF layer can trap the migrating polysulfides species and retain them within the cathode region. The FE-SEM image of the CNTF interlayer after 200 charge-discharge cycles is given in figure 15(b) and the inset shows the enlarged form.
The morphology of the interlayer after cycling is quite different from that of the interlayer before cycling. The pores of the interlayer have almost disappeared after cycling as they have been blocked by the precipitate. The agglomeration found in the interlayer after cycling indicates the trapping of the migrating polysulfides from the cathode region. The EDAX elemental distribution pattern shown in figure 16 confirm the nature of the precipitate that blocks the pores of the CNTF interlayer. It is clear that the precipitate contains elemental sulfur which further supports the entry of the polysulfides and their accumulation in the interlayer. The CNTF interlayer thus suppresses the polysulfide shuttle phenomenon and effectively improves the electrochemical activity of the Li-S cells

## Slide 36
There is a sharp fall in the value of charge transfer resistance (Rct) of the cell from 1050 Ω to 250 Ω for the Li-S cells with the CNTF interlayer
The significant decrease in the value of Rct is due to the formation of a conductive pathway for charge transfer by the interconnected CNTs network.
Nyquist plot of Li-S cell without and with CNTF interlayer
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: The EIS measurements were carried out in the frequency range between 1 MHz and 10 mHz at the open-circuit voltage. The observed Nyquist plots of the Li-S cells without and with the CNTF interlayer are shown in figure 14. In the Nyquist plot, the diameter of the semicircular portion in the high-frequency region gives the charge transfer resistance (Rct) of the cell.
The significant decrease in the value of Rct after the insertion of the CNT interlayer is attributed to the formation of a conductive pathway for charge transfer by the highly electrically conducting CNT interlayer [60,61]. The interlayer acts as an upper current collector, reducing the resistance of cathode material and thereby conversely enhancing the utilization of the SPMC composite cathode [44,62,63]. The CNT interlayer can improve the electrochemical environment at the cathode interface by accelerating the electrochemical kinetics taking place at the cathode by allowing rapid electron transfer and efficient accessibility of active material to the electrolyte [29,64]. The increase in the available surface area by the introduction of conductive CNT matrix is the main reason for the improved kinetics taking place at the cathode.

## Slide 37: Conclusions
The coconut shell derived, steam activated carbon, treated with HF acid to achieve maximum purity, termed as AC, is used as the material to make the composite with sulfur to serve as the composite cathode ACS.
The use of the flexible film of acid-functionalized carbon nanotubes (CNTF) as the interlayer is also part of the green approach, because acid functionalization removes the inherent toxic effects of the CNTs
The adoption of this type of cathode assembly is a green approach, since the AC sample is obtained from the bio product coconut shell.
The interlayer effectively hinders the polysulfide shuttle effect and stimulates the performance of the Li-S cells by providing much higher discharge capacity of 542 mA h g-1 at 1 C and excellent cycling stability
The Li-S cells deliver an initial discharge capacity of 1562 mA h g-1 at 0.05 C rate and retain 71% of the initial capacity at 1 C rate after 200 cycles.
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 38: Chapter 4
Sulfur-polyaniline coated mesoporous carbon composite in combination with carbon nanotubes interlayer as a superior cathode assembly for high capacity lithium-sulfur cells.
Manoj M., et.al, Applied Surface Science. (2018) - Accepted
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 39: Introduction
Mesoporous Carbon (MC).
An inexpensive and highly conductive carbon material.
High surface area and pore volume facilitates the effective confining of sulfur particles within its pores
Polyaniline (PANI)
High electrical conductivity.
Ease of synthesis
Highly stable and eco-friendly.
Sulfur-Polyaniline coated Mesoporous Carbon (SPMC)
Sulfur-polyaniline coated mesoporous carbon composite (SPMC)-Cathode
CNT interlayer
Li-S cells of excellent performance
Sulfur.
High theoretical specific capacity of 1675 mA h g-1
Low electrical conductivity
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: The electrically conducting polymer PANI is extensively used to improve the electrochemical properties of various energy storage devices including rechargeable cells, supercapacitors and fuel cells owing to its ease of synthesis, environmental stability and relatively high electrical conductivity

## Slide 40
(Ammonium peroxydisulfate)
APS Solution
Aniline monomer + Mesoporous Carbon in HCl solution
Sulfur
6 hours stirring
Ice bath
Filtration and washing
PANI Coated
Mesoporous Carbon (PMC)
Sulfur with PANI Coated
Mesoporous Carbon (SPMC)
Solvothermal process at 120 ℃ for 4 hours
Synthesis of Sulfur-PANI coated Mesoporous Carbon (SPMC) composite.
Sulfur : PMC
80 : 20
Ultrasonicationand stirring
3 hours
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 41
Structural and morphological characterization
In SPMC composite, the diffraction peaks of sulfur are obvious while those of MC are not apparent due to the high degree of crystallization of sulfur.
XRD pattern of MC shows a sharp peak at 26° corresponding to (002) diffraction from graphitic carbon.
XRD peaks of sulfur (15° to 60° ) represent its orthorhombic structure.
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
(002)
(002)
Notes: For PANI, characteristic diffraction peaks are observed at 12°, 20° and 25°.
the dominant peak at 23.1° is attributed to the (222) crystal plane of sulfur.

## Slide 42
FESEM images of (a) PANI (b) Mesoporous carbon and TEM images of PMC composite (c-d)
(e)FESEM image of PMC and (f), (g) and (h) elemental mapping of PMC
TEM images of PMC composite clearly show the PANI coating on the surface of MC
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: Elemental mapping of the PMC composite is carried out to confirm the distribution of carbon and is shown in figure 3(f). The presence of elements such as oxygen and sulfur (figure 3(g-h)) observed in the elemental mapping of the PMC composite arises from the oxidant, ammonium persulfate used in the polymerization of aniline and further confirms the existence of PANI on the surface of MC .

## Slide 43
Lattice fringes with an interlayer spacing of 0.38 nm correspond to the (222) plane.
TEM images (a-c) and (d) SAED pattern of SPMC (e) FESEM image of SPMC
EDX of SPMC
TGA curves
Sulfur ~ 80%
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: The crystalline nature of sulfur particles is visible in the HR-TEM image. The lattice fringes observed with an interlayer spacing of 0.38nm
correspond to the (222) plane of sulfur.

## Slide 44: Cell fabrication
Li-S test cells : Swagelok type.
Cathode : SPMC composite
Anode : Li foil,
Separator : Celgard
Electrolyte : 1M lithium perchlorate in a mixed solvent of 1, 3 dioxolane (DOL) and 1, 2 dimethoxymethane (DME) at a volume ratio of 1:1 including 0.5 M LiNO3 .
Voltage window : 1.5 V - 3V
Sulfur loading ~ 1.3 mg cm-2
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: The ACS composite cathode electrodes for Li-S cells were prepared from the slurry containing 80 wt. % ACS composite, 10 wt. % of acetylene black and 10 wt. % of polyvinylidene difluoride (PVDF) in N-methyl pyrrolidinone (NMP) solvent as explained earlier. The homogeneous slurry was then spray coated on an aluminium foil and after drying at 60 °C under vacuum for 12 hours, the cathode electrodes were cut into circular disks of 10 mm in diameter with a sulfur loading of approximately 1.3 mg cm-2. Using stainless steel Swagelok cells, Li-S cells were assembled by stacking ACS composite as the cathode active material, Li foil as the anode and Celgard as the separator in an argon-filled glove box,with 1 M lithium perchlorate in a mixed solvent of 1, 3-dioxolane (DOL) and 1, 2-dimethoxymethane (DME) at a volume ratio of 1:1 including 0.5 M LiNO3 as an electrolyte additive, as the electrolyte[42,43]. The synthesized CNTF interlayer was placed between the separator and the ACS cathode and the amount of electrolyte added to each cell was 70 μl. The cyclic voltammetry (CV) test was carried out at a scan rate of 0.1 mV s-1 in the voltage window of 1.5-3 V and the electrochemical impedance spectroscopy (EIS) studies in the frequency range between 1 MHz and 10 mHz, using Bio-Logic SP300 workstation. The test cells were charge-discharge cycled between 1.5 and 3 V at various C-rates (1C=1650 mA g-1) using the 8 channel battery analyzer (MTI Corporation-USA) at room temperature

## Slide 45: Electrochemical studies
Increase in redox currents observed in the Li-S cells with CNT interlayer, which indicates better utilization of the sulfur cathode material.
The slight over potential observed in the initial cathodic and anodic peaks in the cells with interlayer disappears after the first cycle, perhaps due to the rearrangement of the active material to electrochemically favorable positions
Cyclic voltammograms of the Li-S cell (a) without and (b) with CNT interlayer
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 46
The cells without the CNT interlayer show rapid capacity fading (one-forth of the initial values on cycling at 0.2 C and 0.5 C rates) after 50 cycles.
Li-S cell without interlayer: 315 mA h g-1 at 0.5 C
Li-S cell with interlayer: 1093 mA h g-1 at 0.5 C and 968 mA h g-1 at 1 C
Initial Discharge-charge profiles of the Li-S cell (a) without and (b) with CNT interlayer
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: The cells without the CNT interlayer show an initial lithiation capacity of 1095 mA h g-1 at 0.1 C with rapid capacity fading. At higher C-rates of 0.2 C and 0.5 C, the initial discharge capacities observed are 555 mA h g-1 and 315 mA h g-1 respectively which gives an indication of the weakening of the electrochemical activity in the cells. The inset of figure 7(a) shows the cycling stability curves of the Li-S cells without the CNT interlayer at the rates of 0.2 C and 0.5 C. The discharge capacities of the Li-S cells without employing the CNT interlayer are found to deteriorate sharply to below one-forth of the initial values on cycling at both the C rates, after 50 cycles.
The cells with the CNT interlayer show much better electrochemical performance during the charge-discharge process with higher charge-discharge capacities

## Slide 47
Li-S cells with the interlayer
Specific capacity : 360 mA h g-1 at 2 C after 200 cycles.
Capacity retention : 67% at 2 C and 72.3% at 1 C
Coulombic efficiency : 98% at 2 C
Rate capability of the Li-S cells: Capacity of 890 mA h g-1 obtained after the C-rate was reverted back to 0.5 C from 2 C.
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: This retention of discharge capacity even after undergoing cycling at higher C-rates indicates good compatibility between the CNT interlayer and the SPMC cathode, which facilitates the smooth transport of lithium ions also, suppressing the shuttling of polysulfides across the electrodes.

## Slide 48: Role of CNT interlayer
Functions of the CNT interlayer
  It facilitates the localization of the polysulfides within the cathode region
  Acts as a pseudo-upper current collector and enhances the performance of the Li-S cells
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: Figure 9. Rate capability of the Li-S cells with the CNT interlayer from 0.5 C to 2 C.
From these observations, it is quite clear that the insertion of the CNT interlayer between the separator and the sulfur composite cathode significantly improves the electrochemical performance of the Li-S cells. The CNT interlayer helps in better utilization of the sulfur composite cathode material by improving the conductivity of the interface and thereby accelerating the electrochemical kinetics taking place. This is in addition to the effects of the polyaniline coated mesoporous carbon (PMC) in improving the electrical contact and thereby enhancing the utilization of sulfur. The presence of the PMC helps in blocking the dissolution of the polysulfides in the electrolyte and the CNT interlayer facilitates the localization of the polysulfides within the cathode region and the combined effects substantially hinder the polysulfide shuttle phenomenon.

## Slide 49
In Nyquist plots, the semicircular loop at high to medium frequency region is related to the charge transfer resistance.
The Li-S cell with the CNT interlayer shows a drastic decrease in Rct from 1073 Ω to 150 Ω.
FESEM images of the CNT interlayer after 200 cycles
Nyquist plots of Li-S cell
Before cycling
After cycling
Trapped Polysulfides
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: The CNT interlayer helps to reduce the charge transfer resistance by providing a conductive path

## Slide 50: Conclusions
The SPMC composite cathode with the CNT interlayer significantly improves the performance of the assembled Li-S cells
The presence of the conducting PMC network facilitates good electrical contact for the sulfur particles
The polyaniline coating over sulfur particles also limits the enormous volume expansion of sulfur during lithium intake.
The network of the carbon nanotubes of the interlayer acts as a “store-room” of the polysulfides by holding back the migrating polysulfides.
The conducting network of the interlayer helps in lowering the charge transfer resistance and subsequently ensuring better utilization of the sulfur composite cathode material during the cycling process.
The Li-S cells with the CNT interlayer offer high discharge capacity of 968 mA h g-1 at 1 C and 700 mA h g-1 after 200 cycles corresponding to an extremely low capacity decay of 0.14% per cycle
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 51: Chapter 5
Polyaniline–Graphene Oxide based ordered nanocomposite
electrodes for high-performance supercapacitor applications.
Manoj M., et.al, Journal of Material Science: Materials in Electronics (2017) 28: 14323
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 52: Introduction
The suitability of polyaniline (PANI)–graphene oxide (GO) nano-composite for developing high power supercapacitors is investigated.
Interfacial double layer capacitance
Carbon based electrode materials
Pseudo-capacitance
Conducting polymers and transition metal oxides based electrodes
Polyaniline (PANI)
Ease of synthesis, environmental stability and tunable electrical properties
PANI has lower surface area.
Poor cycling stability due to the low mechanical strength.
Conducting polymer composites with carbon-based materials can be used to serve as electrode materials in super capacitors to eliminate the above-mentioned limitations.
Graphene oxide (GO) is chosen as the material to make composites with PANI because of its ease of synthesis and good mechanical properties
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 53
Synthesis of PANI-GO composite.
APS Solution
Aniline monomer + GO in HCl solution
6 hours stirring
Ice bath
Filtration and washing
Modified Hummer’s method
Graphite powder
Graphene oxide (GO)
PANI-GO composite
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 54
Structural and morphological characterization
In the PANI–GO composite formation, GO acts as a supporting material and provides sites for the nucleation and growth processes of PANI rods on the surfaces of GO sheets
X-Ray diffraction
(002)
FESEM of (a) GO, (b) PANI and (c-d) GO-PANI composite
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: The synthesized GO shows diffraction peaks at 11.4° and 42.6° corresponding to the (002) and (100) planes.
The XRD peaks observed for PANI indicate the semi-crystalline nature of the polymer
The same nature of the peaks observed for the PANI–GO composite confirms that the semi-crystalline nature of PANI is maintained after the insitu polymerization
The FE-SEM image of PANI–GO composite exhibits a layered structure of GO with PANI rods on the surfaces of the GO sheets.

## Slide 55
Structural and morphological characterization
For GO, the peaks at 1025, 1220 and 1720 cm−1 are assigned to C–O (alkoxy groups) stretching, C–O (epoxy groups) stretching and C=O stretching modes respectively.
For PANI, the characteristic peaks at 1480 and 1560 cm−1 correspond to the benzenoid and quinoid ring vibrations respectively.
FTIR spectral analysis
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: The peaks at 1292, 1111 and 793 cm−1 can be associated with the C–N stretching of the secondary aromatic amine, C–H in-plane bending and C–H out of plane bending vibrations, respectively.

## Slide 56: Electrochemical studies
Working electrode (PANI-GO)
Standard calomel electrode
Platinum
wire
Electrolyte
( 1 M LiClO4)
Mass loading ~ 2 mg
Voltage window
  Aqueous electrolyte ~ 1 V
  Organic electrolyte ~ 3 V
CV curves at 10 mV s-1
Three electrode configuration
GO- EDLC (Rectangular shape)
PANI-GO composite EDLC + Pseudo capacitor
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 57
CV curves of PANI-GO composite
GCD curves of GO
GCD curves of PANI-GO composite
– Discharge current
- Discharge time
- Mass of the active material
– Voltage window
GO : 177 F g-1 at 0.2 A g-1
PANI-GO : 810 F g-1 at 0.2 A g-1
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 58
Two electrode configuration
GCD curves at 5 Ag-1
Specific capacitance
3 A g-1 : 230 F g-1
4 A g-1 : 175 F g-1
5 A g-1 : 132 F g-1
Coin-type super capacitor test cell
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 59
Nyquist plots in the frequency range of 20 kHz–10 mHz
Cycling stability
GO
Rs : 1.508 Ω
Rct :240 Ω
PANI-GO:
Rs :0.7441 Ω
Rct :13.5 Ω
After 1000 cycles:
Specific capacitance :112 F g-1 at 5 A g-1
84.8% of the initial capacitance
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: This is the Nyquist plot of the device which determines the series and charge transfer resistance. These are the resisitance values observed for GO and PANI-GO composite. For PANI-GO composite the significant decrease in Rct value was observed due to the increased SA of the composite.
The series resistance and charge transfer resistance of the GO electrode are found to be 1.508 and 240 Ω and those of the PANI–GO composite electrode are 0.7441 and 13.5 Ω. The significant decrease in the value of the charge transfer resistance is due to the increased surface area of the composite which offers added area of contact between the electrode and the electrolyte and thus reduces the resistance at the interface.

## Slide 60: Conclusions
Specific capacitance around 810 F g-1 at a current density of 0.2 A g-1 was obtained for the PANI–GO composite electrode in three electrode configuration.
The in-situ oxidative polymerization of aniline in the presence of GO facilities the ordered growth of PANI with rod like structure, with the GO sheets acting as the templates for the growth.
Charge storage mechanism involves both EDLC and pseudo capacitance.
The capacitance around 132 F g-1 at a current density of 5 A g-1 obtained for PANI–GO composite based super capacitor test cells.
The cells are found to have remarkable cycling stability with a retention of 84.8% of the initial capacitance after 1000 cycles.
This simple and cost effective synthesis technique helps in the designing of high-power super capacitors.
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 61: Chapter 6
Mn3O4-mesoporous carbon composite as a promising anode material for rechargeable lithium ion cells.
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 62: Introduction
Graphite: The most commonly used anode material for LIBs.
Layered structure: Li ions can intercalate and de-intercalate easily.
Abundant, relatively low-cost and long cycle life.
Low theoretical capacity (375 mA h g-1)
( Insufficient to meet large scale applications)
Transition metal oxides (TMOs): Possible replacements for graphite.
Conversion-type reaction with Li
Mn3O4.
High theoretical capacity (936 mA h g-1)
Earth abundance and environmentally benign nature
Limitations
Poor electrical conductivity
Volume expansion during cycling
Mesoporous carbon: Excellent substrate to host anode materials
  Short diffusion path of lithium ions
  Easy electrolyte penetration through mesopores.
  High surface area and good electrical conductivity.
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 63
Synthesis of Mn3O4- MC composite.
Hexadecyltrime- thylammonium bromide
(CTAB) in water
Hydrazine Hydrate
Solvothermal process at 180 ℃ for 12 hours
Mesoporous carbon
Filtration and washing
Mn3O4 rods
Ultra sonication
Acetone
Drying
Mn3O4-MC composite
Stirring
Mn3O4: MC
1 : 1
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Manganese acetate tetra hydrate (MATH)
dissolved in water

## Slide 64
Structural and morphological characterization
The diffraction peaks at 2 angles are indexed which suggests the presence of highly pure Mn3O4 with tetragonal spinel structure.
The XRD pattern of MC shows a sharp peak at 26° corresponding to (002) diffraction from graphitic carbon.
The XRD pattern of the composite has peaks corresponding to both Mn3O4 and MC phases, which confirms that in the final composite, the structures of Mn3O4 and MC are retained without any changes.
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: As seen in this figure, an intense vibrational mode located a 655 cm-1 which is the characteristics of the spinel structures assigned to the A1g mode, which corresponds to the Mn–O breathing vibration of Mn2+ ions in tetrahedral coordination [19]. It is also observed that two low-intensity bands at 316 and 370 cm-1 witch in well agreement with the literature reports on Mn3O4 Raman features
The strong peak at 647 cm-1 (Mn-O breathing vibration of Mn2+ ions) and a minor peak at 358 cm-1 can be ascribed to crystallined Mn3O4. 21, 23, 24 All of the experimental facts clearly indicate the formation of Mn3O4@C nanocomposites.

## Slide 65
Structural and morphological characterization
Mn3O4-MC composite has a higher ID/IG than bare MC
In Mn3O4-MC, the increase of ID/IG is presumably due to two reasons: (i) Mn3O4 may occupy some portion of crystalline graphite, and (ii) graphite surface may be partially destroyed during the composite formation.
Pure Mn3O4: Peak at 640 cm-1 corresponds to the Mn–O breathing vibration of Mn2+ ions in tetrahedral coordination .
Two characteristic Raman peaks of MC:
  D – band: 1350 cm-1 attributed to amorphous carbon or deformation vibrations of the hexagonal ring.
  G - band 1580 cm−1 assigned to the stacking of the graphite hexagon network plane.
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
640 cm-1
D band
G band
Notes: As seen in this figure, an intense vibrational mode located a 655 cm-1 which is the characteristics of the spinel structures assigned to the A1g mode, which corresponds to the Mn–O breathing vibration of Mn2+ ions in tetrahedral coordination [19]. It is also observed that two low-intensity bands at 316 and 370 cm-1 witch in well agreement with the literature reports on Mn3O4 Raman features
The strong peak at 647 cm-1 (Mn-O breathing vibration of Mn2+ ions) and a minor peak at 358 cm-1 can be ascribed to crystallined Mn3O4. 21, 23, 24 All of the experimental facts clearly indicate the formation of Mn3O4@C nanocomposites.

## Slide 66
FESEM images of composite establish the dispersion of Mn3O4 nanorods within the MC upon physical mixing.
EDX mapping displays a uniform distribution of elements such as Carbon, Manganese and Oxygen in the composite.
EDX analysis
FESEM images of (a-b) Bare Mn3O4 (c) MC and (d) Mn3O4-MC composite
200 nm
200 nm
200 nm
100 nm
(a)
(b)
(c)
(d)
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: The element mapping analysis confirmed the coexistence and homogeneous dispersion of elements Mn, C and O in the as-obtained Mn3O4@C nanocomposites.

## Slide 67: Cell fabrication
Li-ion test cells : Swagelok type.
Anode : Mn3O4-MC composite on Cu foil
Cathode : Li foil
Separator : Celgard
Electrolyte : 1M LiPF6 in mixed ethylene carbonate and diethyl carbonate (1:1)
Voltage window : 0.01 - 3V
Mass loading ~ 1.5 mg
CV curve of Mn3O4-MC composite at 0.1 mV s-1
Cathodic peak
1.03 V and 0.6 V : Solid electrolyte interface (SEI) layer formation – electrolyte decomposition on the electrode surface and some irreversible reactions.
[during the initial discharge ].
0.02 V: Decomposition of MnO to metallic Mn.
Anodic peak
1.3 V: Oxidation of Mn to MnO.
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 68
Loss in capacity is due to the SEI layer formation and the irreversible reaction of the samples.
Discharge profile in the first cycle differs from the subsequent cycles and is in congruence with the results from CV studies.
GCD curves of Mn3O4 and Mn3O4-MC composite at 100 mA g-1
Bare Mn3O4 :
  First discharge capacity : 1301 mA h g-1
  First charge capacity : 650 mA h g-1
Mn3O4-MC composite
  First discharge capacity : 1601 mA h g-1
  First charge capacity : 894 mA h g-1.
    Coulombic efficiency- 55.8 %
  Second discharge capacity : 920 mA h g-1
  Second charge capacity : 882 mA h g-1
    Coulombic efficiency- 95 %
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: The first discharge curve is different from other cycles, which may relate to the irreversible reaction from Mn (III) to Mn (II) and the formation of amorphous Li2O matrics.11, 37

## Slide 69
During conversion reaction Mn3O4 gets disintegrated to fragments while it is transformed into MnO and subsequently to metallic Mn
In subsequent cycling, charge storage has been proposed to involve only Mn and MnO
The higher capacity in the first cycle is not only contributed by the conversion of Mn3O4 to Mn, but with the formation of SEI as well, which is not included in the theoretical capacity of Mn3O4.
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
*

## Slide 70
Rate capability of Mn3O4 and Mn3O4-MC composite
Current density (mA g-1) | Specific capacity (mA h g-1) |  |  | 
 | Mn3O4 - MC |  | Bare Mn3O4 | 
 | Discharge | Charge | Discharge | Charge
100 | 1601 | 894 | 1390 | 640
200 | 780 | 723 | 533 | 504
500 | 627 | 610 | 334 | 306
1000 | 488 | 469 | 204 | 189
2000 | 378 | 356 | 126 | 118
100 | 810 | 725 | 380 | 340
Cycling stability of Mn3O4-MC composite
After 100cycles
730 mA h g-1
CE: 92%
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: The average reversible discharge capacities of Mn3O4@C nanocomposites are 584 mA h g-1 (0.2 A g-1), 500 mA h g-1 (0.5 A g-1), 430 mA h g-1 (1 A g-1), 320 mA h g-1 (2 A g-1), 170 mA h g-1 (5 A g-1) at different current densities. What is more, the discharge capacity of Mn3O4@C nanocomposites can return to 588 mA h g-1 when changing the current density to 0.2 A g-1, indicating the high electrochemical reversibility of the process.

## Slide 71: Conclusions
The Mn3O4-MC composite can be explored as a high-capacity, low-cost and eco-friendly anode material for Li-ion battery applications.
FESEM studies and Raman analysis confirm the formation of Mn3O4-MC composite by the incorporation of Mn3O4 on the surfaces of MC.
After the first discharge/charge cycle, coulombic efficiency is increased to 95%.
Discharge and charge capacities of 920 mA h g-1 and 882 mA h g-1 at 100 mA g-1, respectively, are obtained by reversible electrochemical reaction.
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 72: Chapter 7
A Li-ion full cell using LiFePO4 cathode and
Mn3O4-mesoporous carbon anode
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 73: Introduction
LiCoO2 - first cathode material when Li-ion batteries were commercialized in 1990.
Cathode materials such as, LiNiO2, LiMn2O4, and LiFePO4 have also been developed
LiCoO2 is costly and toxic, and its resources are no longer abundant
LiFePO4:
  Olivine structure
  Low cost and non toxicity
  High thermal stability
  High specific capacity of 170 mA h g−1.
This electrode configuration can be a highly attractive model for applications requiring high power, low cost, and reliability.
For realization of a full cell configuration, LiFePO4 (cathode)-Mn3O4-MC (anode)- full cells are assembled with a cathode limiting capacity
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: This electrode configuration could be a highly attractive candidate for applications requiring high power, low cost, and reliability.

## Slide 74: Synthesis
Lithium Nitrate
Iron Oxalate dihydrate
Ammonium dihydrogen phosphate
Dried at 80 oC and fired at 700 oC in argon atmosphere
HNO3 + Citric Acid
(1 M) at 50 oC
LiFePO4
All of the reflections can be attributed to the orthorhombic phase LiFePO4.
300 nm
LiFePO4
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
LiFePO4
(020)
(011)
(120)
(111)
(121)
(031)
(131)
(211)
(140)
(221)
(112)
Notes: that lacks any impurity phase. The profiles of the reflection peaks are quite narrow and symmetric, indicating the high crystallinity of the LiFePO4 sample

## Slide 75
Electrochemical characterization of LiFePO4
It shows two peaks:
Anodic peak at 3.6 V due to oxidation of Fe2+ to Fe3+.
Cathodic peak at 3 V due to reduction of Fe3+ to Fe2+.
CV curve of LiFePO4 half cell at 0.1 mVs-1
GCD curves of LiFePO4 at 0.2 C
Initial discharge capacity: 55 mA h g-1 at 0.2 C
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 76
Full cell configuration
Pre-lithiation of anode
Li-ion full cell : Swagelok type.
Cathode : LiFePO4 (1.4 mg)
Anode : Pre-lithiated Mn3O4-MC composite (1.5 mg)
Separator : Celgard
Electrolyte : 1M LiPF6 in mixed ethylene carbonate and diethyl carbonate (1:1).
Voltage window : 2.5 V to 4.2 V
Mn3O4-MC composite coated on Cu foil partially pre-lithiated by placing it in direct contact with a Li foil wetted with electrolyte (12 hours)
To suppress the irreversible capacity loss
Lithium ions from Li metal are released into the electrolyte. In order to obtain charge neutrality, lithium ions of the electrolyte are intercalated/inserted into the active material.
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1
Notes: Lithium ions from Li metal are released into the electrolyte. In order to obtain charge neutrality, lithium ions of the electrolyte are intercalated/inserted into the active material of the

## Slide 77
Electrochemical characterization of Full cell
CV curve of Mn3O4-MC-LiFePO4 full cell at 0.1 mV s-1
GCD curves of Mn3O4-MC-LiFePO4 at 0.2 C
Initial discharge capacity: 33 mA h g-1 at 0.2 C
Cycling stability of full cell for 50 cycles at 0.2 C
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 78
Conclusions
The LiFePO4-Mn3O4-MC full cell configuration can be developed as a reliable lithum cell, potentially offering low cost, high rate capability, and excellent safety features.
The electrochemical properties of Mn3O4-MC as anode and LiFePO4 as cathode for LIBs were investigated in a half cell configuration.
Prelithiated Mn3O4-MC was combined with LiFePO4 cathode for a complete Li-ion cell with a cathode limiting capacity.
The Mn3O4-MC electrode was prelithiated by placing it in direct contact with a Li foil wetted with electrolyte.
The LiFePO4-Mn3O4-MC full cell delivers reversible capacity without capacity fading for 50 cycles, at 0.2 C.
Chapter 7
Chapter 6
Chapter 5
Chapter 4
Chapter 3
Chapter 2
Chapter 1

## Slide 79
General Conclusions
The coconut shell derived, steam activated carbon, treated with HF acid (AC) is used as the material to make the composite with sulfur for high performance Li-S cells.
The concept of having free-standing and flexible film of acid-functionalized carbon nanotubes (CNTF) interlayer simplifies the battery processing techniques.
Incorporated CNT interlayer localizes the polysulfides in the cathode region and provides high specific capacity and serves as pseudo-secondary current collector.
ACS based Li-S cells deliver an initial discharge capacity of 1562 mA h g-1 at 0.05 C rate and retain 71% of the initial capacity at 1 C rate after 200 cycles.
The interlayer effectively hinders the polysulfide shuttle effect and stimulates the performance of the Li-S cells by providing much higher discharge capacity of 542 mA h g-1 at 1 C and excellent cycling stability

## Slide 80
In SPMC based Li-S cells, the presence of the conducting PMC network facilitates good electrical contact for the sulfur particles and also limits the adverse effects of the possible enormous volume expansion of sulfur during lithium intake.
In these Li-S cells , the network of the carbon nanotubes interlayer also acts as a “store-room” of the polysulfides by holding back the migrating polysulfides.
SPMC based Li-S cells with CNT interlayer delivers an initial discharge capacity of 968 mA h g-1 at 1 C and 700 mA h g-1 after 200 cycles corresponding to an extremely low capacity decay of 0.14% per cycle.
SPMC based Li-S cells show high discharge capacity at higher C rates than ACS based Li-S cells.
High performance PANI-GO based super capacitors are assembled.
PANI-GO composite electrode shows 810 F g-1 at 0.2 A g-1 in three electrode configuration.
Charge storage mechanism involves both EDLC and pseudo capacitance.

## Slide 81
PANI–GO composite based super capacitor shows high capacitance of 132 F g-1 at a current density of 5 A g-1 and remarkable cycling stability with a retention of 84.8% of the initial capacity after 1000 cycles.
Mn3O4-MC composite can be explored as a high-capacity, low-cost and eco-friendly anode material for Li-ion battery applications.
Mn3O4-MC composite based Li-ion cells show high coulombic efficiency (95%) with second discharge/charge capacity of 920 mA h g-1/882 mA h g-1.
Li-ion full cells using LiFePO4 cathode and Mn3O4-MC anode are assembled.
The LiFePO4-Mn3O4-MC based full cell delivers reversible capacity without capacity fading for 50 cycles at 0.2 C.
The LiFePO4-Mn3O4-MC full cell configuration can be developed as a reliable lithium cell potentially offering low cost, high rate capability, and good safety features.

## Slide 82
Future Plans
Optimization of various parameters for the development of next generation Li-S full cells with suitable anode materials.
Realization of LiFePO4 -Mn3O4-MC based Li-ion full cells meeting commercial standards.

## Slide 83
Journal Publications
Manoj, M., Anilkumar, K.M., Jinisha, B, S Jayalekshmi, Polyaniline–Graphene Oxide based ordered nanocomposite electrodes for high-performance supercapacitor applications, J Mater Sci: Mater Electron (2017) 28: 14323
Manoj M, Jasna M, Anilkumar K M Jinisha B, Abhilash A, Pradeep VS, S. Jayalekshmi, Sulfur-with polyaniline coated mesoporous carbon composite in combination with carbon nanotubes interlayer as a superior cathode assembly for high capacity lithium-sulfur cells, Applied Surface Science (2018).
K.M. Anilkumar, B. Jinisha, M. Manoj, V.S. Pradeep, S. Jayalekshmi, Layered sulfur/PEDOT:PSS nano composite electrodes for lithium sulfur cell applications, Applied Surface Science 442 (2018) 556–564.
K.M. Anilkumar, B. Jinisha, M. Manoj, S. Jayalekshmi, Poly(ethylene oxide) (PEO) – Poly(vinyl pyrrolidone) (PVP) blend polymer based solid electrolyte membranes for developing solid state magnesium ion cells,, European Polymer Journal 89 (2017) 249–262.
Jinisha B, Anilkumar KM, Manoj M, Pradeep V.S, Jayalekshmi S, Development of a novel type of solid polymer electrolyte for solid state lithium battery applications based on lithium enriched poly (ethylene oxide) (PEO)/poly (vinyl pyrrolidone) (PVP) blend polymer, Electrochimica Acta 235 (2017) 210–222.

## Slide 84
Jinisha, B., Anilkumar, K.M., M.Manoj, S Jayalekshmi. Poly (ethylene oxide) (PEO)-based, sodium ion-conducting‚ solid polymer electrolyte films, dispersed with Al2O3 filler, for applications in sodium ion cells, Ionics (2018) 24.
Joseph John, M. Manoj, K. M. Anilkumar, V. S. Pradeep, S. Jayalekshmi, Lithium-enriched polypyrrole as a prospective cathode material for Li-ion cells, Ionics (2018).
C. Muhamed Ashraf, K. M. Anilkumar, B. Jinisha, M. Manoj, V. S. Pradeep and S. Jayalekshmi Acid Washed, Steam Activated, Coconut Shell Derived Carbon for High Power Supercapacitor Applications, Journal of The Electrochemical Society, 165 (5) A900-A909 (2018).
Anand B. Puthirath, Sudeshna Patra, Shubhadeep Pal, Manoj M., Aravind Puthirath Balan, Jayalekshmi S. and Narayanan Tharangattu N. Transparent flexible lithium ion conducting solid polymer electrolyte. J. Mater. Chem. A, 2017, 5,11152.
Anilkumar KM, Manoj M, Jinisha B, Pradeep VS, S. Jayalekshmi, Mn3O4/reduced graphene oxide nanocomposite electrodes with tailored morphology for high power supercapacitor applications, Electrochimica Acta 236 (2017) 424–433

## Slide 85
Conference Publications
On the structural and electrical properties of Polyaniline-graphene nanocomposite films, M Manoj, S Jayalekshmi, 2nd International Conference on Advanced Functional Materials (ICAFM 2014), Trivandrum, India.
Polyaniline zinc oxide composite electrode materials for supercapacitor applications, Manoj M, Anilkumar K M, Jinisha B, S Jayalekshmi, 28th Kerala Science Congress, Jinisha B, Anil Kumar K M, S Jayalekshmi Calicut University Campus, Thenhippalam.
Polyaniline graphene oxide composite electrode materials for supercapacitor applications, Manoj M, Anilkumar K M, Jinisha B, S Jayalekshmi National conference on Carbon Materials (NCCM 2015) Conducted by NPL , New Delhi ,India.
Polyaniline coated CNT-Sulfur composite as cathode material for lithium-sulfur batteries, Manoj M, V.S. Pradeep, Anilkumar K M, Jinisha B, S. Jayalekshmi, International Conference on Advances in Functional Materials,ICAFM-2017, January, 6-8, 2017, Anna University, Chennai, India.
Anilkumar K M, Jinisha B, Manoj M, S Jayalekshmi, “Will Mg-ion cells serve as substitute for Li-ion cells ?” Proceedings of IC CAST, 2015, BHU-Varanasi, August 7-9.

## Slide 86
Acknowledgments
Prof. S Jayalekshmi , Supervising Guide.
Prof.M Junaid Bushiri, HOD, and all former HODs, Department of Physics, CUSAT.
Former and Present Teachers of DOP , CUSAT
Prof. M.K. Jayaraj, Doctoral committee member
Anil Kumar K M, Assistant Professor, MSM College Kayamkulam
Dr. Pradeep V S, Empa, Swiss Federal Laboratories for Materials Science and Technology, Switzerland.
Ms Jasna M, Research Scholar, DOP, CUSAT
All Non-Teaching staffs , DOP , CUSAT
UGC-BSR for Research fellowship.
OED Lab and Other lab friends
STIC, Kochi
Members of Dream Lab

## Slide 87
Thank You

## Slide 89
Figure 3. (a) Nitrogen adsorption isotherms of acid washed activated carbon (b) Pore size distribution curve of acid washed activated carbon.
(a)
(b)
BET Surface Area Analysis
Back

## Slide 90
For example: LiFePO4 → FePO4 + 1Li+ + 1e-
In this case we have:
Molecular weight of LiFePO4 is 157.7×10-3 kg mol-1 = 157.7 g mol-1
n=1Li+=1
F=96 485.3329 sA mol-1
So finally we obtain: Q=170 mA h g-1
Theoretical capacity calculation by Faraday’s law:
Qtheoretical = (nF) / (3600*Mw) A h g-1
Where,
n is the number of charge carrier,
F is the Faraday constant and
Mw is the molecular weight of the active material.

## Slide 91
C-rate calculation
Suppose if current density 60 mA g-1
1 g
60 mA
1 mg
60 µA
If mass is 1.5 mg
60 µA * 1.5 = 0.09 mA
If 0.09 mA is given to the sample with mass 1.5 mg, then the current density is 60 mA g-1