## Slide 1
Experimental and Theoretical Investigation of Metal-free Organic Dyes for DSSC Applications
Under the guidance of
Dr. Kothandaraman R
Divya Unny
CY16D035
Research Proposal Seminar
1st February 2019
Venue: CB 310

## Slide 2
Outline
Introduction
Energy demand & need for green energy
Types of solar cells
Dye sensitized solar cell [DSSC]
Components involved in DSSC
Operational principle of DSSC
Electron transfer dynamics in DSSC
DSSC Parameters [I-V characteristics & Electrochemical impedance spectroscopy]
Photosensitizer
Metal complex & metal-free organic dyes
Research Proposal
Conclusion

## Slide 3
Energy Demand & Need for green energy
Past, present & future (anticipated) world energy demand
Renewable vs. Non-Renewable
Variation in the mean annual solar irradiance
Phys. Chem. Chem. Phys., 2014, 16, 6838-6858.

## Slide 4
Why solar energy ?
February 2015 The IEA said:
“ Solar energy will be the largest global energy source by 2050”
September 2014, German thinktank, Agora Energieweinde:
“ Solar PV will provide the cheapest electricity of any source within 10 years”
“More energy from sunlight strikes earth in 1 hour than all of the energy consumed by humans in an entire year” (Lewis,2007).
Solar energy
Solar fuel
Solar thermal
Solar electricity
Solar electricity / Photovoltaics:
Photovoltaic(PV) collective name for devices that directly convert sunlight into electricity.
http://www.hessen-nanotech.de/mm/NanoEnergy_web.pdf

## Slide 5
Solar cell : A Historical Background
2nd generation solar cell
1st generation solar cells
22.1 %
22.6 %
Energy Environ. Sci., 2018, 11, 476-526
First crystalline silicon solar cell (SSC) with 6% efficiency envisioned by Bell Lab in 1954
1) Monocrystalline silicon cells
2) Polycrystalline silicon cells
3) Amorphous silicon cells
26.6 %
19.5 %
13.6 %
Based on thin film solar cells
GaAs Solar cell 28.8 %

## Slide 6
3rd generation solar cell
2) Perovskite solar cell
Quantum dot solar cell
Perovskite solar cell
3) Dye sensitized solar cell (DSSC)
1) Quantum dot solar cell
3) Dye sensitized solar cell (DSSC)
Efficiency > 10 %
Efficiency : 23.3 %
Efficiency: 12.6 %
Energy Environ. Sci., 2018, 11, 476-526

## Slide 7
DSSC is a photovoltaic cell, which converts solar energy into electrical energy.
Discovered by Michael Gratzel and Brain O’Regan in 1991, also known as Gratzel cell / Gcell.
The working of DSSC is similar to a leaf on a plant [natural photosynthesis] and is often refered to as artificial photosynthesis.
What DSSC is all about……???
Visible light
Infrared Light
Solar spectrum
Applications of DSSC
200 m2 of DSSC panels installed in Newcastle (Australia) – the
first commercial DSSC module
Source of figures: Internet

## Slide 8
Characteristics of DSSC
Flexible
Colourful
Transparent
Low cost
Biocompatible
Prototype models of dye sensitized solar
cell panels for decoration purpose
Light weight
http://www.sony.co.jp/Products/SCHP/cx_pal/vol80/pdf/sideview80.pdf

## Slide 9
Components involved in DSSC
Pt/FTO
5) Counter electrode
FTO or ITO
1) Transparent conducting oxide
3) Photosensitizer
FTO/TiO2/N719 dye
4) Redox electrolyte
I-/I3-
2) Semiconductor metal oxide (TiO2)
Other than I-/I3-
Co2+/Co3+
Source of figures: Internet

## Slide 10
e
I3-
3I-
e
e
e
e
Schematic diagram of energy flow in DSSC
Dye
TiO2
Pt
Redox electrolyte
FTO
FTO
Operational Principle
e
e
e
e
e
e
e
e
e
Overall Reactions in DSSC
(Photoexcitation)
S+ + e- CB (TiO2 charge injection)
 2S + I3- (Regeneration of S)
+ 2e-  3I- (Regeneration of I-)
LUMO
HOMO

## Slide 11
decay to ground
 ns
Dye
Dye
Electron injection
 100 ps
Recombination to dye, s - ms
Dye+/e-
I3- /e- TiO2
Regeneration reaction
 1 s
Recombination to electrolyte,
ms - s
Charge transport to electrode,
ms - s
I-
I3-
10 ms
10 ns
Electrolyte
Electron transfer dynamics in DSSC : Bottleneck issues
(1)
(2)
(3)
TiO2
Phys. Chem. Chem. Phys., 2014, 16, 6838--6858

## Slide 12
DSSC Parameters and I-V Characteristic
The FF is defined as the ratio of the actual maximum obtainable power from the solar cell to the product of and . It is a measure of the “squareness” of the IV curve
ɳ is the ratio of the generated maximum electric output power to the total power of incident light
VOC : Open-circuit voltage
JSC : Short-circuit current density
FF : Fill Factor
ɳ : Power conversion efficiency
Pin : Intensity of light (100 mW cm-2)
www.pveducation.org

## Slide 13
Electrochemical Impedance Spectroscopy (EIS)
R1
R2
R3
R4
C2
C4
C3
Equivalent circuit R(RC)(RC)(RC)
Nyquist Plot
Energy Environ. Sci., 2017, 10, 672-709
Rct @ Pt/ I-/I3-
interface
Rct @ dye/TiO2/electrolyte
interface
Solution
resistance (Rs)
Nernstian diffusion within the
electrolyte

## Slide 14
Photosensitizer
Metal-based
Metal-free
Condition to be satisfied by dye:
Absorption range of the dye should cover the whole visible region as well as near IR.
Molar extinction coefficient of dye must be as high as possible.
Anchoring group should strongly grafted to the TiO2 surface.
The HOMO of the dye should lie below the energy level of redox mediator.
LUMO of dye should be localized near the anchoring group, and above the CB edge of the semiconductor.
The periphery of the dye should be hydrophobic to minimize the direct contact between anode and electrolyte.

## Slide 15
Well known metal based sensitizers
N3 dye :  = 10.3 %
N719 :  = 11.18 %
Black dye(N749) :  = 10.40 %
Z907 :  = 9.5 %
Nazeeruddin et al. 1993
Wang et al. 2005
Nazeeruddin et al. 2001
Characteristics of Metal complex dyes
MLCT responsible for the light absorption
Broad absorption range from UV to near IR
High molecular stability
High excited state lifetime

## Slide 16
Absorption spectra
Soret band
Q- band
 = 12 %
 = 13 %
Dye | VOC (V) | ISC (mA cm-2) | FF | η (%)
SM371 | 0.96 | 15.9 | 0.79 | 12
SM315 | 0.91 | 18.1 | 0.78 | 13
[Co(bpy)3] 2+/3+ electrolyte
IV characteristics
Nature., 2014, 6, 242-247
Ethynylbenzoic acid acceptor
Functionalization increases the conjugation & CT character
SM371
SM315

## Slide 17
Design strategy: Push pull metal-free organic dyes
Simple classical design of an organic dye
Donors
Triphenylamine
Carbazole
Phenothiazine
Indole
Coumarin
Perylene
Linkers
Thiophene
Benzothiadiazole
Vinylbenzene
Pyrrole
Ethylene & Acetylene
Furan
Acceptors
Cyanoacrylic acid
Rhodanine 3- acetic acid
Carboxylic acid
Pyridine
e-
e-
e-
They exhibit a high molar extinction coefficient.
It is easy to design dyes with various structures & adjust the absorption wavelength range.
No use of expensive or rare metal
Advantages of organic dyes
Drawbacks of metal complex dye
High cost of noble metals & their limited availability
Low molar extinction coefficient compared to organic dyes.
Complicated synthesis route
Low yield of the product

## Slide 18
 = 4.54 %
 = 3.26 %
D-A-ℼ-A structure with  = 8.7 %
D-ℼ-A structure with  = 9.1 %
Modified dye architectures
Sustainable Energy Fuels., 2017, 1, 969–985.
D-D-ℼ-A structure
A-D-ℼ-D-A structure
 = 4.35 %
 = 2.42 %
 = 6.87 %
D-(ℼ-A)2 structure with  = 2 %
L(D-ℼ-A)2 structure/ H-type structure
 = 8.1 %

## Slide 19
Organic dyes with near IR light absorption
JK - 216 :  = 6.29 %
JK – 217 :  = 5.99 %
DTS - CA
Squarine based dyes
Highest reported efficiency in literature for
squarine dyes
Chem. Mater., 2015, 27, 2480-2487
Absorption spectra (Solution & Solid state)
max @ 669 & 672 nm
Chem. Commun., 2011, 47, 2874–2876
max in the range of
600 - 700 nm
2-Ethyl hexyl
2-Ethyl hexyl

## Slide 20
Types of acceptors & mode of linkage
Carboxylic acid
Type 1: Two step process by bidentate bridging linkage
Cyanoacrylic acid
Rhodanine 3–acetic acid
Yang et. al
Type 11: One step process
Photoexcited dye injects electrons directly from the HOMO of dye to
CB of TiO2
Catechol dyes possess both PET & DTCT characteristics.
 = 2.55 %
 = 4.28 %
 = 0.43 %
 = 0.49 %
 = 0.60 %
 = 0.57 %
Mater. Chem. Front., 2017, 1, 2243-2255.
Catechol based anchoring groups
Pyridine
 = 0.5 %

## Slide 21
Multi-anchored Sensitizers
 = 4.56 %
 = 6.08 %
Dyes with more number of anchoring groups shows:
Longer wavelength absorption (max ) and high molar extinction coefficient (max )
More efficient charge injection rate & longer electron life time
Increased current density & long term stability due to higher binding energy
No significant difference in voltage among the dyes with respect to number of acceptor
J. Org. Chem., 2015, 80, 9034–9040
Synth. Met., 2016, 217, 248–255
TPA3T1A
TPA3T3A
TPA3T2A
 = 4.9 %
 = 6.1 %
 = 6.3 %
λ max = 419 nm
λ max = 421 nm
λ max = 436 nm
λ max = 479 nm
λ max = 488 nm

## Slide 22
Π-Spacer/Linker
Spacer with electron-deficient moieties
Π-Spacer for extending the conjugation & hence better charge separation is achieved between HOMO & LUMO of the dye
Structures with binary spacers or multi spacers
 = 7.6 %
Energy Environ. Sci., 2011, 4, 4735–4742
 = 8.99 %
 = 8.56 %
Energy Environ. Sci., 2012, 5, 8261–8272
 = 10.1 %
binary spacer
Electron deficient moieties separates the ICT much better
Red shift the absorption maximum
Higher molar extinction coefficient & LUMO of the dye can be tuned
to get directionality
Improves the photovoltaic performance
Spacer connect the lipophilic alkoxy substituted
TPA & Hydrophilic CA
Alkyl chain repel iodine
Electrolyte from TiO2 surface

## Slide 23
(B) Multilayer Co-sensitization
Co-sensitization
(A) Direct Co-sensitization
J. Am. Chem. Soc. 2004, 126, 5670-5671
New J. Chem. 2005, 29, 773-776
Co-sensitization is the co-adsorption of two or more sensitizers with different absorption spectrum ranges are mixed together, to broaden the spectrum response range.
(A) Absorption spectra
380 nm
535 nm
642 nm
Efficiency is raised to 6.5 %
Concentration of dye solution
10: 10 :1 molar ratio
Aggregation behaviour can be altered
Co-adsorption results in compact
coverage of TiO2 surface
Dye loading on TiO2 film :
5:1:1.5
2.8 %
4.6 %
3.9 %
Yellow Merocyanine dye

## Slide 24
LEG4
ADEKA 1
Chem. Commun. 2015, 51, 15894-15897
J-V Characteristics
Electrolyte | Counter electrode | Light intensity (mWcm-2) | VOC (V) | JSC (mA cm-2) | FF | η (%)
I3-/I- | FTO/Pt | 100 | 0.783 | 19.11 | 0.748 | 11.2
[Co(Phen)3]3+/2+ | FTO/Pt | 100 | 1.018 | 17.77 | 0.765 | 13.8
[Co(Phen)3]3+/2+ | FTO/Au/GNP | 100 | 1.014 | 18.27 | 0.771 | 14.3
[Co(Phen)3]3+/2+ | FTO/Au/GNP | 50 | 0.994 | 9.55 | 0.776 | 14.7
Co–sensitization of two organic dyes :
ADEKA 1 & LEG4
Cobalt – phenathroline as redox couple
Top efficiency : 14.3 %

## Slide 25
The absorption spectrum of I3- shows a small molar extinction coefficient of 2.73 * 104 M-1 cm-1 with a dip at 320 nm.
The VOC enhancement is attributed to the combined and
complementary light harvesting ability of Y1, TP2A and HSQ dyes.
Panchromatic absorption range reported is the highest recorded value for triple based dyes.
Sustainable Energy Fuels., 2018, 2, 209–214
Y1
TP2A
Panchromatic absorption in the range
300 – 820 nm
350 nm
I-V Parameters
390 nm
350 & 581 nm
390 & 703 nm
HSQ4
Highest efficiency based on
cosensitization of triple organic dyes
 = 7.48 %

## Slide 26
Aryl amine based donors
Favourable properties :
Strong electron donating ability
Presence of redox center
Tunable charge transfer towards higher ICT
Energy level match with iodine/triiodide redox couple
Representative examples
Chem. Soc. Rev., 2013, 42, 3453-3488
N
N
R
R
N
N
R
X
N
R
N
R
N
R
PTZ
X=S
POZ
X=O
Tetrahydroquinoline
carbazole
TPA
Substituted
TPA
DPA
Indoline
N
R
R
N,N
-dialkylaniline

## Slide 27
J. Am. Chem. Soc., 2014, 136, 5722-5730
Dye | Counter electrode | Light intensity (mWcm-2) | VOC (V) | JSC (mA cm-2) | FF | η (%)
IQ4 | GNP | 100 | 0.767 | 14.83 | 0.666 | 7.57
YA421 | GNP | 100 | 0.797 | 15.58 | 0.712 | 8.84
YA422 | GNP | 100 | 0.882 | 15.71 | 0.693 | 9.60
 | Au + GNP | 50 | 0.890 | 16.25 | 0.737 | 10.65
Λ max in the range of 522- 534 nm (ICT)
Bulky donor moieties prevent the approach of redox electrolyte
closer to the TiO2 surface.
Pt is known as the best catalyst for the regeneration of iodine based electrolyte.
Carbonaceous type catalyst outperforms Pt with the cobalt redox electrolyte, due to the low CT resistance at the counter electrode.

## Slide 28
Comparison of dyes in two different electrolytes
Due to the smaller size of triiodide species compared to Co3+ complex the introduction of long alkyl chains has less influence in retarding the recombination in the iodide/triiodide redox electrolyte based devices.
The electron recombination with one electron-transfer cobalt redox electrolyte is more facile than that with two electron-transfer iodide-based electrolyte.
The decreased recombination in YA422-based device contributes to an increase in the Voc value by more than 100 mV compared to the IQ4-based devices.
The photovoltaic performance of all the three dyes studied with Pt as a CE show opposite trend with iodide/triiodide
(IQ4 > YA421 > YA422) and cobalt redox electrolytes (YA422 > YA421 > IQ4).
J. Am. Chem. Soc., 2014, 136, 5722-5730

## Slide 29
RSC Adv., 2017, 7, 33975–33985
CB 1
CB 3
CB 2
CB 4
Absorption spectra
Λmax in the range of 400 – 600 nm (ICT)
Photophysical & electrochemical characteristics for dyes
N- octyl carbazole
N- methoxyphenyl carbazole
C-3
C-3
C-2
C-2

## Slide 30
I-V Performance
Photovoltaic parameters of the DSSC
The electron-donating ability and substitution positions of the donor have a significant effect on these dyes electronic and photovoltaic properties.
The N- methoxyphenyl based CB2 and CB4 displayed broader and more intensive absorption both in solution and on the surface of TiO2 & hence superior photovoltaic performance is observed.
The dihedral angle between the carbazole unit and the BODIPY framework are computed to be 61.8 for CB1, 52.3 for CB2, 60.4 for CB3, and 50.0  for CB4.
Dye | JSC /mAcm-2 | VOC /mV | ff |  /% | Dihedral angle/ degree
CB1 | 6.30 | 540 | 0.76 | 2.58 | 61.8
CB2 | 9.18 | 560 | 0.73 | 3.74 | 52.3
CB3 | 6.84 | 540 | 0.73 | 2.68 | 60.4
CB4 | 10.20 | 600 | 0.70 | 4.28 | 50.0

## Slide 31
Research Proposal

## Slide 32
D1d
D2d
D3d
Proposed dye structures
Three different D-π–A systems are designed with varying donors such as diphenylamine, carbazole & phenothiazine for comparative study.
The Vinylbenzene, Methoxy benzene & Cyanoacrylic acid act as π-spacer, auxiliary donor and acceptor, respectively. The octyl chain is intended to reduce dye aggregation.
DFT calculation was carried out to optimize the dye structure and to understand the HOMO and LUMO level and also absorption properties.

## Slide 33
Frontier orbital diagram
D1d
D2d
D3d
B3LYP/6-31G(d)

## Slide 34
Absorption spectra
Experimental
Theoretical (M06-2X/6-31G(d)
Intramolecular charge transfer (ICT)
 - 
Dyes | State | max/ nm | Oscillator strength /f |  / M-1cm-1 | Major transition
D1d | S0 to S1 | 442 | 1.8595 | 1.3  104 | HOMO to LUMO (83%)
D2d | S0 to S1 | 450 | 1.7448 | 5.1  104 | HOMO to LUMO (75%)
D3d | S0 to S1 | 461 | 1.4480 | 4.1  104 | HOMO to LUMO (78%)
 - 
ICT

## Slide 35
WE: Glassy carbon
CE: Pt mesh
RE: Ag/AgNO3 (0.01 M)
Supporting electrolyte: TBAPF6
Solvent: Dicholoromethane
Scan rate: 100 mVs-1
Electrochemical studies: Cyclic voltammogram
CV shows two oxidation peaks & one reduction peaks
D2d shows the lowest oxidation potential & also highest reduction potential
CV of dyes
0-0 calculation

## Slide 36
Natural Bond Orbital Analysis & calculation of reorganization energy
NBO | Donor | Linker | Acceptor
D1d | 0.068 | 0.069 | -0.136
D2d | 0.077 | 0.053 | -0.133
D3d | 0.084 | 0.045 | -0.128
Natural bond orbital analysis(NBO)
Dye | Λe / eV | Λh / eV | Λtotal / eV
D1d | 1.06 | 0.75 | 1.81
D2d | 0.94 | 0.76 | 1.70
D3d | 0.94 | 0.84 | 1.78
Reorganization energy
M06/6-31G(d) method
To understand charge distribution & electron transfer in D-π –A system
positive NBO value indicates that the donating ability of an electron donor unit and the negative NBO value represents the electron accepting ability by an electron acceptor unit.
The reorganization energy of dye is the extent of energy required due to the conformational reorganization of molecule induced by ICT from donor to acceptor.

## Slide 37
Dyes | VOC / V | JSC / mAcm-2 | FF |  / %
D1d | 0.711 | 2.89 | 0.49 | 1.02
D1d +CDCA | 0.697 | 3.72 | 0.68 | 1.75
D2d | 0.813 | 6.24 | 0.73 | 3.70
D2d +CDCA | 0.834 | 6.67 | 0.76 | 4.21
D3d | 0.789 | 4.55 | 0.73 | 2.62
D3d+ CDCA | 0.816 | 5.52 | 0.70 | 3.14
Photovoltaic Performance (I-V diagram)
Efficiency order (
Similar trends observed in , & .
Addition of co-adsorbent improved the performance in all the case indicates that CDCA reduces the dye aggregation on TiO2 surface.
Observations:

## Slide 38
Conclusions
D2d showed the highest power conversion efficiency of 4.21% in presence of CDCA.
From electrochemical studies, D2d dye showed lowest oxidation potential which is reflected in VOC (0.83 V; highest value)
D2d showed the highest molar extinction coefficient and highest driving force for electron injection and low reorganization energy among the other two dyes.
The above factors along with rigid & planar nature of carbazole donor contributed for the efficient ICT in the D-π-A system & hence its best performance compared to other donors.

## Slide 39
Thank you all for your kind attention !