## Slide 1: Direct conversion of methane to methanol by iron exchanged MFI Zeolite
May – June,2019

## Slide 2
Industrial Routes
Steam Reforming
Syn gas
Reactor
Methanol
∆HR = + 206 kJ mol-1
∆HR = - 92 kJ mol-1
Methane
Indirect Route
Methane
Direct Partial Oxidation Process
Methanol
∆HR = - 126 kJ mol-1
O2
Direct Route

## Slide 3: Selected catalyst for various routes of MeOH synthesis
Direct Partial Oxidation of Methane | Active catalyst | Oxidant | Xmethane (%) | SMeOH (%) | Yield (µmol gcat-1)
Willox et al | V2O5/SiO2 | N2O | 0.07 | 56.7 | 
Hutchings et al | H-ZSM-5 | H2O2 | 0.3 | 19 | 
Hutchings et al | Fe-ZSM-5(30) | H2O2 | 0.7 | 12 | 22
Hutchings et al | 2.5% Fe - ZSM-5(30) with 10umol of Cu2+ | H2O2 | 0.7 | 85 | 140
Hutchings et al | Fe-Silicalite-1 / Cu-Silicalite-1 | H2O2 | 10 | 93 | 168
Van Bokhoven et al | Cu-MOR | O2 |  |  | 84.3
R. F. Lobo et al | Cu-MOR | H2O |  | 97% | 
Hutchings et al | AuPd/TiO2 | H2/O2 |  | 68.2 | 46.1

## Slide 4: X-ray Diffraction Pattern of metal exchanged Silicalite-1

## Slide 5: N2 adsorption isotherms and textural properties
N2 adsorption isotherm of (a) Uncalcined Fe-Silicalite-1 (b) Calcined Fe-Silicalite-1
Sample | SBET (m2 /g) | VP (cm3 /g)
Un calcined Fe-Silicalite-1 | 196 | 0.086
Calcined Fe-Silicalite-1 | 286 | 0.111
Chart: 
| 114.39701275202135 | 81.170589108614934 | 56.205576969595171 | 38.624306481225595 | 28.126875139274748 | 22.26755353709056 | 18.421685595455507 | 15.684626845228436 | 13.640852004688206 | 12.09996628538979 | 10.825215531074225 | 9.6631796341356946 | 8.7190502250062067 | 7.922909024461581 | 7.2403148206617267 | 6.6577720192129606 | 6.1807277302895374 | 5.7713805654571164 | 5.3956454849166287 | 5.0652174080470616 | 4.7654566243656555 | 4.5056668270399554 | 4.2692394052993938 | 4.0507773847045332 | 3.8577097235916669 | 3.6851524784383942 | 3.5234480629295888 | 3.3667203379729451 | 3.2263047400065012 | 3.0950692658627408 | 2.9725302273415952 | 2.8625041332050474 | 2.7552505455821614 | 2.6518702954562681 | 2.5561082730486797 | 2.42090163314304 | 2.2610378156229216 | 2.1183897255229032 | 1.9873795872812963 | 1.8655574124369085 | 1.7553008368495797 | 1.6529670956391476 | 1.5578782708856538 | 1.4714835232882655 | 1.3879364968497292 | 1.3097750211356587 | 1.2340417987937746 | 1.1615144577319136 | 1.0938899691395219 | 1.029474716908892
 | 0.14113 | 0.14806 | 0.062603 | 0.021349 | 0.011547 | 0.010146 | 0.0090221 | 0.0090891 | 0.0081953 | 0.0087774 | 0.0084692 | 0.0072971 | 0.0060524 | 0.0069001 | 0.0067951 | 0.006386 | 0.0043787 | 0.0060914 | 0.0052689 | 0.0064246 | 0.004819 | 0.0037345 | 0.0051934 | 0.0049428 | 0.0049618 | 0.0027914 | 0.006993 | 0.0054899 | 0.0028823 | 0.0056574 | 0.0060054 | 0.0042971 | 0.0067599 | 0.0094645 | 0.0091367 | 0.0086523 | 0.0088782 | 0.01576 | 0.021484 | 0.023923 | 0.039871 | 0.049263 | 0.070561 | 0.1047 | 0.15647 | 0.23664 | 0.27828 | 0.20979 | 0.085002 | 0.004599
Pore Size Distribution of calcined Fe-Silicalite-1
rp (nm)
dV/dD(a.u)

## Slide 6: DRS-UV Spectra of Fe-Silicalite-1
A1
A3
A4
A2
Bruckner et al., J. Catal., 227 (2004), pp. 384-397
A1 - Framework Fe
A2 - Extra-framework Fe
A3 - fine iron oxide clusters
A4 - bulk iron oxide

## Slide 7: DRS-UV Spectra of Cu/Silicalite-1

## Slide 8: Catalytic testing of 0.5wt% Fe-Silicalite-1
S.No | Pressure | Temperature | H2O2 (M) | Copper nitrate conc. (umol) | Methanol (umol)
1 | 3bar | 70oC | 1 | 10 | 8
2 | 30bar | 50oC | 0.5 | - | 15
3 | 30bar | 50oC | 0.5 | 10 | 40
4 | 30bar | 50oC | 0.5 | 15 | 55
Hutchings et al., Angew. Chem., Int. Ed., 2012, 51, 5129–5133

## Slide 9: Active site – Iron Zeolite- complex
Ligand 1 – Diethylene triamine
Ligand 2 – Di-(2-picolyl) amine
Ligand 3 – N,N-dimethyl-N-
(pyrid-2-ylmethyl) ethylenediamine
Hutchings et al., Angew. Chem., Int. Ed., 2012, 51, 5129–5133

## Slide 10: Preparation of Ligand L3
Dalton Trans., 2016, 45, 11422-11436
Impure Ligand L3

## Slide 11: Preparation of diiron(III) complex
Dalton.Transac, 2016, 45, 11422-11436

## Slide 12: Electronic spectral data of [Fe2O(OAc)2(L)2]2+ in acetonitrile
1
2
3
1
2
3
band no | Bridged complex 1 | Bridged complex 2 | Bridged Complex 3 | Assignment
1 | 268 | 263 | 265 | π π* (LLCT)
2 | 350 | 347 | 350 | n π* (LMCT)
3 | 437 | 428 | 432 | d-d transition [4 T2 (4 D)]
J. Am. Chem. Soc., Vol. Ill, No. 21, 1989
Notes: 5 X 10-4 M

## Slide 13: Bond vibrational modes of Neat Fe-Complex
Complex | v(NH2 ) cm-1 | v(COO- ) free cm-1 | v(COO) bridged cm-1 | v(N-H ) cm-1 | v(Fe-O-Fe) bridged cm-1 | v(Fe-N ) cm-1
Fe-L1 | 3140 | 1585 | 1445 | 1356,1048 | 760 | 442
Fe-L2 | - | 1571 | 1432 | 1353,1052 | 769 | 435
Fe-L3 | 3149 | 1560 | 1438 | 1351,1051 | 768 | 438
K Nakamoto - Handbook of Vibrational Spectroscopy, 2006 - Wiley Online Library