## Slide 1
Photocatalytic oxidation of naphtalene in aqueous and organic solvents

## Slide 2
J. Catal. 2002, 211, 434-444
Selective oxidation of alcohols in gas phase using light activated TiO2

## Slide 3
Electric Vehicles Smart Fleets
Electric Unmanned aerial vehicles
ELECTRICAL VEHICLES

## Slide 4
1 MJ/Kg
2 hrs 250 Kg of batterie
7 hrs 260,000 Kg of batteries
ELECTRIC / HYBRID AIRCRAFT
43 MJ/Kg

## Slide 5
Nature Energy 4 (2019), 575-584
VISIBLE-LIGHT-DRIVEN COPRODUCTION OF DIESEL FUEL PRECURSORS AND HYDROGEN

## Slide 6
VISIBLE-LIGHT-DRIVEN COPRODUCTION OF DIESEL FUEL PRECURSORS AND HYDROGEN
Nature Energy 4 (2019), 575-584

## Slide 7
VISIBLE-LIGHT-DRIVEN COPRODUCTION OF DIESEL FUEL PRECURSORS AND HYDROGEN
Nature Energy 4 (2019), 575-584
Doped-ZnIn2S4 photocatalysts

## Slide 8
VISIBLE-LIGHT-DRIVEN COPRODUCTION OF DIESEL FUEL PRECURSORS AND HYDROGEN
Nature Energy 4 (2019), 575-584
3.3 mmol of H2 g cat-1 h-1
0.56 g of DPF g cat-1 h-1
AQY 15.2 %
2,5-DMF
2-MF
2,5-DMF + 2-MF
Ru-ZnIn2S4 photocatalyst

## Slide 9
VISIBLE-LIGHT-DRIVEN COPRODUCTION OF DIESEL FUEL PRECURSORS AND HYDROGEN
Ru-ZnIn2S4 photocatalyst
Nature Energy 4 (2019), 575-584

## Slide 10
VISIBLE-LIGHT-DRIVEN COPRODUCTION OF DIESEL FUEL PRECURSORS AND HYDROGEN
Ru-ZnIn2S4 photocatalyst
Nature Energy 4 (2019), 575-584
Radical mechanism
confirmed

## Slide 11
VISIBLE-LIGHT-DRIVEN COPRODUCTION OF DIESEL FUEL PRECURSORS AND HYDROGEN
Ru-ZnIn2S4 photocatalyst: role of Ru
Nature Energy 4 (2019), 575-584
Decreased band gap
Stabilization of e-/h+ pairs
Reduction of Ru ions to Ru(0) justifies slight deactivation

## Slide 12
Conventional synthesis of benzimidazoles:
Very toxic and
carcinogenic
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
T = 100 – 200 °C
Strong acidic conditions
Strong oxidants
Synthesis of natural products and pharmaceuticals (bactericides, anticarcinogens, peptic ulcera agents, etc.)
Metal complexes (homogeneous catalysts, sensors, etc.)

## Slide 13
Very toxic and
carcinogenic
T = 100 – 200 °C
Strong acidic conditions
Strong oxidants
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
Conventional synthesis of benzimidazoles:

## Slide 14
Alternative processes:
Less toxic reagents
Renewable and cheap solvent
[H]ads
hn, cat
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES

## Slide 15
Anatase
Brookite
Rutile
TiO2
TiO2-B,N
 | Composition (wt%) |  |  | Crystallite size (nm) |  |  | Surface area (m2 g-1)
 | Anatase | Brookite | Rutile | Anatase | Brookite | Rutile | 
TiO2 | 64 | 28 | 8 | 11 | 11 | 32 | 80
TiO2-B,N | 68 | 26 | 6 | 8 | 7 | 12 | 138
Mixture of polymorphs
High surface area
Improved by B,N doping
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
Inorg. Chim. Acta 520 (2021), n° 120289
TiO2-B,N

## Slide 16
Metal photodeposition
Metal/TiO2-B,N
Support +
metal nitrate
50% water- 50% ethanol
UV-vis irradiation
Pd 0.5wt%
Ag 0.5wt%
Pt 0.5wt%
Cu 1.0wt%
HAADF-STEM
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES

## Slide 17: Characterization of the M/TiO2-B,N
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
Inorg. Chim. Acta 520 (2021), n° 120289

## Slide 18: H2 production from ETHANOL 96%
Gas phase
Effect of:
Support
Metal
Doping TiO2, leaching is significantly reduced
More stable performances for TiO2-B,N supported catalysts
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
Cu/TiO2
Cu/TiO2-B,N
Inorg. Chim. Acta 520 (2021), n° 120289

## Slide 19: Synthesis of 2-methylbenzimidazole
Conditions:
60 mL DNB/NA 2mM in EtOH 96%
150 mg Pd/TiO2-B,N
Ar flow, 30°C
Simulated sunlight irradiation
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
Inorg. Chim. Acta 520 (2021), n° 120289

## Slide 20: Synthesis of 2-methylbenzimidazole
Conditions:
60 mL DNB/NA 2mM in EtOH 96%
150 mg Pd/TiO2-B,N
Ar flow, 30°C
Simulated sunlight irradiation
0
200
400
600
800
1000
1200
H
2
production rate
(
m
mol g
-1
h
-1
)
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
Inorg. Chim. Acta 520 (2021), n° 120289

## Slide 21
Inorg. Chim. Acta 520 (2021), n° 120289
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES

## Slide 22: Substituted 2-methylbenzimidazole
Br
Futher functionalization
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
Inorg. Chim. Acta 520 (2021), n° 120289

## Slide 23: 5-bromo-2-methylbenzimidazole
Br
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
Br-2-MBI
N-Et-2-MBI
2-MBI
Br-N-Et-2-MBI
Pt highly active and selective
Pd promotes hydrodehalogenation
Ag and Cu take long reaction time and selectivity is not satifactory
Inorg. Chim. Acta 520 (2021), n° 120289

## Slide 24: 5,6-dichloro-2-methylbenzimidazole
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
diCl-2-MBI
2-MBI
Cl-2-MBI
Pt highly active and selective
Pd promotes hydrodehalogenation
Inorg. Chim. Acta 520 (2021), n° 120289

## Slide 25: 5-carboxymethyl-2-methylbenzimidazole
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
COOMe-2-MBI
COOMe-
2-MBI
COOMe-
N-Et-2-MBI
COOMe-
N-Et-2-MBI
Inorg. Chim. Acta 520 (2021), n° 120289

## Slide 26
Photocatalytic reduction of CO2 to solar fuels

## Slide 27
Photocatalytic reduction of CO2 to solar fuels
pH = 7
Highly negative reduction potential arises from change in ibridization of C
Proton-Coupled Electron Transfer (PCET) are preferred

## Slide 28
Photocatalytic reduction of CO2 to solar fuels
Schematic of the possible CO2 adsorption
configurations on surfaces of photocatalysts
The reduction potentials for the PCET reactions are within the range of −0.7 to −0.2 V and are close to the reduction potential of water (−0.414 V at pH 7). The reduction products of CO2 (HCHO, CH3OH, and CH4) require multielectron transfer, whereas the reduction of water is a two-electron process. Reduction of water therefore competes with the reduction of CO2. Because of this, the extent of hydrogen generation is greater in liquid-phase reactions compared to vapor-phase reactions.

## Slide 29
Photocatalytic reduction of CO2 to solar fuels
Photocatalytic CO2 reduction on (a) Ag-NaTaO3:Ca, (b) Ag-NaTaO3:Sr, and (c) Ag-NaTaO3:Ba in the liquid phase under UV irradiation. Figure legends: hydrogen (open circle), oxygen (solid circle), and CO (triangle).
ChemSusChem 2017, 10, 112– 118

## Slide 30
Photocatalytic reduction of CO2 to solar fuels
(a) Electronic absorption spectra of nitridation products of Zn2GeO4 and (b) corresponding photocatalytic methane product activities. (c) Curve depicting the recyclability and stablitity of the photocatalyst.
Eur. J. Inorg. Chem. 2017, 2017, 2195– 2200

## Slide 31
Photocatalytic reduction of CO2 to solar fuels
Comparison of (a) density of states and (b) relative band positions in (001) and (101) facets of TiO2. (c) Photocatalytic CO2 reduction to CH4 with different ratios of (001) to (010) facets in TiO2.
TEM image of HF0 and (b and c) FESEM images of HF4.5 and HF9.
J. Am. Chem. Soc. 2014, 136, 8839– 8842

## Slide 32
Photocatalytic reduction of CO2 to solar fuels
(a) Schematic illustration of the process of charge transfer and CO2 reduction in Cu2ZnSnS4/TiO2 heterostructures. (b) Comparison of photocatalytic activities of Cu2ZnSnS4/TiO2 with different compositions and individual Cu2ZnSnS4 and TiO2.
RSC Adv. 2017, 6, 38964– 38971

## Slide 33
Photocatalytic reduction of CO2 to solar fuels
(a) Schematic illustration of the process of Z-scheme charge transfer and CO2 reduction in α-Fe2O3/Cu2O heterostructures. (b) Comparison of yield of CO production with varying the Cu content in these heterostructures.
ACS Appl. Mater. Interfaces 2015, 7, 8631– 8639

## Slide 34
Photocatalytic reduction of CO2 to solar fuels
Tandem CH3OH oxidation and CO2 reduction by Ag and Ru complex, respectively. [Ru(bpy)3]2+ derivative and TaON are light absorbers.
Ru catalyst on
visible light absorbing C3N4
Re catalyst and organic dye on TiO2.